| 1 | Manufacture & check pattern equipment, Locate, identify cast on test material per specification | NPAT-SOP-0100/ Section 4.2.2 | Test reports | Section 4.2.2 | NA | A1 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | Check chemical composition | QUAL-SOP-0048 Rev 5 | Test Certificate Report chem. from each ladle and weighted average. | Section 3.1 | Verify chemistry at outside laboratory. | A1 | R1 |  | ** |  |
| 3 | Heat treat | Heat – SOP 0100 Rev 8 and Note below | Heat charts | NA | Test material and sample material to be located in corresponding zone | A1 | R1 |  |  |  |
| 4 | Room Temperature Tensile Test including tensile, yield, elongation and elastic modulus | A703/A703M-03 | Test Certificate | Section 3.1 | 1 per zone/3 per casting – retain all test material* | A1 | R1 |  | ** |  |
| 5 | Cryogenic Tensile Test(77K) including tensile, yield, elongation and elastic modulus | A703/A703M-03 | Test Certificate | Section 3.1 | 1 per zone/3 per casting - retain all test material* | A1 | R1 |  | ** |  |
| 6 | Room Temperature Charpy Test | A703/A703M-03 | Test Certificate | Section 3.1 | 1 per zone/3 per casting - retain all test material* | A1 | R1 |  | ** |  |
| 7 | Cryogenic Charpy Test (77K) | A703/A703M-03 | Test Certificate | Section 3.1 | 1 per zone/3 per casting - retain all test material* | A1 | R1 | Test Hold W1 | ** |  |
| 8 | Sample material, not less than 3”x 3”x 1” 3 pieces per zone | NA | NA | Section 4.2.2.4 | Submit with casting | A1 | R1 |  |  |  |
| 9 | Weld material testing Tensile and charpy each lot. Test at –320 F and +70 F Check chemical composition | A703/A703M-03 QUAL-SOP-0048 Rev 5 | Test Certificate Test Certificate | Section 3.1 | Retain all test material* | A1 | R1 |  | ** |  |
| 10 | Weld repair Welds <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) Welds <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 | CQP-60 Rev 5 | Map major welds | Weld map Send map within 24 hours of welding | Major weld is 20% of thickness or 1” whichever is less or 10” square. Also report multiple repairs of the same defect | H | R1 | W2- 5 day notice |  |  |
| 11 | Initial interim layout inspection by Lawton | NA | NA | NA | Performed on –1 castings by Lawton | NA | R1 | W2 5 day notice |  |  |
| 12 | Interim layout inspection | Layout SOP 0100 Rev 0 | File | NA | Performed on –2 through –6 castings | A2 | R1 | W2 5 day notice |  |  |
| 13 | Sand Blast | BLAS SOP 0100 Rev 6 | NA | NA | Remove all blast material from casting | NA |  |  |  |  |
| 14 | Liquid Penetrant Examination – High Stressed Areas | CQP-300 Rev 10 | Test Certificate ASTM A903M, S1 | A903/A903M Level I | Performed by ASNT Level II | A1 | R1 | W2 5 day notice |  |  |
| 15 | Liquid Penetrant Examination – Low Stressed Areas | CQP-300 Rev 10 | Test Certificate ASTM A903M, S1 | A903/A903M Level II | Performed by ASNT Level II | A1 | R1 | W2 5 day notice |  |  |
| 16 | Final visual inspection | CQP-500 Rev 4 | Inspection report & test certificate | A802/A802M Level III | Performed by ASNT Level II | A2 | R1 | W2 5 day notice |  |  |
| 17 | Radiographic examination | CQP-401 Rev 5 X-ray at MQS PROCEDURE 20.H.010 REV 0 | Reader sheets and film | MSS SP-54 | Performed by ASNT Level II | A1 | R1 | W2 5 day notice |  |  |
| 18 | Magnetic permeability inspection | CQP- Mag Perm – 0100 R1. Must also meet S24, A703and S1 of A800 | Test Certificate and weld map list | Less than 1.02 | Test 6 inch grid and all weld repairs | A1 | R1 | W2 5 day notice |  |  |
| 19 | Heat treat – Stress Relief | Heat – SOP 0100 Rev 8 and Note below | Heat charts | NA | NA | A1 | R1 |  |  |  |
| 20 | Preparation for shipment |  |  |  |  | A1 |  |  |  |  |
| END | Release for shipment | Quality Plan / Customer specifications | Inspectors Release |  |  |  | H |  |  |  |

* submit to PPPL

** Submit NCR to EIO for these non conformances

# Inspection surveillance Codes

A1   =	100% Inspection Performed (measurement or pass / fail)			Company References (Columns A, B, C …)

A2   =	Sample Inspection Performed

W1  = 	100% Witness Inspection						A:	MetalTek

W2  =	Sample Witness Inspection – Requires five day notice		B: 	Energy Industries of Ohio

S      =	General surveillance of operations					C: 	DCMA

R1    =	100% Review of Documentation                                                        D:        Other

R2    =	Sample Review of Documentation

H     =	Manufacture Hold Point

Heat Treat Procedure:

SOLUTION ANNEAL.  MAKE SURE TO BLOCK ALL FLANGES OF FORM AND RACETRACK TO MINIMIZE CREEP DISTORTION. Soak Temp:  2050F, Soak Time:  4HR + 1/2 HR/IN, Quench Type:  Air Cool     MAKE SURE TEST MATERIAL IS PLACED IN THE CORRECT ZONE.

Stress Relief Procedure:

Load casting into cold furnace.  Ramp up to 1100 F at rate of 200 F per hour.  Hold at temp 4 hours.  Furnace cool to 500 F at 50 F per hour.  Air cool.  Submit furnace charts to QA.