Pg 1 of 2

Energy Industries of Ohio

Corrective Action Report/Request            ID#0001

Date 12-28-05

Due: N/A

Initiated By: Peter Djordjevich

Issue/Non Conformance:  Metallurgical Defects C2/C3

Root Cause: C2 linear indications possibly missed during initial

inspection due to location. Original surface linear indications may

have been aggravated by further excavations. C3 casting porosity/

shrinkage revealed itself during machining. Review of film shows

C3 to be within acceptable casting limits.

Corrective Action: Prior to initiation of any rework team members

are to be consulted to document, identify, and approve the course of

action. Inspection efforts have been enhanced to include added

personnel  for LPI inspection and verification at MTK. Request

DCMA to take more of an active role during LPI.

Verification of Corrective Action: Per team discussions the above has

been implemented.

Pg 2 of 2

Completion / Verification Date 01-03-06

Signature EIO Quality

Peter Djordjevich