| NOTES: Repair of A-1 Coil Casting Date:1-11-06 |  |  |  |  |  | # SUPPLEMENTAL ROUTING CARD |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | PART NUMBER: A-1 Coil |  |  |  | SERIAL NUMBER: A-1 |  |  |  | ## AUTHORITY C Ruud |  |  |
| OPER NUMBER |  |  |  |  |  |  |  |  |  | OPERATOR SIGN/DATE |  |  |
| 10 | WELD SOP 0100 REV 7 |  | Verify with Engineering before and after performing work. EXCAVATE AREA WITH EXCESS MATERIAL. |  |  |  |  |  |  |  |  |  |
| 20 | GRIND GCHI SOP 0100R2 |  | HAND GRIND AREA. |  |  |  |  |  |  |  |  |  |
| 30 | SAND BLAST BLAS SOP 0100R6 |  | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |  |  |  |  |  |  |  |
| 40 | L.P. EXCAVATION CQP-300 REV 10 |  | L.P. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE _______AND GO TO STEP 40 . IF REJECTED CHECK HERE ______ RETURN TO STEP 20. |  |  |  |  | LP - LEVEL II |  |  |  |  |
| 50 | VISUAL INSPECTION CQP-500 REV 4 |  | VISUALLY INSPECT ACCORDING TO ASTM A802 LEVEL 3 ALL CONDITIONS. IF OK CHECK HERE _______. IF REJECTED MARK AND REPAIR BY GRINDING. DO NOT PROCEED UNTIL ACCEPTABLE. MUST BE PERFORMED BY LEVEL II in VT. |  |  |  |  | VT - LEVEL II |  |  |  |  |
| 60 | MAG PERM INSPECTION SOP MAG PERM 100, REV 1 |  | PERFORM MAG PERM TESTING WITH SEVRIN GAUGE. ACCEPTANCE 1.02. CHECK THE ENTIRE SURFACE ON A 6”BY6” GRID. REPORT RESULTS. USE A 6” SQUARE BLOCK TO INDICATE TEST LOCATIONS AND RECORD RESULTS. COMPLIANT AREAS WILL NOT BE MARKED. MARK NONCOMPLIANT AREAS WITH AN “X” FOR REPAIR. GRIND UNTIL ACCEPTABLE. OK CHECK HERE _____AND GO TO STEP 70. |  |  |  |  |  |  |  |  |  |
| 70 | PACK AND SHIP |  | PACKAGE AND SHIP TO MAJOR TOOL. MAKE SURE PROPER MARKINGS ARE PRESENT. PART NUMBER, SERIAL NUMBER A-1, AND FOUNDRY MARK, CERT NUMBER |  |  |  |  |  |  |  |  |  |

- Attachment to Supplemental router for A-1

- Differences between A-1 & A-2

This detail is acceptable, leave as is.

This is excess material, remove.

Detail D on A-1 – MTM to machine flat

A-1

See engineering for the material to be removed from this boss.

A-2 correct