Document reviewed: D-NCSX-MCF-002

Title:  MC Fabrication- Winding Station Activities for the Twisted Racetrack Coil

Date: July 8, 2005

Attendees: Frank Terlitz, Pete Szara, Mike hause and Buddy Kearns

- Add Kapton to edges of casting prior to mold release.  The Kapton on the cladding back cracks during forming.  This will correct that problem.  (Station 1 activity)

- Increase the length of upper shafts for conductor spools so that a crane can be used for loading spools.

- During the Groundwrap installation, ensure that the GW is positioned high enough so that it does not become trapped behind the upper most turns.

- Procure spare drive gears.  Several teeth were lost during the TRC winding operations.

- Periodically recheck the torque of the clamps.  The conductor creeps.

- When working the conductor to tighten or to reposition, it is important to work from the coil side to the conductor spool.

- Add to procedure that a metal sheet was used to protect the coil during soldering of the cooling lines.

- Procure 1/16 in. diameter solder for soldering the cooling tubes.  1/8 inch diameter solder was used for the TRC.

- Ensure that the flux loops are insulated prior to receipt.  The TRC loops were varnished in-house resulting in globs of varnish along the length of the flux loop.

- Add to procedure that the chill plates need to be punched in the area that the sprues are being installed.

- Add to procedure to ensure that the sprues/fittings are properly oriented on the coil to minimize any trapped air volumes on the coil during VPI.

- Add to procedure to sling and rope lower the guide rollers to the floor during the assembly/disassembly of the ring/casting into the turning fixture.  This will eliminate straining the backs of the technicians.

- Remove reference to French toast for structural wall and add chopped glass and epoxy (“Cotton Candy”) as alternative shell.

- Add additional tapped holes to side bars to support the “Cotton candy” structural shell.