March 26, 2005

To: Brad Nelson and Dave Williamson

From: Wayne Reiersen

Subject: Critical issues for the modular coils

As I was updating the critical issues list, I was struck again by the amount of work remaining in the modular coil area outside of completing fabrication drawings.  These critical issues are shown in Table 1.  The entry (14-1) deals with developing reference materials properties and design allowable for the modular coils.  We have done a lot of material testing for the modular coil conductor and casting alloy.  We have learned that the conductor shear modulus in the 3-point bend tests appears to be MUCH lower than anticipated.  In tensile tests, the casting alloy elastic modulus was about 2/3 of what we would expect for a wrought alloy of similar composition.  We just completed cyclic tensile testing of the short racetrack coils at PPPL last week with the implications on design allowables TBD.  Additional 3-point bend tests of the beam specimens at ORNL are still planned.  Fracture constants of the casting alloy are also still TBD.  The bottom line is that testing results have not always been what we expected and we still do not have a reference, documented set of material properties and design allowables for the analysts to use.  Near as I can tell - and I may be wrong - they are using their own “best guesses” at what these should be.  The question I have is simple – is there a plan for translating the test results into a documented set of reference material properties and design allowables which the analysts will use in completing their design basis analyses?

The second entry has to do with acceptance criteria for local high permeability zones.  I expect that this work was done but I do not recall what the final acceptance criteria were.  I will follow up with Malinowski.

The third entry has to do with completing the modular coil final design.  We have been focused on staying ahead of the procurements – developing specs and fabrication drawings – and that is the way we planned our remaining design reviews.  However, there is clearly a lot of other work that remains for completing modular coil final design.  A comprehensive list would include.

- Technical procurement packages provided – includes all specifications and fabrication drawings required to support procurement or in-house fabrication of Modular Coil System (WBS 14) components.  Shims, bolts, and insulating breaks are particular concerns.

- Interface documentation finalized– All interfaces defined and documented to the satisfaction of interfacing WBS Managers.

- All chits from previous design reviews closed out.

- A complete set of design basis calculations (including a FMECA) developed, documented, checked, and posted along with properly archived data files.

- A comprehensive bill of materials developed for WBS 14 that can be used to verify that each part has been ordered and received.

- A schedule for developing assembly and test procedures in Title III that is consistent with project need dates.

There should be no surprises on this list.  Please make sure that the activities required to provide these deliverables are identified in your job so that we can measure progress towards their completion.  The activities should be completed and addressed at one of the remaining FDRs.

Thanks for your cooperation.  Please advise if there is anything we are missing.

Table 1 - Modular coil critical issues

Cc: Neilson, Strykowsky, Simmons