NCSX Modular Coil Inner Leg Weld Requirements and Determination of Sm

Compendium of Information:

Weld Configuration:

1.  Stelalloy and weld wire chemical composition

2.  Specified properties for Stelalloy and the weld wire (ref.  NCSX-CSPEC-101-03-14).

- Data on the actual casting  & weld material properties

- Derivation of Sm:  Per the NCSX Structural Design Criteria, Sm shall be the lesser of 1/3 of the ultimate strength or 2/3 of the yield strength at temperature.  Since the weld region includes the Stelalloy casting,  weld metal, HAZ, and shims that will likely be made of 316-LN, the strength values shall be the lesser of these.

At this time, 316-LN for the shim material has not been finalized, so for the present we shall use  the lowest values between the Stellalloy and the weld material at 77K.  For the yield, this is 93.2 ksi for the C2 casting;  2/3 of yield =61.5 ksi.  The lowest ultimate strength is 157.5 for the weld wire;  1/3 of this =52.5, so this is what we shall use.  We’ll have to re-visit this after the shim material is determined.

A “knock down” factor of 0.6 shall be applied to this, since it is a butt joint. Therefore, the Sm=0.6*52.5=31.5 ksi.

# Text boxes

Winding form (Stelalloy)

316-LN shim

TIG welds