EVERSON TESLA INC.

# Manufacturing Process Outline/Traveler

# For the

# PPPL NCSX TF COIL PROJECT

# Coil Serial Number:

Everson Tesla Inc. #	53028			Work Order#

DWG # & Rev.	SE131-003 Rev 1   	Date:	4/07/06

Specification    NCSX CSPEC-131-01-01       Date: 4/13/06

NCSX-SOW-131-03-01          Date: 4/13/06

Customer:	Princeton Plasma Physics Lab.

PO Box CN-17

US Rte 1 North at Sayre Drive

Princeton, NJ 08543

PPPL Purchase Order Number: 	S006639 	Date:	5/01/06

| Original Authors: John Stafiniak | APPROVED BY (Signature & Date) |
| --- | --- |
| Date: Preliminary | Project Engineer: |
| Revised by: | Manufacturing Rep: |
| Revision Date: | Quality Assurance: |
| Revision #: | PPPL Rep : |

# Revision Table

| Revision | Description | Date |
| --- | --- | --- |

1.0	Scope

This MPO/Traveler along with QA Plan – 53028-QAP address the testing and Quality Assurance procedures to deliver a 12 turn, 4 layer ( 3 turns/layer) , vacuum impregnated “D” shaped magnet coil to PPPL in accordance with the following drawings and specification:

PPPL Drawing #		                       Description

SE131-003 Rev2                                      TF Coil Final Assembly

SE131-005 Rev2                                      TF Coil Ground Wrapped Assembly

SE131-035 Rev2                                      TF Coil Winding Assembly/Details

NCSX_CSPEC-131-01-02                       TF Coil Assembly

NCSX-SOW-131-03-01                           TF Coil Assembly

# All non-conformances will be directed to QA or the Engineer.

It is the intent of this MPO to fabricate the coils in strict accordance with the drawings and specifications and meet the requirements of Princeton Plasma Physics Laboratory.

# GENERAL NOTES FOR COIL FABRICATION:

Correct errors by line, signature, and date.  Do not write over or use white out !

No repair of any discrepancy shall be initiated without prior approval from PPPL &

Engineer.  All discrepancies require an NCR.

All work up to and including installation of the coil into the mold must be performed in the

designated PPPL Cleanroom.

Clean, lint-free gloves should be worn at all times when handling the conductor

or insulation.

Coil parts that are inadvertently handled with bare hands or otherwise soiled must be

cleaned with acetone.

Take protective measures to prevent contamination. Keep parts and conductor covered at all

times. Also cover winding during work stoppage.

Keep metal cuttings and filings out of winding, leads and insulated conductor during metal

cutting, filing, sanding and polishing operations.

Never use forced air to remove particles or debris.  Use a vacuum.

Round all sharp edges on conductor (.02" radius typical) that contact insulation.

Fill all voids in the coil with clean fiberglass roving or cloth or NEMA G-11CR. G-11CR must be  sanded on all sides with heavy grip non-conductive sand paper.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

All Everson Tesla safety procedures must be followed.

2.0	Materials and Parts

The following provides a list of the parts and materials required to fabricate the coil:

| Item | Part # | Qty coil | Description |
| --- | --- | --- | --- |
| 1 | * SC131-014 | 4 RLS | .709” x .966” x .312”ID x .039”CR C10700 Copper |
| 2 | Cust. Supplied | AR | 1” x .0035” Adhesive Kapton Tape |
| 3 | Cust. Supplied | AR | 1” x .007” S2 Glass Tape |
| 4 | SE131-032 | 1 | G-11 Filler |
| 5 | SE131-031 | 1 | G-11 Filler |
| 6 | SE131-041 | 1 | G-11 Filler |
| 7 | SE131-054 | 1 | Short Lead |
| 8 |  |  |  |
| 9 |  |  |  |
| 10 |  |  |  |
| 11 |  |  |  |
| 12 |  |  |  |
| 13 |  |  |  |
| 14 |  |  |  |
| 15 |  |  |  |
| 16 |  |  |  |
| 17 |  |  |  |
|  | * Material Certs Req’d |  |  |

3.0	Fabrication Process

3.1	Coil Winding

The TF magnet coil is comprised of 4 layers with 3 turns/layer of .709”x.966” wound the “hard way”– each layer is wound from continuous conductor (no splices). There are three brazed splices connecting the four layers. The turn to turn insulation is comprised of one layer half-lapped of 1”x .0035” thick adhesive Kapton tape and three layers half-lapped of   1”x.007” S2 glass tape.

| Operation-001 | Layer 1Conductor Inspection |
| --- | --- |

.709 “+/- .005”  __________        X       .966” +/- .005” __________

.312” ID +/- .005”       __________

Check Conductor Hole a min. of 12” deep with q- tip to verify ID was cleaned:  ____________

Hardness Check “F” scale(60-82):  ______5ft from end ______center ______5ft from opp end

Verify Kapton tape on taping machine is 1” x .0035” _____________

Verify Glass tape on taping machine is 1” x .007” ______________

Lot No.______________           Spool No. ______________

QA Signature and Date:

| Operation-002 | Layer 1 Winding |
| --- | --- |

NOTE: White (Lint Free) gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Place copper roll on  dereeler turn table.

Spread turns using plastic or G-10 wedges.

Check  conductor and remove any nicks or  burrs with emery paper or scotchbrite while using a vacuum to catch any  slivers or dust.

Wipe-down conductor with acetone.

Signature and Date:

Cover cleaned conductor with plastic and seal with tape.

Butt-splice conductor to previous conductor roll by torch brazing. This will provide a means for         pulling conductor thru tensioner and taping machine. After conductor reaches the winding machine,  cut away the butt splice along with 1 foot of copper from either side of the butt-splice. Give cutout section to QA to verify all annealed copper was removed.

Disgard plastic used to wrap conductor.

Signature and Date:

Hardness of cutout section (60-82Rf):  12” left of torch braze_______

12” right of torch braze_______

QA Signature and Date:

Prep end of conductor for the layer to layer splice by facing-off end of conductor and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .570” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

Measure 4 ft +/- 1” from end of conductor to center of layer to layer offset. Using fixture 53028-

900-A and the enerpac C-press at 8000PSI, press the layer to layer offset into the conductor.

Remove any burrs or scratches with emery or scotchbrite and vacuum to catch dust. Wipe with

Acetone. Hand insulate conductor with one layer half-lapped of  kapton tape and three layers

half lapped of glass tape up to taping machine.

Signature and Date:

Verify kapton tape is 1” x .0035” and glass tape is 1” x  .007”.

Signature and Date:

This layer will be wound in the counterclockwise direction. Prep winding fixture by checking

winding fixture scribe line marked “offset center”.  Place G-11 filler SE131-032 as shown on     drawing  SE131-035 sheet 4  Section D-D. Clamp end of conductor to winding

fixture. Start taping machine and wind three turns with 400PSI (3450lbs) tension on load cell.

While winding , clamp conductor to winding fixture every three to four feet.  After ¾ to 7/8 turn and again after turn 1 ¾ to 1 7/8 turn measure and press the turn to turn offset into the conductor using fixture 53028-800-A and Enerpac “C” press at 8000PSI. Reinsulate offset area. At the end of turn three, clamp the conductor to the winding fixture.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify filler SE131-032 was sanded.

Signature and Date:_______________________

Check overall conductor plus insulation build a minimum of once per turn;

Turn # 1 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 2 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 3 – 1.064”+/-.010 ________ X .807”+/- .010__________

A minimum of once per turn check for gaps no larger than .020” between turns or turn and fixture(this does not include the long straight section which will be bumped into place after completiuon of winding)  and that conductor is not visibly twisted;

Turn #1 - Pass_________   Fail_______

Turn #2 -  Pass_________   Fail_______

Turn #3-    Pass_________   Fail_______

Signature and Date:

QA verification of offset area  reinsulation.

Layer to layer offset:______________________QA Signature and Date

Turn 1 offset:_____________________________ QA Signature and Date

Turn 2 offset:______________________________ QA Signature and Date

Prep end of short lead SE131-054 for brazing to the end of Layer 1 Turn 3 by facing-off end of lead and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .570” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

Place short lead in position on winding fixture with center of .500” dia hole in lead on center of     winding fixture (see sheet 2 of dwg SE131-035). Mark end of lead on turn 2 and/or winding fixture – this mark will be transferred to turn 3 when it is brought into position. Remove lead and wind turn 3 into position – transfer mark that represents the end of the lead to turn 3. Prep end of conductor for lead brazing by facing-off end of conductor (up to the mark made above) and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .570” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

| Operation-003 | Braze Short Lead Water Fitting |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of lead with bottle brush and acetone..

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Torch braze brass water fitting to lead using SP15 silfos rod. Position as shown on dwg SE131-003 sheet 4 of 5.

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Clean entire lead and remove any sharp edges by filing and buffing with scotchbite pads.

Signature and Date:

| Operation-004 | Braze Short Lead to Layer 1 |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of conductor with bottle brush and acetone a minimum of 8” deep.

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Position brazing fixture 53028-700.

Place ferrule, silfos rings, silfos wafer, and silfos 3-sided hairpins as shown on drawing SE131-035 sheet 4 of 5.

Close brazing fixture with 80PSI on air cylinder.

Check joint for a max. gap of .002”- adjust fixture if necessary.

Check that misalignment between conductors is not greater than .006”.

(use straight edge and feeler gage on all 4 sides)

Stencil target for infrared thermometer on copper using 1/2”dia template and high temp. paint.

Center brazing coil around joint using ceramic spacers.

Aim infrared thermometer on target.

Turn cooling water on to brazing fixture and Robitron.

Turn on main power switch to Robitron.

Turn on circulating pump.

Turn DC power on.

Use foot control to start brazing cycle.

Robitron will turn off automatically at end of timed cycle.

Record the following :

Power-            ________          Frequency-                 ________

Voltage-          ________           Time @ full power-    ________

Total Time -     ________           Max. Temp Reached-  ________

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Signature and Date:

Attach tension fixture equally spaced around braze joint.  This fixture uses two 5 ton cylinders @  4250PSI to apply 8500lbs of tension on the braze joint during the helium leak test.    Wrap splice joint with plastic and insert helium leak check sniffer. Purge conductor with helium then pressurize to 50psi. Leak check to 10-6. After leak check is complete, purge conductor with nitrogen.

Leak Detector; Model__________            Serial #_____________

Leak Rate:		(Spec= <10-5 cc/sec)

Note: Joints failing this test must be cut out beyond the heat affected zone and re-brazed.

Signature and Date:

Check Rockwell Hardness  (55F min annealed, 60-82F unannealed);

¼”either side of joint-  ________      2” Left of Joint -          ________

2” Right of Joint -        ________      3” Left of Joint -          ________

3” Right of Joint -         ________     4” Left of Joint -     ________

4” Right of Joint -        ________

QA Signature and Date:

Insulate lead with one layer ½ lapped .0035”x1.0” adhesive kapton and three layers ½ lapped  .007”x 1.0” glass tape.  Two layers of 5-6” wide kapton tape may be used in place of the 1” half lapped kapton in the heavy section of the lead. Clamp lead in place. Insert filler SE131-041. Material may be removed if there is interference. Fill gaps with glass tape.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify filler SE131-041 was sanded.

Signature and Date:_______________________

| Operation-005 | Layer 2Conductor Inspection |
| --- | --- |

.709 “+/- .005”  __________        X       .966” +/- .005” __________

.312” ID +/- .005”       __________

Check Conductor Hole a min. of 12” deep with q- tip to verify ID was cleaned:  ____________

Hardness Check “F” scale(60-82):  ______5ft from end ______center ______5ft from opp end

Verify Kapton tape on taping machine is 1” x .0035” _____________

Verify Glass tape on taping machine is 1” x .007” ______________

Lot No.______________           Spool No. ______________

QA Signature and Date:

| Operation-006 | Layer 1 to Layer 2 Splice |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Place copper roll on  dereeler turn table.

Spread turns using plastic or G-10 wedges.

Check  conductor and remove any nicks or  burrs with emery paper or scotchbrite while using a vacuum to catch any  slivers or dust.

Wipe-down conductor with acetone.

Signature and Date:

Cover cleaned conductor with plastic and seal with tape.

Butt-splice conductor to previous conductor roll by torch brazing. This will provide a means for         pulling conductor thru tensioner and taping machine. After conductor reaches the winding machine,  cut away the butt splice along with 1 foot of copper from either side of the butt-splice.

Give cutout section to QA to verify all annealed copper was removed.

Disgard plastic used to wrap conductor.

Signature and Date:

Hardness of cutout section (60-82Rf):  12” left of torch braze_______

12” right of torch braze_______

QA Signature and Date:

Prep end of layer 2 conductor for the layer to layer splice by facing-off end of conductor and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of conductor with bottle brush and acetone a minimum of 8” deep.

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Position brazing fixture 53028-700.

Place ferrule, silfos rings, silfos wafer, and silfos 3-sided hairpins as shown on drawing SE131-035 sheet 4 of 5.

Close brazing fixture with 80PSI on air cylinder.

Check joint for a max. gap of .002”- adjust fixture if necessary.

Check that misalignment between conductors is not greater than .006”.

(use straight edge and feeler gage on all 4 sides)

Stencil target for infrared thermometer on copper using 1/2”dia template and high temp. paint.

Center brazing coil around joint using ceramic spacers.

Aim infrared thermometer on target.

Turn cooling water on to brazing fixture and Robitron.

Turn on main power switch to Robitron.

Turn on circulating pump.

Turn DC power on.

Use foot control to start brazing cycle.

Robitron will turn off automatically at end of timed cycle.

Record the following :

Power-            ________          Frequency-                 ________

Voltage-          ________           Time @ full power-    ________

Total Time -     ________           Max. Temp Reached-  ________

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Signature and Date:

Attach tension fixture equally spaced around braze joint.  This fixture uses two 5 ton cylinders @  4250PSI to apply 8500lbs of tension on the braze joint during the helium leak test.    Wrap splice joint with plastic and insert helium leak check sniffer. Purge conductor with helium then pressurize to 50psi. Leak check to 10-6. After leak check is complete, purge conductor with nitrogen.

Leak Detector; Model__________            Serial #_____________

Leak Rate:		(Spec= <10-5 cc/sec)

Note: Joints failing this test must be cut out beyond the heat affected zone and re-brazed.

Signature and Date:

Check Rockwell Hardness  (55F min annealed, 60-82F unannealed);

¼”either side of joint-  ________      2” Left of Joint -          ________

2” Right of Joint -        ________      3” Left of Joint -          ________

3” Right of Joint -         ________     4” Left of Joint -     ________

4” Right of Joint -        ________

QA Signature and Date:

Insulate splice area with one layer ½ lapped .0035”x1.0” adhesive kapton and three layers ½ lapped  .007”x 1.0” glass tape.

Signature and Date:

QA Signature and Date:_____________________________

| Operation-007 | Layer 2 Winding |
| --- | --- |

NOTE: White (Lint Free) gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

This layer will be wound in the clockwise direction.  Place G-11 filler SE131-031 as shown on     drawing  SE131-035 sheet 4  Section D-D. Start taping machine and wind three turns with 400PSI (3450lbs) tension on load cell.

While winding , clamp conductor to winding fixture every three to four feet.  After ¾ to 7/8 turn and again after turn 1 ¾ to 1 7/8 turn, and again after turn 2 ¾ to 1 7/8 turn, measure and press the turn to turn offset into the conductor using fixture 53028-800-A and Enerpac “C” press at 8000PSI. Reinsulate offset area. At the end of turn three, continue winding 6 ½ ft past the center line of the winding fixture.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify filler SE131-031 was sanded.

Signature and Date:_______________________

Check overall conductor plus insulation build a minimum of once per turn;

Turn # 1 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 2 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 3 – 1.064”+/-.010 ________ X .807”+/- .010__________

A minimum of once per turn check for gaps no larger than .020” between turns or turn and fixture(this does not include the long straight section which will be bumped into place after completiuon of winding)  and that conductor is not visibly twisted;

Turn #1 - Pass_________   Fail_______

Turn #2 -  Pass_________   Fail_______

Turn #3-    Pass_________   Fail_______

Signature and Date:

QA verification of offset area  reinsulation.

Turn 1 offset:_____________________________QA Signature and Date

Turn 2 offset:_____________________________ QA Signature and Date

Turn 3 offset:______________________________ QA Signature and Date

Prep end of layer 2 for brazing to the end of Layer 3 by facing-off end of lead and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

| Operation-008 | Layer 3 Conductor Inspection |
| --- | --- |

.709 “+/- .005”  __________        X       .966” +/- .005” __________

.312” ID +/- .005”       __________

Check Conductor Hole a min. of 12” deep with q- tip to verify ID was cleaned:  ____________

Hardness Check “F” scale(60-82):  ______5ft from end ______center ______5ft from opp end

Verify Kapton tape on taping machine is 1” x .0035” _____________

Verify Glass tape on taping machine is 1” x .007” ______________

Lot No.______________           Spool No. ______________

QA Signature and Date:

| Operation-009 | Layer 3 Winding |
| --- | --- |

NOTE: White (Lint Free) gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Place copper roll on  dereeler turn table.

Spread turns using plastic or G-10 wedges.

Check  conductor and remove any nicks or  burrs with emery paper or scotchbrite while using a vacuum to catch any  slivers or dust.

Wipe-down conductor with acetone.

Signature and Date:

Cover cleaned conductor with plastic and seal with tape.

Butt-splice conductor to previous conductor roll by torch brazing. This will provide a means for         pulling conductor thru tensioner and taping machine. After conductor reaches the winding machine,  cut away the butt splice along with 1 foot of copper from either side of the butt-splice.

Give cutout section to QA to verify all annealed copper was removed.

Disgard plastic used to wrap conductor.

Signature and Date:

Hardness of cutout section (60-82Rf):  12” left of torch braze_______

12” right of torch braze_______

QA Signature and Date:

Prep end of conductor for the layer to layer splice by facing-off end of conductor and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

Measure 5 ft 2” +/- 1” from end of conductor to center of layer to layer offset. Using fixture           53028-900-A and the enerpac C-press at 8000PSI, press the layer to layer offset into the conductor. Remove any burrs or scratches with emery or scotchbrite and vacuum to catch dust. Wipe with Acetone. Hand insulate conductor with one layer half-lapped of  kapton tape and three layers  half lapped of glass tape up to taping machine.

Signature and Date:

Verify kapton tape is 1” x .0035” and glass tape is 1” x  .007”.

Signature and Date:

This layer will be wound in the counterclockwise direction. Prep winding fixture by checking

winding fixture scribe line marked “offset center”.  Clamp end of conductor to winding

fixture. Start taping machine and wind three turns with 400PSI (3450lbs) tension on load cell.

While winding , clamp conductor to winding fixture every three to four feet.  After ¾ to 7/8 turn and again after turn 1 ¾ to 1 7/8 turn measure and press the turn to turn offset into the conductor using fixture 53028-800-A and Enerpac “C” press at 8000PSI. Reinsulate offset area. At the end of turn three, clamp the conductor to the winding fixture.

Check overall conductor plus insulation build a minimum of once per turn;

Turn # 1 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 2 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 3 – 1.064”+/-.010 ________ X .807”+/- .010__________

A minimum of once per turn check for gaps no larger than .020” between turns or turn and fixture(this does not include the long straight section which will be bumped into place after completiuon of winding) and that conductor is not visibly twisted;

Turn #1 - Pass_________   Fail_______

Turn #2 -  Pass_________   Fail_______

Turn #3-    Pass_________   Fail_______

Signature and Date:

QA verification of offset area  reinsulation.

Layer to layer offset:______________________QA Signature and Date

Turn 1 offset:_____________________________ QA Signature and Date

Turn 2 offset:______________________________ QA Signature and Date

| Operation-010 | Layer 4Conductor Inspection |
| --- | --- |

.709 “+/- .005”  __________        X       .966” +/- .005” __________

.312” ID +/- .005”       __________

Check Conductor Hole a min. of 12” deep with q- tip to verify ID was cleaned:  ____________

Hardness Check “F” scale(60-82):  ______5ft from end ______center ______5ft from opp end

Verify Kapton tape on taping machine is 1” x .0035” _____________

Verify Glass tape on taping machine is 1” x .007” ______________

Lot No.______________           Spool No. ______________

QA Signature and Date:

| Operation-011 | Layer 2 to Layer 3 Locking Braze Joint |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Place and of Layer 2 Turn 3 into position, this should be 6 ½ feet from center of winding fixture.

Place Turn 3 of Layer 3 into position but over top of the end of Layer 2 Turn 3.

Scribe Turn 3 of Layer 3 with machined end of Layer 2 Turn 3.

Machine end of  Layer 3 Turn 3 .125” shorter than scribe line to account for conductor stretch and scribing error.

Prep end of conductor for the layer to layer splice by facing-off end of conductor and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering ..709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

The ends of the conductors and an additional ¼ turn in each direction will need to be raised above the coil to create sufficient space to get the brazing fixture into postion. After the brazing fixture is in position the fixture along with the conductors must be pulled toward the center of the coil (using ratchet straps) to close up the splice. Wrap raised sections of turns with mylar tape to protect turn insulation during repositioning of turns.

Braze Locking Joint:

Clean silfos and copper with scotchbrite and acetone. Scrub bore of conductor with bottle brush and acetone a minimum of 8” deep.

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Position brazing fixture 53028-700.

Place ferrule, silfos rings, silfos wafer, and silfos 3-sided hairpins as shown on drawing SE131-035 sheet 4 of 5.

Close brazing fixture with 80PSI on air cylinder.

Check joint for a max. gap of .002”- adjust fixture if necessary.

Check that misalignment between conductors is not greater than .006”.

(use straight edge and feeler gage on all 4 sides)

Stencil target for infrared thermometer on copper using 1/2”dia template and high temp. paint.

Center brazing coil around joint using ceramic spacers.

Aim infrared thermometer on target.

Turn cooling water on to brazing fixture and Robitron.

Turn on main power switch to Robitron.

Turn on circulating pump.

Turn DC power on.

Use foot control to start brazing cycle.

Robitron will turn off automatically at end of timed cycle.

Record the following :

Power-            ________          Frequency-                 ________

Voltage-          ________           Time @ full power-    ________

Total Time -     ________           Max. Temp Reached-  ________

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Signature and Date:

Attach tension fixture equally spaced around braze joint.  This fixture uses two 5 ton cylinders @  4250PSI to apply 8500lbs of tension on the braze joint during the helium leak test.    Wrap splice joint with plastic and insert helium leak check sniffer. Purge conductor with helium then pressurize to 50psi. Leak check to 10-6. After leak check is complete, purge conductor with nitrogen.

Leak Detector; Model__________            Serial #_____________

Leak Rate:		(Spec= <10-5 cc/sec)

Note: Joints failing this test must be cut out beyond the heat affected zone and re-brazed.

Signature and Date:

Check Rockwell Hardness  (55F min annealed, 60-82F unannealed);

¼”either side of joint-  ________      2” Left of Joint -          ________

2” Right of Joint -        ________      3” Left of Joint -          ________

3” Right of Joint -         ________     4” Left of Joint -     ________

4” Right of Joint -        ________

QA Signature and Date:

Preform radius using radius fixture and  Enerpac “C” press at 8000 psi.

Signature and Date:

Insulate splice area with one layer ½ lapped .0035”x1.0” adhesive kapton and three layers ½ lapped  .007”x 1.0” glass tape.  Protect  turn insulation with one wrap of mylar tape.

Signature and Date:

QA Signature and Date:_____________________________

Carefully  place the turn back in the stack and remove the mylar tape.

Signature and Date:

| Operation-012 | Layer 3 to Layer 4 Splice |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Place copper roll on  dereeler turn table.

Spread turns using plastic or G-10 wedges.

Check  conductor and remove any nicks or  burrs with emery paper or scotchbrite while using a vacuum to catch any  slivers or dust.

Wipe-down conductor with acetone.

Signature and Date:

Cover cleaned conductor with plastic and seal with tape.

Butt-splice conductor to previous conductor roll by torch brazing. This will provide a means for         pulling conductor thru tensioner and taping machine. After conductor reaches the winding machine,  cut away the butt splice along with 1 foot of copper from either side of the butt-splice.

Give cutout section to QA to verify all annealed copper was removed.

Disgard plastic used to wrap conductor.

Signature and Date:

Hardness of cutout section (60-82Rf):  12” left of torch braze_______

12” right of torch braze_______

QA Signature and Date:

Prep end of layer 4 conductor for the layer to layer splice by facing-off end of conductor and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of conductor with bottle brush and acetone a minimum of 8” deep.

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Position brazing fixture 53028-700.

Place ferrule, silfos rings, silfos wafer, and silfos 3-sided hairpins as shown on drawing SE131-035 sheet 4 of 5.

Close brazing fixture with 80PSI on air cylinder.

Check joint for a max. gap of .002”- adjust fixture if necessary.

Check that misalignment between conductors is not greater than .006”.

(use straight edge and feeler gage on all 4 sides)

Stencil target for infrared thermometer on copper using 1/2”dia template and high temp. paint.

Center brazing coil around joint using ceramic spacers.

Aim infrared thermometer on target.

Turn cooling water on to brazing fixture and Robitron.

Turn on main power switch to Robitron.

Turn on circulating pump.

Turn DC power on.

Use foot control to start brazing cycle.

Robitron will turn off automatically at end of timed cycle.

Record the following :

Power-            ________          Frequency-                 ________

Voltage-          ________           Time @ full power-    ________

Total Time -     ________           Max. Temp Reached-  ________

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Signature and Date:

Attach tension fixture equally spaced around braze joint.  This fixture uses two 5 ton cylinders @  4250PSI to apply 8500lbs of tension on the braze joint during the helium leak test.    Wrap splice joint with plastic and insert helium leak check sniffer. Purge conductor with helium then pressurize to 50psi. Leak check to 10-6. After leak check is complete, purge conductor with nitrogen.

Leak Detector; Model__________            Serial #_____________

Leak Rate:		(Spec= <10-5 cc/sec)

Note: Joints failing this test must be cut out beyond the heat affected zone and re-brazed.

Signature and Date:

Check Rockwell Hardness  (55F min annealed, 60-82F unannealed);

¼”either side of joint-  ________      2” Left of Joint -          ________

2” Right of Joint -        ________      3” Left of Joint -          ________

3” Right of Joint -         ________     4” Left of Joint -     ________

4” Right of Joint -        ________

QA Signature and Date:

Insulate splice area with one layer ½ lapped .0035”x1.0” adhesive kapton and three layers ½ lapped  .007”x 1.0” glass tape.

Signature and Date:

QA Signature and Date:_____________________________

| Operation-013 | Layer 4 Winding |
| --- | --- |

NOTE: White (Lint Free) gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

This layer will be wound in the clockwise direction.  Place G-11 filler SE131-032 as shown on     drawing  SE131-035 sheet 4  Section G-G. Start taping machine and wind three turns with 400PSI (3450lbs) tension on load cell.

While winding , clamp conductor to winding fixture every three to four feet.  After ¾ to 7/8 turn and again after turn 1 ¾ to 1 7/8 turn, measure and press the turn to turn offset into the conductor using fixture 53028-800-A and Enerpac “C” press at 8000PSI. Reinsulate offset area. Do not bring the end of turn three into position until the end of the long lead has been marked on turn two or the fixture for transfer to turn three.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify filler SE131-032 was sanded.

Signature and Date:_______________________

Check overall conductor plus insulation build a minimum of once per turn;

Turn # 1 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 2 – 1.064”+/-.010 ________ X .807”+/- .010__________

Turn # 3 – 1.064”+/-.010 ________ X .807”+/- .010__________

A minimum of once per turn check for gaps no larger than .020” between turns or turn and fixture(this does not include the long straight section which will be bumped into place after completiuon of winding)  and that conductor is not visibly twisted;

Turn #1 - Pass_________   Fail_______

Turn #2 -  Pass_________   Fail_______

Turn #3-    Pass_________   Fail_______

Signature and Date:

QA verification of offset area  reinsulation.

Turn 1 offset:_____________________________QA Signature and Date

Turn 2 offset:_____________________________ QA Signature and Date

Turn 3 offset:______________________________ QA Signature and Date

Prep end of Long Lead SE131-053 for brazing to the end of Layer 4 Turn 3 by facing-off end of lead and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

Place long lead in position on winding fixture with center of .500” dia hole in lead on center of     winding fixture (see sheet 2 of dwg SE131-035). Mark end of lead on turn 2 and/or winding fixture – this mark will be transferred to turn 3 when it is brought into position. Remove lead and wind turn 3 into position – transfer mark that represents the end of the lead to turn 3. Prep end of conductor for lead brazing by facing-off end of conductor (up to the mark made above) and counterboring  .570 + .010/ -.005” deep x .437 +.002/-.000” diameter using the climax mill.

Signature and Date:

Inspect flatness of faceoff and  counterbore dimensions.

Faceoff Flatness .002” - ______________ (check with straight edge and feeler gage)

Bore Diameter .437 +.002”/-.000 - ______________(check with pin gages- 80% of depth))

Bore Depth .570 +.010/-.005” - __________________(check with depth mic.)

Centering .966” direction – Left Side Wall Thickness = ___________

Right Side Wall Thickness=___________

.015”max allowable difference- ___________

Centering .709” direction – Top Side Wall Thickness = ___________

Bot. Side Wall Thickness=___________

.015”max allowable difference- ___________

Check misalignment between c’bore and hole in conductor by placing ferrule in c’bore and

inserting .250”dia pin thru ferrule into hole in conductor- _______Pass  _______ Fail

QA Signature and Date:

| Operation-014 | Braze Long Lead Water Fitting |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of lead with bottle brush and acetone..

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Torch braze brass water fitting to lead using SP15 silfos rod. Position as shown on dwg SE131-003 sheet 4 of 5.

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Clean entire lead and remove any sharp edges by filing and buffing with scotchbite pads.

Signature and Date:

| Operation-015 | Braze Long Lead to Layer 4 |
| --- | --- |

NOTE: Lint free gloves or Surgical Latex Gloves shall be worn by all personnel when handling insulated or bare conductor after cleaning.

Clean silfos and copper with scotchbrite and acetone. Scrub bore of conductor with bottle brush and acetone a minimum of 8” deep.

Wipe surfaces of silfos and copper with alcohol to remove acetone residue.

Position brazing fixture 53028-700.

Place ferrule, silfos rings, silfos wafer, and silfos 3-sided hairpins as shown on drawing SE131-035 sheet 4 of 5.

Close brazing fixture with 80PSI on air cylinder.

Check joint for a max. gap of .002”- adjust fixture if necessary.

Check that misalignment between conductors is not greater than .006”.

(use straight edge and feeler gage on all 4 sides)

Stencil target for infrared thermometer on copper using 1/2”dia template and high temp. paint.

Center brazing coil around joint using ceramic spacers.

Aim infrared thermometer on target.

Turn cooling water on to brazing fixture and Robitron.

Turn on main power switch to Robitron.

Turn on circulating pump.

Turn DC power on.

Use foot control to start brazing cycle.

Robitron will turn off automatically at end of timed cycle.

Record the following :

Power-            ________          Frequency-                 ________

Voltage-          ________           Time @ full power-    ________

Total Time -     ________           Max. Temp Reached-  ________

Remove excess silfos and inspect joint for voids or cracks (Pass/Fail)-    _______

Signature and Date:

Attach tension fixture equally spaced around braze joint.  This fixture uses two 5 ton cylinders @  4250PSI to apply 8500lbs of tension on the braze joint during the helium leak test.    Wrap splice joint with plastic and insert helium leak check sniffer. Purge conductor with helium then pressurize to 50psi. Leak check to 10-6. After leak check is complete, purge conductor with nitrogen.

Leak Detector; Model__________            Serial #_____________

Leak Rate:		(Spec= <10-5 cc/sec)

Note: Joints failing this test must be cut out beyond the heat affected zone and re-brazed.

Signature and Date:

Check Rockwell Hardness  (55F min annealed, 60-82F unannealed);

¼”either side of joint-  ________      2” Left of Joint -          ________

2” Right of Joint -        ________      3” Left of Joint -          ________

3” Right of Joint -         ________     4” Left of Joint -     ________

4” Right of Joint -        ________

QA Signature and Date:

Insulate lead with one layer ½ lapped .0035”x1.0” adhesive kapton and three layers ½ lapped  .007”x 1.0” glass tape.  Two uninterrupted layers of 5-6” wide kapton tape may be used in place of the 1” half lapped kapton in the heavy section of the lead. Glass cloth with a build of .042” may be used in areas where where taping with the .007”x 1.0” tape is not pratical.  Clamp lead in place. Insert filler SE131-041. Material may be removed if there is interference. Fill gaps with glass tape.

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify filler SE131-041 was sanded.

Signature and Date:_______________________

| Operation-015 | Install G-11 Lead Locking Block |
| --- | --- |

All G11CR fillers must be sanded with heavy grit non-conductive sand paper on all sides.

Verify Lead Locking Block SE131-047, SE131-078, and SE131079 were sanded.

Signature and Date:_______________________

Grinding and/or filing may be necessary to fit block . After block has been fitted match drill 5 ½” dowel pin holes and insert G11-CR dowels. Fill gaps with glass tape.

Signature and Date:_______________________

Inspect Lead Dimensions & Block Fit per dwg 131-035 sheet 3;

9.9 +/- .1 = __________________

1.71 +/-.030 = ________________

45( +/- 15minutes=____________

Engineering or QA Signature and Date:_______________________

| Operation-016 | Straightness Check – Long Straight Section |
| --- | --- |

Coil is acceptable if the straight section can be held against the winding fixture with a minimal amount of pressure from two C-clamps.

Clamp #1 Force _______________ Lbs

Clamp #2 Force _______________ Lbs

Max Allowable=______________

Operator Signature and Date:_______________________

Engineering or QA Signature and Date:_______________________

| Operation-017 | Hydro and Flow Tests |
| --- | --- |

Hydro :

Hydrostatically test at 600 PSI  for 10 minutes recording pressure within 2 PSI accuracy every 2 minutes. No drop in pressure is allowed.

Minutes                               PSI

0                                      _________

2                                     __________

4                                     __________

6                                     __________

8                                     __________

10                                  _________

Repeat test at 600 PSI for 1 hour recording pressure within 2 PSI accuracy every 10 minutes. Maximum allowable drop in pressure is 10 PSI.

Minutes                               PSI

0                                    __________

10                                  __________

20                                  __________

30                                  __________

40                                  __________

50                                  __________

60                                  __________

Pressure Gage Model # ______________        Serial # _______________

Signature and Date:_______________________

Flow :

With inlet pressure at 200PSI and outlet pressure at 100 PSI,  purge coil for 2 minutes to remove trapped air and then weigh the quantity of water discharged from the coil in 120 seconds (using stop watch).

Weight of water discharged  in 120 seconds =  ___________________

Divide weight by 16.666 =   _______________GPM

Minimum allowable flow rate is 1.35 GPM.

Inlet Pressure Gage Model # ______________         Serial # _______________

Outlet Pressure Gage Model # ______________        Serial # _______________

Scale  Model # ______________        Serial # _______________

Signature and Date:_______________________

| Operation-018 | Remove Coil from Winding Fixture |
| --- | --- |

There are milled slots on the winding fixture that indicate the area where the ground insulation is tapered from 3/8” thickness to 1/8” thickness at the ends of the long straight section of the coil. Transfer these marks from the fixture to the coil.

Signature and Date:_______________________

Prepare the coil for opening the cleanroom ceiling panels by covering all exposed glass tape with plastic stretch wrap material. Prior to sliding the ceiling panels, tape-up the vinyl seals at the panel joints to prevent the seals from wiping off dirt and debris from a passing panel.

Signature and Date:_______________________

Position lifting fixture over coil and place plastic blocking between fixture and coil to secure coil prior to releasing winding fixture.

Signature and Date:_______________________

After coil is removed from winding fixture, the lifting fixture and coil must be flipped since the coil is installed in the mold with the leads up.

Signature and Date:_______________________

| Operation-019 | Electrical Tests |
| --- | --- |

Surge at 750Volts to stress insulation .

Ring test using Sencore LC 103 Tester

Model # ______________        Serial # _______________

# Rings_______           Min Allowable= 32

Signature and Date:_______________________

Measure DC Resistance  -   1192 to 1204 micro ohms at 20 degrees C.

Tester Model # ______________        Serial # _______________

Resistance  ________   Temp   _______ F

Corrected to 20 C  __________

Signature and Date:_______________________

Inductance and “Q” @ 1KHZ.

Tester Model # ______________        Serial # _______________

L= ____________mH           Q= ____________

Signature and Date:_______________________

Wrap coil with aluminum foil and Megger test at 1 KV.

Tester Model # ______________        Serial # _______________

Insulation Resistance ____________ (1000 Mega Ohms Minimum)

Signature and Date:_______________________

| Operation-020 | Ground Insulation |
| --- | --- |

Note: The coil must remain secured by the lifting fixture at all times, this requires stepping-off and splicing of the ground wrap layers at the attachment points.

The coil is ground wrapped with half lapped layers of .015” x 2” glass tape at 10% compression to a build of 1/8” thickness in the wedge area of the coil and a build of 3/8” for the remainder of the coil. The 1/8” build will require 4 to 5 half lapped layers and the 3/8” build will require 12 to 13 layers. The lead area and G-11 Lead Locking Block also gets the 3/8” build of glass. Glass cloth may be used in areas where half lapping is not practical but the build must remain 3/8”. To determine the exact number of layers, measure the coil at several locations prior to applying the ground insulation and again after several layers heve been applied. Prior to installing the last layer of ground wrap install the “Diagnostic Loop Wire” as shown on drawing SE131-005.

.125” Build in Wedge Area

| Location | Width (over turns) | Height (over turns) | Width (over 3 layers) | Height (over 3 layers) | Avg Build | Additional Req’d to meet .125” | Final Build |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |  |
| 3 |  |  |  |  |  |  |  |

If the average additional build required per the above table is;

.060 to .070 then add 2 half lap & 1 butt

.050 to .060 then add 2 layers half lapped.

.040 to .050 then add 1 half lap & 1 butt lap

.030 to .040 then add 1 half lapped

Signature and Date:_______________________

.375” Build  Area

| Location | Width (over turns) | Height (over turns) | Width (over 11 layers) | Height (over 11 layers) | Avg Build | Additional Req’d to meet .375” | Final Build |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |  |
| 3 |  |  |  |  |  |  |  |
| 4 |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |

If the average additional build required per the above table is;

.060 to .070 then add 2 half lap & 1 butt

.050 to .060 then add 2 layers half lapped.

.040 to .050 then add 1 half lap & 1 butt lap

.030 to .040 then add 1 half lapped

Signature and Date:_______________________

Attach second lifting fixture with plastic blocking and remove first lifting fixture.  Ground wrap stepped-off areas remaining from attachment points of first lifting fixture.

Signature and Date:_______________________

Position “Diagnostic Loop Wire” over coil lead area as shown on drawing SE131-005. Twist wires in this area with a twist spacing of 5/8 to ¾”.  The minimum allowed bend radius is 1/8”.

Check resistance of sheath (90ohms) - __________________

Check resistance of center conductor (1400 ohms) - ____________________

Megger between center conductor and sheath at 100 volts ( 1megaohm) - _________________

Signature and Date:_______________________

| Operation-021 | Install Coil in Mold |
| --- | --- |

Install coil on mold base plate and use pushers to hold coil in shape prior to removing lifter.

Install dummy wedges.

Use pushers to align coil with scribe line representing location of outside rail.

Install outside rail.

Check position of “ Diagnostic Loop Wire”  and place excess wire in a plastic bag then fill bag with  RTV.

Signature and Date:_______________________

Install inside rail.

Install sheet copper, armalon, and steel blocking in lead area to assist in cleanup after VPI.

Install lid.

Install reservoir and resin fittings.

Signature and Date:_______________________

Apply 10PSI of pressure to mold and check that there is no drop in pressure after 1 hour.

Signature and Date:_______________________

| Operation-022 | Mold Bakeout |
| --- | --- |

Place mold on oven buggy with lead area at high point. Connect 6 riser tubes and glass reservoir to the vacuum manifold in oven and open valves. Run copper fill line to outside of oven and close valve.

Degas mold to .5 Torr or less for 8 hrs at 120 deg F.  After vacuum has stabilized, check for leaks by closing valve to pump and monitor vacuum gage. Changes in 1 or 10 millitorr increments would be an acceptable leak rate. Changes in 100 millitorr increments would require repair of the leak. Prior to filling, raise the mold vacuum level to .5 torr higher than the resin component mixing and degassing pressure for a minimum of 1 hr prior to filling.

Signature and Date: ______________________________

| Operation-023 | Vacuum Impregnation-Epoxy Mixing |
| --- | --- |

NOTE:  All temperatures and cycle times used during the impregnation and curing processes will be accurately measured and recorded on the Traveler.  Attach all graphs to this section of the Traveler.

The coil mold will be equipped with 8 temperature sensors to monitor uniform heating and cooling of the coils.  One sensor on coil lead, 6 sensors on mold and one measuring oven air temperature. During bake-out, curing and cool down, the temperature at each sensor will be recorded at least once every 15 minutes.

No resin will be used that exceeds the manufacturers recommended shelf life.  Also, no coloring agent will be mixed with the epoxy system.

The mixture is as follows:

Part A Epoxy Resin CTD-101K		100 p.b.w.

Part B Hardener CTD-101K		90 p.b.w.

Part C Accelerator CTD-101K		1.5 p.b.w.

Record lot number off of resin drum and hardener drum.

Resin					Hardener

Degasing operations will be performed on resin at 1-1.5 Torr.

Set mixing tank temperature to 120(F.

Mechanical mixing is required.

Mix Part A and degas simultaneously for a minimum of 15 minutes.

Add Part B to Part A , mix and degas simultaneously for approximately 20-40 minutes until bubbles evolve infrequently from the mixture.

Add Part C to the above mixture and mix and degas simultaneously for a minimum of 30 minutes.

DO NOT wait longer than 35 minutes from the time the accelerator (Part C) is mixed in to begin impregnating the coil.

Total weight of Mix    _____________________

Mix Resin		Start Time:_____________Finish Time_______________

Mix Resin & Hardener	Start Time:_____________Finish Time_______________

Accelerator Added	Start Time:_____________Finish Time:_______________

Vacuum ___________ Torr

Signature and Date:_____________________________

| Operation-024 | Vacuum Impregnation |
| --- | --- |

Begin impregnation between 30 to 35 minutes of the initiation of Part C to A & B. Bring resin tank to atmospheric pressure and remove tank from mixer. Connect tank to lowest fill point on mold. Impregnate mold at a pressure between 1.5 – 2.0 Torr and a temperature of 120 deg. F. Establish a slow but steady flow of epoxy.  The mold has six riser tubes and one reservoir.  As the level of epoxy reaches a riser tube, allow the resin to fill the tube within 2 ft of the shutoff valve before closing the valve. These riser tubes give an indication of the fill rate and the location of the resin in the mold. After the mold is filled,  the reservoir will be kept full with epoxy resin during the curing process.    ?????? Hold atmospheric pressure for 20-30 minutes then pull vacuum of 2.0 torr for 20-30 minutes and observe size and  quantity of air bubbles. Repeat this pressure-vacuum cycle 3 times or until bubbles cease.

Filling:	Start Time:______________	Finish Time_________________

Weight of unused resin mix:_________________

Signature and Date: ______________________________

| Operation-025 | Epoxy Curing |
| --- | --- |

Apply 30 PSI overpressure to mold. Use the following cure cycle with a maximum ramp rate of 20 (F/hour from 120(F to 230(F (5.5hrs) and 10 (F/hour from 230 to 257(F (3 hrs).  which thermocouples on the mold or air temp???  Provide the chart data and attach to MPO? Monitor and record every ½ hr must have manned

120 to 230 over 5.5

230(F for 5 hrs. 		Start Time:_____________Finish Time:____________Date:______________

230 to 257 for 3hrs

257(F for 15 hrs.		Start Time:_____________Finish Time:____________Date:______________

Signature and Date: ______________________________

| Operation-026 | Mold Cool Down |
| --- | --- |

After the coil has completed its cure cycle, it will be cooled at a rate of 20( -25(F per hour until it reaches 113(F.  Do not force cool. Approximately 6 hrs. cool down.

When the coil and mold have cooled to 113(F or less, it will be removed from the oven. Attach oven recorder chart and mold sensor chart to traveler and write serial number and date on charts.

Do not force cool the coil.

Record Time/Date when mold has stabilized at room Temperature:______________________

Signature and Date:_________________________________

| Operation-026 | Remove Coil From Mold |
| --- | --- |

STOP- DO NOT PROCEED BEYOND THIS POINT WITHOUT WRITTEN INSTRUCTIONS!!!!