February 22, 2207

To: Distribution

From: Wayne Reiersen

Subject:  Stellalloy properties

The purpose of this memo is to document Stellalloy properties from EIO (E, Sy, Su, elongation, and Charpy v-notch compiled by Frank Malinowski) and from measurements taken at PPPL (CTE from Ed Bush and Geoff Gettelfinger).  The results are interesting and merit contemplation.

Stellalloy mechanical properties are shown in Table 1.  Bar charts by coil are provided for each of the properties in Figure 2 through Figure 6.  The results are largely encouraging.  In all cases, the required minimum values were exceeded.  The room temperature yield strength properties ranged from 22-27 ksi, all exceeding the required value of 20 ksi.  The 77K yield strength values ranged from 93-104 ksi, far exceeding the required minimum value of 72 ksi.  Likewise, the 77K tensile strength ranged from 160-173 ksi, exceeding the required minimum value by even larger margins.  We should review our design margins at operating temperature in light of the favorable mechanical properties from the test data.

Table 1 - Stellalloy mechanical properties

What is striking is the variation seen in some instances.  For instance, the elastic modulus varied from 23-27 Msi at RT and from 23-30 Msi at 77K.  The range is one-quarter (25%) of the average!  I sure hope this does not introduce substantial field errors due lack of stellarator symmetry in coil deflections.

Yield strength varied from 35-44 ksi at RT and from 99-104 ksi at 77K.  Curiously, there seems to be a strong secular trend in yield strength based on the order in which the castings were produced, as shown in Figure 1.

Figure 1 - Yield strength versus production order

The data is even more puzzling for the coefficient of thermal expansion (CTE) for Stellalloy.  Up until recently, we only had data for the alloy used in the JP Pattern (JPP) casting.  (See reference material at end of document).  The data (ref. Table 2) showed a strain of approximately -3000  upon cooldown from RT to 77K which is close (within 10%) to the expected value of -2760  for SS316LN.  Ed Bush was asked to measure the CTE on some Stellalloy pieces we had here at PPPL.  He measured a cutoff that was approximately 12 inches long (Bush-12 in Table 2).  The strain was -2583  which is also close to the published value for SS316LN.  However, he also measured two smaller coupons that were 3 inches long (Bush-3a and Bush-3b in Table 2) and less than 1 inch wide.  For the 3 inch measurements, the strain ranged from -3570  .  For the 1 inch measurements, the strain ranged from -3250  .  Discounting the 1 inch measurement due to the small dimension, the strains measured on the 3 inch coupons are 40% higher than the strains measured on the 12-inch article.

Table 2 - Stellalloy CTE data

Clearly, there must have been a measurement error so Gettelfinger went back and measured the 12 inch article and one of the 3 inch coupons.  Lo and behold, the answer came back the same.  The 3 inch coupon appears to have a CTE that is 40% higher than for the 12 inch article.  For now, I would propose using the ITER SS316LN value of -2760  which is in between the Bush and Gettelfinger values for the 12 in article.  However, the wild disparities among the measured Stellalloy values are disturbing.

Cc: Gettelfinger, Heitzenroeder, Brooks, Fan, Dudek, Nelson, Cole, Williamson, Freudenberg

Figure 2 - Elastic Modulus

Figure 3 - Yield Strength

Figure 4 - Tensile strength

Figure 5 - Elongation

Figure 6 - Charpy V-notch energy

Table 3 - MCWF castings compiled data

Table 4 - MCWF weld material compiled data

# Reference Material

## JPP CTE data

## Original stellalloy CTE measurements (Bush)

## Repeated Stellalloy CTE measurements (Gettelfinger)