Progress Report – 2

Cure Induced Stresses during Cure of Copper/CTD 401 and Copper/CTD 404

Madhu S. Madhukar, The University of Tennessee, 865-974-7676, mmadhuka@utk.edu

During a typical cure cycle of a thermoset polymer its temperature is ramped to some intermediate level and the polymer is soaked at this temperature. This temperature is not high enough to initiate significant chemical reactions. The purpose of this step is to lower the polymer viscosity so it can flow easily. The ramp-and-hold step is followed by another ramp-and-hold to a higher temperature. The second ramp-and-hold temperature is where polymer cure is completed. After the chemical reactions are complete, the cured polymer is cooled to the room temperature. One of the characteristics of thermoset polymeric materials is that these materials undergo volume change (both expansion and shrinkage) during their thermal processing. The expansion is the result of thermal expansion due to temperature increase and the shrinkage is the result of a chemical reactions (crosslinking) and the formation of a rigid 3-dimensional network. Also important to note is that in most cases the expansion and the shrinkage occur at different times during a cure cycle. These volume changes are not of great concern if these polymers are cured by themselves. However, if they are used as “fillers” to form a composite material, the volume changes may introduce residual stresses which in turn may cause composite part warpage and/or property degradation.

The University of Tennessee has developed an experimental procedure called Cure Induced Stress Test (CIST), which can be applied to a given fiber-matrix system to determine the effect of different cure cycles on the fiber residual stresses. This information can then be used to optimize the cure cycle to minimize the unwanted internal stresses and thus improve the part quality.  In this method (see Figure 1),

Figure 2. Schematic of CIST

the fiber is stretched taut between two fixed supports and the polymer is cured around the taut fiber. As the polymer cures, its volume changes.  The change in the volume produces a proportional change (depending on the instantaneous stiffness and the stress relaxation behavior of the polymer) in the fiber tension. A load cell attached to one of the fiber ends measures the fiber load change.

The fiber/polymer system used in this study was copper strands with CTD 401 and CTD 404 matrix systems. These are considered to be the low cure shrinkage resins that are candidates for being used by ORNL in the fusion energy program.

CIST was used in three different types of experimentations – Copper strand alone, Copper strand in CTD 401 and Copper strand in CTD 404 resins.

CIST Results with Copper Fiber Alone

In the first experiment, a copper strand was fixed taut under an initial tension between two fixed supports and subjected to a temperature cycle. The temperature cycle consisted of a ramp from room temperature to 230oF, hold at 230oF for 2 hours followed by cool down to room temperature. As can be seen, the fiber tension decreases during the heat ramp due to the thermal expansion of copper fiber. However, the tension continues to decrease even during the temperature hold. This slow and continuous decrease is attributed to fiber creep under load and temperature. During the cooldown to room temperature, the tension returns to its initial value.

Figure 2. 	CIST result on copper fiber alone. The rapid decrease in fiber tension during the temperature ramp is due to fiber thermal expansion. The slow decrease in fiber tension during temperature hold is due to fiber creep. The fiber tension returns to its initial value after cooldown to room temperature.

CIST Results with Copper Fiber/CTD 101

For this system, the cure cycle suggested by the resin manufacturer was applied. The cure cycle consisted of two ramps and two soaks followed by a cooldown to room temperature as shown in Figure 3. These results are shown in two charts – in the first chart (Figure 3a), to highlight the fiber tension change prior to cooldown, the cooldown data is not included, and in the second chart (Figure 3b) the cooldown data is included.  As can be seen that there is a large decrease in fiber tension during the first ramp. Comparing this figure with Figure 2, it is clear that this decrease is mostly from the thermal expansion of the copper strand. Then during the first soak at 230oF, the fiber tension begins to increase. As shown in Figure 2 that copper fiber shows significant creep during temperature hold, hence there are two opposing mechanisms occur during the temperature hold:

( i) a decrease in fiber tension due to fiber creep, and

(ii) an increase in fiber tension due to resin shrinkage.

A net increase in fiber tension during the first temperature hold indicates that the resin shrinkage effects dominate the fiber creep effects. During the second ramp, the tension drops rapidly. During the temperature ramp, there are four mechanisms that may occur simultaneously. These are:

- fiber tension drop due to fiber thermal expansion,

- tension drop due to resin thermal expansion,

- fiber tension drop due to fiber creep, and

- fiber tension increase due to continued resin shrinkage.

Since there is a net fiber tension drop during the second temperature ramp, the first three mechanisms dominate over the last one. During the second thermal soak, there are again two competing mechanisms:

( i) a decrease in fiber tension due to fiber creep, and

(ii) an increase in fiber tension due to resin shrinkage.

A relatively unchanged fiber tension suggests that there these two opposing mechanisms balance each other out.

Figure 3. 	CIST result on copper/CTD 101. The rapid decrease in fiber tension during the temperature ramp is due to fiber thermal expansion. The gradual increase in fiber tension is slow decrease in fiber tension during temperature hold is due to fiber creep. The fiber tension returns to its initial value after cooldown to room temperature.

The results of Figure 3 are again plotted in Figure 4 to show the effect of cooldown on resin shrinkage. As can be seen there is a very large amount of resin shrinkage during cooldown. In fact, the fiber tension increased beyond the 10V capacity of the load cell. Clearly, most of this tension increase is due to polymer shrinkage. As we saw earlier from Figure 2 that the fiber shrinkage brings the fiber tension back to its original value. Hence, the contribution of copper fiber compared to that of the CTD 101 to the total tension increase during the cooldown is relatively insignificant.

Figure 4. 	CIST result on copper/CTD 101. This is the same data of Figure 3 plotted on a different scale to show the effect of cooldown on fiber tension. The resin shows a very large amount of shrinkage during cooldown.

CIST Results with Copper Fiber/CTD 404

The suggested cure cycle for CTD 404 and the resulting fiber tension data is shown in Figure 5. Unlike the CTD 101, this resin does not show much shrinkage during the first temperature hold. In fact, the fiber tension continues to decrease gradually during the first hold suggesting that resin shrinkage (if any) during this period is not able to cancel the fiber creep that was observed earlier (see Figure 2). Then during the second ramp, there is fiber tension drop due to copper thermal expansion. Interestingly, the fiber tension begins to increase during the second temperature hold and continues to increase till the end of the cure cycle. In fact, significant resin shrinkage may have started during the temperature ramp. This suggests that the increase in temperature caused resin chemical reactions to start rapidly. Also, the continued fiber tension increase till the end of the second temperature ramp suggests that resin shrinkage continued till the end, i.e. the cure may have been terminated prior to completion of the resin cure.

Figure 5. 	CIST result on copper/CTD 404. The rapid decrease in fiber tension during the temperature ramp is due to fiber thermal expansion. The slow decrease in fiber tension during the first temperature hold suggests that significant resin shrinkage has not begun during this period. The fiber tension increase during the second ramp is the result of rapid resin curing. The continued fiber tension increase until the end of second temperature ramp suggests that the cure cycle may have been terminated prior to completion of resin cure.

Figure 6 shows the plot of the same data (as in Figure 5) on a different load scale to see the effect of resin cooldown. As can be seen the cooldown produces a significant shrinkage. Also, compared to CTD 101 (Figure 4),  CTD 404 shows much larger cooldown shrinkage (compare the load axis scales in Figures 4 and 6). Again most of the cooldown shrinkage is attributed to the resin shrinkage because, Figure 2 shows that cooldown shrinkage in copper fiber alone is relatively insignificant.

In addition to the two major mechanisms, i.e. cure shrinkage and thermal expansion, there may also be polymer stress relaxation affecting the fiber tension.

Conclusions:

- Copper strand shows evidence of creep under load and temperature.

- CTD 101 completes most of its cure during the two-hour soak at 230oF.

- There is no fiber tension change during the 16-hour soak at 257oF. However, there may still be additional cure (shrinkage) during period, because any increase in copper fiber may have been cancelled by the corresponding load decrease due to fiber creep.

Figure 6. 	CIST result on copper/CTD 404. This is the same data of Figure 5 plotted on a different scale to show the effect of cooldown on fiber tension. The resin shows a very large amount of shrinkage during cooldown.

- Major part of cure shrinkage of CTD 404 is seen during the second temperature ramp from 176oF to 302oF and during the soak at 302oF.

- During the cure of CTD 404, the fiber tension continues to increase till the end of the cure cycle suggesting the cure cycle suggested by the resin manufacturers may not be long enough to complete the resin cure.

- Both CDT 101 and CTD 404 show very large shrinkage (compared to other commonly used resins) during cooldown. The shrinkage during the cooldown of CTD 404 is about 1.5 times larger than that in CTD 101. However, this comparison may be a little misleading because compared to CTD 101, the CTD 404 is cured at higher temperature (302oF versus 257oF)

Work In Progress

More definitive conclusions regarding the resin shrinkage during the cure cycle and cooldown will be made when copper fiber alone data is obtained for the same cure cycle as used in Figures 3-6. Thus, work is currently underway to obtain fiber alone data for these cure cycles. Another useful information will be to quantify the resin shrinkage during different stages of cure cycles including cooldown.