From: Keilbach, Robert [mailto:Robert.Keilbach@wgint.com]

Sent: Thursday, August 04, 2005 11:57 AM

To: Phil Heitzenroeder

Subject: RE: MetalTek Zoned Product Analysis Results

Phil,

I was unaware of the proposed spec change. Based on the "real values" found, for additional hot cracking resistance I would recommend limiting P and S content further than the proposed .04% maximums, e.g. ~.035% max. for P and .025% max. for S.

Bob