Phone: 636-475-2199  •  Fax:  636-479-3399

Charles.Ruud@MetalTek.com

Draft Corrective Action 	1671

Carondelet Division

Corrective Action Type	NCR

Date	4-10-06

CA Originator	C. Ruud

Applies to: A-6 Coil

Description of Defect / Non-Conformance

Test bar from zone 1 failed elongation at -320 F.  Result was 20% versus a minimum of 32%.

The original set of three bars, Z-1, Z-2 and Z-3 were sent for testing.  Z-1 failed for elongation, 26% vs 32% minimum and Z-3 failed for elongation 19% vs 32% minimum.  All other results were acceptable.  Retests were ordered.  The second results were similar.  Z-1 failed for elongation, 25% vs 32% minimum and Z-3 failed for elongation 13% vs 32% minimum, but broke outside the gauge length.  The third set of bars was tested.  Z-3 passed and Z-1 failed for elongation, 20% vs 32% minimum, but broke outside the gauge length.  All other test results were acceptable.  See attached test reports.

Root Cause

We believe the failures are due to the test bars are located where the metal flowing into the casting is cooler and large grains form as a result.  This has caused failures on C-5 and C-6 coils.  We have ordered photo macrographs to see if this is the case.

Corrective Action

Use A-6 as is.

.

Actual Completion Date

TBD

Signed:  C. Ruud

CC: B. Craig, J. Edwards, E.J. Kubick, J. Markham, J. Galaske