Pg 1 of 2

Energy Industries of Ohio

Corrective Action Report/Request            ID#_032206-1P___________

Date_____03-22-06________

Due_____3-22-06_________

Initiated By     Peter Djordjevich

Issue/Non Conformance

(EIO, MTM) Provide NCR for C-5 flange thickness concern raised by MTM in the 3/7 teleconference. Flange may be shifted so “best fit” makes flange too thin when there‘s actually enough cast thickness. This more than likely will effect all C coils to varying degrees.

Root Cause

Adjust for best fit by machining. Some cleanup stock being removed

on back side of flange (approx .050 - .070 inches) this was not     anticipated. Stock seems to be sufficient in as cast state, but variances

in casting dimensions require best fit setup which detracts from flange

thickness. Castings will vary dimensionally this is typical. Area should

have been called out dimensionally on the model stating min/max dimension.

Corrective Action

Use as is. After evaluating C4 currently being dimensioned at Major

Tool, flange thickness was measured at 1.190 inches. This is an existing

condition that will more than likely effect all C coils, and possibly run

into A & B coils. Also I would like to add that thickness of the flange

actually increases moving in towards the casting due to draft and fillet.

If required a .050 to .100 gain in flange thickness may be achieved by

Eliminating machining on the back side of the flange.

Verification of Corrective Action

N/A use as is

Pg 2 of 2

Completion / Verification Date 03-21-06

Signature EIO Quality

Peter Djordjevich