Major Tool & Machine, Inc.
Page: 1
 1458 East 19th Street
MTM N/C: 18830
Date: 12/09/05
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

ENERGY INDUSTRIES OF OHIO
Customer:
Telephone:
216-496-2314
Contact:
NANCY HORTON
NKHFlowen@aol.com
E-Mail:
216-328-2001
Fax:

S005242-F/Ln:1
Customer P.O.:
ER316MNNF_093_GTAW / WELD WIRE,GTAW .093 DI
Part:
C1
Serial No./Qty:

Revision:

Drawing ID:

317-636-6433
Telephone:
MIKE GRIFFITH
Reported By:
Fax:
317-634-9420
E-Mail:
mGriffith@MajorTool.com

Problem:
NCSX-CSPEC-141-03-10 section 3.1.1.2 table 3-4 requires Elongation percentage to be a minimum of 32% at 77K.
Actual test results for elongation are 27%.

Proposed Disposition:
Major Tool proposes that the elongation percentage be accepted as is and the specification be revised to include this
elongation percentage.

Number of additional pages: 

Customer Disposition:       [   ] Use As Is          [  ] Rework          [  ] Repair          [  ] Scrap          [  ] Replace

Date:
Title:
Technical Contact Approval: 

Date:
Title:
Buyer Approval: 

Title:
Date:

Major Tool Implemented By:

 /Open /WO:65707-1
n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420