Major Tool & Machine, Inc.
Page: 1
 1458 East 19th Street
MTM N/C: 20917
Date: 12/22/06
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

ENERGY INDUSTRIES OF OHIO
Customer:
Telephone:
216-496-2314
Contact:
NANCY HORTON
NKHFlowen@aol.com
E-Mail:
216-328-2001
Fax:

S005242-F/Ln:3
Customer P.O.:
SE141-115 / MODULAR COIL, TYPE B
Part:
B3
Serial No./Qty:
9
Revision:
SE141-115
Drawing ID:
W/O Links:
1-Type:W: 65708/3.0 Sub: 1 

317-636-6433
Telephone:
MIKE GRIFFITH
Reported By:
Fax:
317-634-9420
E-Mail:
mGriffith@MajorTool.com

Problem:
Workorder: 65708/3.0 Sub:1 Op:132
      Inspection Test #: 90  rejected: OUTER AS CAST SURFACES: {g|.5|A|C|B}: -.001 TO .386
      Inspection Test #: 100  rejected: : 2X .03 X 45`: TO SMALL OR INCOMPLETE
      Inspection Test #: 110  rejected: .40: : .300-.506
      Inspection Test #: 120  rejected: : 2X .03 X 45`: TO SMALL OR INCOMPLETE
      Inspection Test #: 140  rejected: 2X .31: : .295-.325
      Inspection Test #: 150  rejected: MACHINED SURFACES M TO M1: {g|.02|R|S|T}: .0206 TO -.023
      Inspection Test #: 160  rejected: DATUM D SIDE VERIFY SHELL INTERSECT CLEARANCE
USING GAGE MTMFX-3473: : REJECTED BETWEEN T HOLES 68-70 AND 81-84
      Inspection Test #: 170  rejected: P TO M: {g|,2|R|S|T}: -.007 TO .110
      Inspection Test #: 190  rejected: MACHINED SURFACES N TO N1: {g|,02|R|S|T}: -.0272 TO .0265
      Inspection Test #: 200  rejected: DATUM E SIDE VERIFY SHELL INTERSECT CLEARANCE
USING GAGE MTMFX-3473: : REJECTED BETWEEN T HOLES 32-46, 49-56 AND 85-90
      Inspection Test #: 210  rejected: Q TO N: {g|.2|R|S|T}: .0119 TO .1136
      Inspection Test #: 260  rejected: : {#|,06|R|S|T}: .013 TO .138
      Inspection Test #: 340  rejected: DATUM E: {f|,01}: .0187
      Inspection Test #: 360  rejected: DATUM D: {f|,01}: .0277
      Inspection Test #: 390  rejected: : 2X d2.50: 2.472 - 2.475
      Inspection Test #: 730  rejected: : 3X d1.885 ~..003 THRU: 1.886 (1 HOLE HAS NON-CLEANUP UP TO
1.902")
      Inspection Test #: 840  rejected: 2X .88/1.13: : 1.10 - 1.16
      Inspection Test #: 1020  rejected: WING SURFACES: {g|-.12;;-.25|A|B|C}: -.115 - .158 

Proposed Disposition: MTM proposes to accept as is

 IDC attachment
Number of additional pages: 

Customer Disposition:       [   ] Use As Is          [  ] Rework          [  ] Repair          [  ] Scrap          [  ] Replace

n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420