Major Tool & Machine, Inc.
Page: 1
 1458 East 19th Street
MTM N/C: 21032
Date: 01/19/07
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

ENERGY INDUSTRIES OF OHIO
Customer:
Telephone:
216-496-2314
Contact:
NANCY HORTON
NKHFlowen@aol.com
E-Mail:
216-328-2001
Fax:

S005242-F/Ln:4
Customer P.O.:
 / 
Part:
B4
Serial No./Qty:
9
Revision:
SE141-115
Drawing ID:
W/O Links:
1-Type:W: 65708/4.0 Sub: 1 

317-636-6433
Telephone:
MIKE GRIFFITH
Reported By:
Fax:
317-634-9420
E-Mail:
mGriffith@MajorTool.com

Problem:
Workorder: 65708/4.0 Sub:1 Op:132
      Inspection Test #: 90  rejected: OUTER AS CAST SURFACES:       {g|.5|A|C|B}: -.074 TO .355
      Inspection Test #: 100  rejected: : 2X .03 X 45`: .010 TO .040
      Inspection Test #: 120  rejected: : 2X .03 X 45`: .01 TO .040
      Inspection Test #: 130  rejected: 2X R.11: : .090 TO .110 ON E       SIDE .090 TO .110 ON D SIDE
      Inspection Test #: 150  rejected: MACHINED SURFACES
      M TO M1: {g|.02|R|S|T}: -.026 TO .014
      Inspection Test #: 160  rejected: DATUM D SIDE
      VERIFY SHELL INTERSECT CLEARANCE
      USING GAGE MTMFX-3473: : AT HOLE 82 WILL NOT ACCEPT          GAGE
      Inspection Test #: 170  rejected: P TO M: {g|,2|R|S|T}: -.018 TO       .104
      Inspection Test #: 190  rejected: MACHINED SURFACES
      N TO N1: {g|,02|R|S|T}: -.026 TO .024
      Inspection Test #: 200  rejected: DATUM E SIDE
      VERIFY SHELL INTERSECT CLEARANCE
      USING GAGE MTMFX-3473: : AT HOLE 37 THRU 45, 50 THRU       57 AND AT 61 WILL NOT ACCEPT
GAGE
      Inspection Test #: 210  rejected: Q TO N: {g|.2|R|S|T}: .014 TO       .102
      Inspection Test #: 230  rejected: : 2X .06-.09 X 45`: .06/.120 X       45
      Inspection Test #: 250  rejected: : 84X b.625 y .188: .622/.625         X  .161/.208
      Inspection Test #: 260  rejected: : {#|,06|R|S|T}: .009 TO .083
      Inspection Test #: 340  rejected: DATUM E: {f|,01}: .021
      Inspection Test #: 360  rejected: DATUM D: {f|,01}: .017
      Inspection Test #: 390  rejected: : 2X d2.50: 2.515/2.523
      Inspection Test #: 510  rejected: : 14X
      d1.885 ~ .003 THRU: 1.879/1.892
      Inspection Test #: 540  rejected: : 10X
      d1.885 ~ .003 THRU: 1.875/1.898
      Inspection Test #: 720  rejected: 14X Ø1.375-6: {#|.06|N|A|E}:       .004 TO .064
      Inspection Test #: 840  rejected: 2X .88/1.13: : 1.060 / 1.160
      Inspection Test #: 1010  rejected: AS CAST SURFACES:       {g|,5|A|B|C}: -.286 TO .241
      Inspection Test #: 1030  rejected: WING POCKET:       {g|+0.0;;-.12|A|B|C}: -.086 TO .051 

Proposed Disposition:
Propose to accept deviations as is.

  11 page IDC attachment
Number of additional pages: 

Customer Disposition:       [   ] Use As Is          [  ] Rework          [  ] Repair          [  ] Scrap          [  ] Replace

n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420

 Major Tool & Machine, Inc.
Page: 2
 1458 East 19th Street
MTM N/C: 21032
Date: 01/19/07
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

Title:
Date:

Major Tool Implemented By:

n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420