A-1 Items

NCR’s

| 1308 MetalTek 6/13/05 | Closed | C and A Coil Shims 11 Pieces. Chemistry for 11 shim castings is out of specification. |
| --- | --- | --- |
| 1320 MetalTek 7/5/05 | Closed | C1, C2 & A1 Coil Castings Lack of test material in violation of paragraph 4.2.2.4 additional test material. |
| 1323 MetalTek 1/18/06 | Closed | A1, C-1 thru C4, Shim C1 and 10 more shims Incorrect analysis results reported for Sulfur and Phosphorous. |
| 1324 MetalTek 7/18/05 | Closed | A-1 Casting Major weld repairs |
| 1347 MetalTek 8/01/05 | Closed | A1 Coil Wall thickness below tolerance |
| 1379 MetalTek 8/31/05 | Closed | MCWF A-1 Material failed elongation and one of three charpy impact tests. |
| 1625 Major Tool 3/1/06 | Open | MCWF A-1 Crack like defect found during machining of A-1 coil. |
| 19783 Major Tool 5/8/06 | Open | MCWF A-1 34 counterbores are under low limit of the tolerance |
| 19891 Major Tool 5/26/06 | Open | A-1 PT indications |
| 19916 Major Tool 5/26/06 | Open | A-1 RT indications |
| 19933 Major Tool 5/31/06 | Open | A-1 Misc. Surface Conditions UAI - PPPL repair, leave G-11 large in future. UAI – prob. Converted to tapped w/”hockey pucks” UAI - PPPL repair, leave G-11 large in future UAI- PPPL Repair Get Penetrant Chemical Composition UAI UAI UAI UAI UAI UAI UAI UAI UAI |