Flex Shim Concept 1

Steps:

- Weld left side of shim to bottom plate with individual stringers, allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

- Position top plate onto shim as shown and perform right fillet weld allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

Flex Shim Concept 2

Steps:

- Weld left side of shim to bottom plate with individual stringers, allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

- Position top plate onto shim as shown and perform right fillet weld allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

Flex Shim Concept 3

Steps:

- Weld left side of shim to bottom plate with individual stringers, allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

- Position top plate onto shim as shown and perform right fillet weld allowing cooling to warm to the touch between stringers. (approx. 7 stringers / fillet weld).

  - Fillet weld sizes shall match shim thickness (0.44”).

  - Monitor and record force between clamp and shim during stringers.

  - Release clamp after fillet is complete and measure and record gap in unrestrained position.

  - Re-clamp and measure and record clamping force to restore shim to flat condition.

# Text boxes

Flex shim

6” long x 4” wide

Top flange, 1.5” thick

Fillet weld (typ – 2 ends)

1.5” top flange

Lower flange, 1.5” thick

1.5” diameter limiter puck  0.5” thick to react compression loads between flanges

0.44”

Side View   (note:  there will be two types of welds on the  right side , one as shown with the fillet weld extending beyond the top flange as shown, and one inside the flanges with a fillet to the top plate.

Flex shim

2.5” long x 4”wide

Flex shim

Top flange, 1.5” thick

Fillet weld (typ – 2 ends)

1.5” top flange

Lower flange, 1.5” thick

1.5” diameter limiter puck  0.5” thick to react compression loads between flanges

0.44”

0.5”

Flex shim – length as material is available, approx. 6” long and 4” wide

Top flange, 1.5” thick length as available

Fillet weld (typ – 2 ends)

7/16”

1.5” top flange

Lower flange, 1.5” thick length as available

1.5” diameter limiter puck  0.5” thick to react compression loads between flanges

0.44”

0.5”