# Week of 5/29/06

PPPL MCWF Quality Notes

Tuesday Teleconference 5/30 9 AM EST (877) 952-1506, Passcode: 833648

- Closed Items:

  - EIO CA for C-4 features compliant to SE141-116, Rev. 7, but not to Rev. 8 has been updated and is considered closed.

- Pending from EIO:

  - (EIO) Provide final documentation packages for completed MCWF’s.

    - C-2 (reopened)
Status: (Open) PPPL on reviewing package noted missing documents  
1) The weld map does not correspond to the attached photos. NOTE - EIO is constructing a new weld map. 
2) The data package is missing NCR CA 1320 Note – will add after resolving above
3) The data package is missing NC’s 18830 & 18831.  These are for weld wire and elongations that were not to specification.  This weld wire was used to repair C-2 (8/05) before the CSPEC was changed in 11/15/05 and so the NCR’s should also be in the C-2 package.

    - C-3 (reopened)
Status: (Open- No Update) EIO will add MetalTek CA 1581.

    - C-4

Status: (Open- No Update) –EIO needs MTM portion (by 6/6)

    - C-5

Status: (Open- No Update) – EIO needs MTM portion (by 6/6)

  - (EIO, MTK/MTM) Update CA 1625 (A-1 linear indication) after machining. 
Status (Open)  MTM issued NC19891 for PT indications includes what is left of this indication.   This MetalTek CA update is to address the root cause. (by 5/23)

  - (EIO, MTK) Update CA 1671 (for A6 test results below spec for elongation) with inspection and analysis results.  
Status (Open) – MetalTek updated the CA on 5/5 to state that the plates had flaws.  Per discussion on 5/8 with PPPL, MetalTek will update again to include photographs with individual plate identification. MTK sent one half of a fractured test bar back to lab to prepare sample for photo macrograph. Lab lost sample and cannot photograph it. MTK has sent other half for photo and expects close-out by 5/25.

  - (EIO) Investigate and take steps to mitigate source of ferromagnetic contamination seen on C-4, B-1 and subsequent castings. Report back with update to CA 1695 so that PPPL can disposition NCR 3633.
Status: (In-Progress) – Awaiting update to corrective action. EIO & PPPL found only 5 high permeability spots, all dark in color, on A-1.  B-1 & A-2, inaccessible at the time, need to be checked and cleaned up. Then the checks on receipt of the next few MCWF’s may provide information to close this issue.

  - (EIO, MTM) Disposition rejected SS316 bearing plate material documented on EIO’s NC 19233 & 19234.
Status: (Open) SS: plates will be shipped with A1.

  - (EIO, MTM) Document Corrective Action to close NC 19783 (A-1Tee hole counter-bore depths).
Status: (Open)  plan to update before A1 is shipped.

  - (EIO, MTM) Document Corrective Action to close NC19710 (C-5 weld repairs w/o RT)
Status: (Open)  Rework router/update after A-1 ships.

  - (EIO, MTM) MTM to propose new location/orientation for B style thermocouple holes.
Status: (Open)  after A-1 ships.

- Pending from PPPL

  - Provide updated requirements documents incorporating the following changes:

    - CSPEC update addressing revised poloidal break inspection/tolerances. Poloidal break flange fit-up, 0.005” through and 0.015” at edges – edge defined as no more that 1/8” penetration. 
Status: (Open- No Update) Rapid response guidance sent 3/16.  Wording for next CSPEC revision is in process.

    - PPPL to incorporate guidance on Type A MCWF thermocouple hole placement provided 3/20 into requirements documents. 
Status: (Open- No Update) – EIO has delivered marked up drawings with proposed locations.

  - PPPL will provide drawings and a formal request for the “hockey pucks” that were discussed during MTM’s visit.
Status: (Open- No Update)

  - PPPL will check and advise MTM on Bushings with acceptable magnetic permeability.
Status: (Open- No Update)

- Discussion Topics for Teleconference:

  - New Specification & Drawing Changes

    - .A NCSX Project-initiated modification to improve the lead block positioning resulted in a slight reorientation (2.2° horizontal change at the top and 0.114” vertical change) of the lead slots as shown below