# Week of 7/3/06

PPPL MCWF Quality Notes

No Tuesday Teleconference

- Closed Items:

  - Dispositioned NC 20044 for LP indications and NC 20080 for Dimensional & Visual on A-2 were transmitted to EIO.

- Pending from EIO:

  - (EIO) Provide final documentation packages for completed MCWF’s.

    - C-4
Status: (Open) – PPPL feedback on preliminary copy provided 6/26.

    - C-5
Status: (Open) – PPPL feedback on preliminary copy provided late 6/30/06

    - A-1
Status: (Open) – In-progress at MTM. Awaiting purchase/receipt of bushings(2.3 below)

    - A-2
Status: (New) –

  - (EIO) Investigate and take steps to mitigate source of ferromagnetic contamination seen on C-4, B-1 and subsequent castings. Report back with update to CA 1695 so that PPPL can disposition NCR 3633.
Status: (In-Progress) – MTK inspected and cleaned-up A-2 on 6/19.  B-1 was not accessible at the time - Inspection/Clean-up will be done by MTM as part of final.

  - (EIO, MTM) Document Corrective Action to close NC 19783 (A-1Tee hole counter-bore depths).
Status: (Open) PPPL sent EIO/MTM direction on 6/20 to use 316 material regardless of the permeability.  MTM to initiate manufacture of the bushings. PPPL needs them mid-August.

  - (EIO, MTM) Provide Stellalloy bearing plates and replacement fasteners for MCWF’s C-1 through C-5. (Needed to close NCR’s 3618 & 3651.)
Status: (Open) Replacement hardware received.  MTM is working on the plates - most of the plates are being machined as a group, so they will ship when all are done - probably with A-3.

  - (EIO, MTM) MTM to obtain ingredients information for Sherwin penetrant (seen on A-1 PB insulator).
Status: (Open) Initial contact of Sherwin got no response. MTM will pursue. In the interim, MTM has sent the MSDS which only lists alcohol as a hazardous substance.

  - (EIO, MTK) Provide additional photos (model) for Type A technique to help match locations to film.
Status: (Open) 7/7 target

  - (EIO, MTK) Provide film locations for Type B Technique.
Status: (Open) – per MTK, they provided hardcopies to EIO

- Pending from PPPL

  - Provide updated requirements documents incorporating the following changes:

    - CSPEC update addressing revised poloidal break inspection/tolerances. Poloidal break flange fit-up, 0.005” through and 0.015” at edges – edge defined as no more that 1/8” penetration. 
Status: (Open- No Update) Rapid response guidance sent 3/16.

    - CSPEC revision to update the inspection points.
Status: (Open) Rapid response guidance sent 5/16.

  - Disposition (mark) rejected SS316 bearing plate material and then close EIO’s NC 19233 & 19234.
Status: (Open).  PPPL to verify that all plates are marked with their permeability. Unmarked plates are being marked.

  - Review updated CA 1671 (for A6 test results below spec for elongation) with inspection and analysis results.  
Status (Open) – in progress

- Discussion Topics for Teleconference:

  - New Specification & Drawing Changes

The production winding form folder of the manufacturing ftp site has been updated with the addition of an IGES file (typeb-new-vpi-holes) that shows the new VPI bleed holes for the Type-B modular coils.

Note: Frank is on vacation 7/3-7/7, returning 7/10.  Questions or concerns that cannot wait should be directed to Phil or Irving at tel. 609 243-2054, email pqa@pppl.gov.