| 1 | Manufacture & check pattern equipment, Locate, identify cast on test material per specification | NPAT-SOP-0100/ Section 4.2.2 |  | Section 4.2.2 | NA | A1 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | Check chemical composition | QUAL-SOP-0048 Rev 5 | Material Test Report chem. from each ladle and weighted average. | Section 3.1 | Verify chemistry at outside laboratory.** | A1 | R1 |  |
| 3 | Heat treat | Heat – SOP 0100 Rev 8 and Note below | Heat charts | NA | Test material and sample material to be located in corresponding zone. | A1 | R1 |  |
| 4 | Test Cast on Bars - Tensile Test including tensile, yield, elongation and elastic modulus at -320 F and at room temperature. Charpy impact test at -320 F and at room temperature. | A703/A703M-03 | Test Certificate | Section 3.1 | 1 per zone/3 per casting – retain all test material* | A1 | R1 | Charpy Test Hold W1 |
| 5 | Sample material, not less than 3”x 3”x 1” 3 pieces per zone | NA | NA | Section 4.2.2.4 | Submit to EIO | A1 | R1 |  |
| 6 | Weld material testing Tensile and charpy each lot. Test at –320 F and +70 F Chemical composition | A703/A703M-03 QUAL-SOP-0048 Rev 5 | Test Certificate Test Certificate | Section 3.1 | Retain all test material* | A1 | R1 |  |
| 7 | Radiographic examination | CQP-401 Rev 5 X-ray at MQS PROCEDURE 20.H.010 REV 1 | Reader sheets and film | MSS SP-54 | All reject, including surface defects must be verified by RT. Performed by ASNT Level II | A1 | R1 |  |
| 8 | Interim Liquid Penetrant Examination | CQP-300 Rev 10 | Final Inspection Report, ASTM A903M, S1 | A903/A903M Level I for high stressed area, Level II for other areas. | Performed by ASNT Level II | A1 | R1 |  |
| 9 | Weld repair Welds <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) Welds <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 | CQP-60 Rev 5 Procedures & personnel must be PPPL approved. | Map major welds | Weld map Send map within 24 hours of welding | Major weld is 20% of thickness or 1” whichever is less or 10” square. Also report multiple repairs of the same defect | H | R1 |  |
| 10 | Magnetic permeability inspection | CQP- Mag Perm – 0100 R1. Must also meet S24, A703and S1 of A800 | Final Inspection Report | Less than 1.02 | Test all weld repairs, 1 point every 2 sq. inches or 3 points per weld whichever is less | A1 | R1 |  |
| 11 | Sand Blast | BLAS SOP 0100 Rev 6 | NA | NA | Remove all blast material from casting | NA |  |  |
| 12 | Initial interim layout inspection by Lawton | NA | NA | NA | Performed on –1 castings by Lawton | NA | R1 |  |
| 13 | Interim layout inspection | Layout SOP 0100 Rev 0 | File | NA | Performed on –2 through –6 castings | A2 | R1 |  |
| 14 | Heat treat – Stress Relief | Heat – SOP 0100 Rev 8 and Note below | Heat charts | NA | NA | A1 | R1 |  |
| 15 | Final visual inspection | CQP-500 Rev 4 | Final Inspection Report | A802/A802M Level III | Performed by ASNT Level II | A2 | R1 | W2 5 day notice |
| 16 | Liquid Penetrant Examination | CQP-300 Rev 10 | Final Inspection Report ASTM A903M, S1 | A903/A903M Level I for high stressed area, Level II for other areas. | Performed by ASNT Level II | A1 | R1 | W2 5 day notice |
| 17 | Magnetic permeability inspection | CQP- Mag Perm – 0100 R1. Must also meet S24, A703and S1 of A800 | Final Inspection Report | Less than 1.02 | Test 6 inch grid and all weld repairs | A1 | R1 | W2 5 day notice |
| 18 | Preparation for shipment |  |  |  |  | A1 |  |  |
| END | Release for shipment | Quality Plan / Customer specifications | Inspectors Release |  |  |  | H |  |

* submit to EIO

** Submit NCR to EIO for non conformances

# Inspection surveillance Codes

A1   =	100% Inspection Performed (measurement or pass / fail)

A2   =	Sample Inspection Performed

W1  = 	100% Witness Inspection

W2  =	Sample Witness Inspection – Requires five day notice

S      =	General surveillance of operations

R1    =	100% Review of Documentation

R2    =	Sample Review of Documentation

H     =	Manufacture Hold Point

Heat Treat Procedure:

SOLUTION ANNEAL.  MAKE SURE TO BLOCK ALL FLANGES OF FORM AND RACETRACK TO MINIMIZE CREEP DISTORTION. Soak Temp:  2050F, Soak Time:  seven hours minimum, Quench Type:  Air Cool     MAKE SURE TEST MATERIAL IS PLACED IN THE CORRECT ZONE.

Stress Relief Procedure:

Load casting into cold furnace.  Ramp up to 1100 F at rate of 200 F per hour.  Hold at temp 4 hours.  Furnace cool to 500 F at 50 F per hour.  Air cool.  Submit furnace charts to QA.

Rev 1 – added note  “Procedures & personnel must be PPPL approved.”  to step 9.