Carondelet Division

8600 Commercial Blvd. -   Pevely, MO  63070 USA

Phone: 636-479-4499 - Fax: 636-479-3399

Material Test Report

ENERGY INDUSTRIES OF OHIO

Purchase Order Number	PPPL-FP-LTS-2	Cert Number	S75920-1

Pattern Number	MCWF-C2	Pour Date	4/15/2005

CAF Metal Designation	CF8MNMnMod

Material Spec	CF8MNMnMOD

Weighted average of 3 heats – 29060(46%),29061(25%),29063(29%) Total Weight 29107 lbs.

Revised  10/26/05

Element	Min	Actual	Max

C	 0.04	 0.06	 0.07

MN	 2.3	 2.8	 2.8

SI	 0.0	 0.5	 0.7

CR	18.0	18.0	18.5

NI	13.0	13.2	13.5

MO	 2.1	 2.3	 2.5

P*	 0.0	 0.023	 0.035

S*	 0.0	 0.018	 0.025

N	 0.24	 0.26	 0.28

*P & S taken from cast on bar, zones 1,2,&3 and analyzed by wet chemistries, ASTM  E1019-03 for sulfur and Colormetric for phosphorous.

PRODUCT  ANALYSIS

Results of spectrometer analysis of cast on test bar after spectrometer preventive maintenance performed and at Wisconsin Centrifugal.

***Not analyzed on spectrograph.

| Element | CAF after PM | WC Analysis |
| --- | --- | --- |
| C | *** | 0.07 |
| MN | 1.6 | 1.6 |
| SI | 0.8 | .09 |
| CR | 18.2 | 18.2 |
| NI | 13.5 | 13.7 |
| MO | 2.3 | 2.2 |
| P | 0.024 | 0.023 |
| S | 0.012 | 0.014 |
| N | *** | 0.23 |

Respectfully Submitted,

Charles A. Ruud

Quality Assurance Manager

Superior Quality Engineered Metal Products

www.MetalTekInt.Com