# Coil A Final shipment record and corebox details

Drag Pattern: 2 Loose pieces.

2 Parting blocks for cheek section. Follow details marked on              parting blocks for correct molding and removal of loose pieces.

Add chills as marked.

Cope Pattern: Sleeve risers per solidification specifications.

Add chills as marked.

Corebox 1: 1 core per mold

(Magenta)

Corebox 2: 1 Loose piece

(Olive)       1 Core per mold

Corebox 3: 1 Top Loose piece

## (drag)         6 Loose pieces

Add chills as marked

X- markes hook locaters

1 Core per mold.

Corebox 4: 3 Loose pieces

(Blue)        Add chills as marked

1 Core per mold.

Corebox 5: 3 Loose pieces

(Red)        No chills

1 core per mold

Corebox 6: 1 Top Loose piece

(Cope)        17 Loose pieces

Add chills as marked

Sleeve risers as marked

2 Top loose hook locator pieces

1 Core per mold.

Corebox 7: 4 Loose pieces

(Yellow)     No chills

1 Core per mold.

Corebox 8: 4 Loose pieces

(Purple)      No chills

1 Core per mold.

Corebox 9: 2 Loose pieces.

(Green)       1 Loose wall.

Add chills as marked.

1 Core per mold.

Corebox 10: 2 Loose pieces.

(Pink)           1 Loose wall.

Add chills as marked.

1 Core per mold

Corebox 11: 1 Core per mold

(Teal)           Paste into cope mold.

Corebox 12: 1 Core per mold.

(Lime Green)   Paste into cope mold.

Corebox 13: 3 Cores per mold.

(Blue)          Paste into cope mold.

TEW 4/8/05