METALTEK INTERNATIONAL

THE CARONDELET DIVISION

STANDARD OPERATING PROCEDURE

NUMBER:  HEAT_SOP_0103  	REVISION:  6

DATE OF ISSUE: 1/18/05

TITLE:  HEAT TREATING

PREPARED BY:	Bob Carlton 	DATE: 	1/18/05

REVIEWED BY:	Chuck Ruud 	 DATE: 	1/18/05

CONTROLLED:					     UNCONTROLLED:

COPY NUMBER: _________

DISTRIBUTED TO:	_____________

This Document is considered uncontrolled unless controlled, copy number and distributed to blanks are filled out.

# METALTEK INTERNATIONAL 			Number	HEAT_SOP_0103

# THE CARONDELT DIVISION			Page		2 of 3

STANDARD OPERATING PROCEDURE 		Revision	6

Date		1/18/05

Revisions and amendments to the above reference procedure are recorded below.    A master log of revisions and amendments shall be maintained by the Quality Assurance Department.

REVISION		       AMENDMENT		      PAGE		DATE

- 04/26/01

1		Spelling corrections made		3		8/15/02

# 2                      Complete Rewrite                               3, 4                  9/10/02

# 3		COMPLETE REWRITE		ALL		3/21/03

# 4		Added CF8M .03C			3		2/4/04

# Added CF8MNMN MOD

# 5		Complete rewrite			all		8/23/04

6		Complete rewrite			all		1/18/05

# METALTEK INTERNATIONAL 			Number	HEAT_SOP_0103

# THE CARONDELT DIVISION			Page		3 of 3

STANDARD OPERATING PROCEDURE 		Revision	6

Date		1/18/05

- SCOPE

  - This procedure describes the minimum required steps for heat treating the alloys as designated in LDB.

- REFERENCED DOCUMENTS

  - HEAT SOP 0100, General Procedure for Heat Treating

  - Lab Data Base

- DEFINITIONS

3.1       Terms are defined in HEAT SOP 0100

- PROCEDURE STEPS

  - Load castings in the gas-fired or electric furnaces (ovens).  The gas-fired furnaces (ovens) are preferred.

  - Check “Special Instructions” in LDB for restrictions for a particular alloy loading into cold (less than 600F) furnace (oven).

  - Check LDB for furnace (oven) Ramp and program controller with the correct Ramp up restriction.

  - Set soak temperature as indicated in LDB.

  - Time at temperature shall be 4 hours.  If the load has castings greater than 4 inches thick, add ½ hour for each inch over 4.

  - Water or Rapid Air Quench per LDB instructions.

- FURNACE FAILURE PROCEDURES

  - If the furnace should fail in the indicated manner take the action designated.

    - If the furnace temperature runs less than 25 F below the set point then water quench at the minimum time at temperature.   If furnace shuts off or drops more than 25 F below the furnace Soak Temperature (as indicated in LDB), restart cycle and time at temperature. Avoid furnace cooling load if furnace is off for extended period.  Notify Quality Assurance.

    - If the furnace temperature runs less than 25 F over, return to the set point then water quench at minimum time at temperature.  If the furnace temperature runs more than 25 F over furnace Soak Temperature contact Supervision, Production Manager and Quality Assurance, give to inspection as a special group and hold for examination and disposition.

    - If the furnace cycle runs 1 hour longer than the indicated time.  Quench as normal and report load to Supervision and Quality Assurance.

    - If the furnace cycle runs more than 1 hour longer than the indicated time quench as normal contact Quality Assurance or Supervision for examination and disposition of castings.