| OPER. # | STATION | DESCRIPTION OF PROCESS | Name | Date |
| --- | --- | --- | --- | --- |
| 10 | QUALITY RELEASE | REVIEW AND APPROVE MTS. RECEIVED APPROVAL FROM EIO ON xxxxx FROM _Pete D._ SIGNED QUALITY MANAGER |  |  |
| 15 | PATTERN NPAT SOP 0100REV2 | APPLY APPROPRIATE PART NUMBER, SERIAL NUMBER, AND FOUNDRY MARK, TO THE PATTERN. CAST ON TEST BARS AND CAST ON BLOCKS (extra 3”x3”x1” specimens) REQUIRED, ID AS TO COIL NUMBER AND ZONE LOCATION. |  |  |
| 20 | COREMAKE CORE SOP 0100 REV 6 CALIBRATION PER CORE SOP 0200R4/0300R6 | MAKE CORES IN SAND MIXTURES AS DESCRIBED BY METALTEK ENGINEERING AND VERIFIED IN MODELING TRIALS. METALTEK CORE SOP 0100 REV 6) CORE WASH WITH ZIRCONIUM CORE WASH. (CALIBRATION OF EQUIPMENT REQUIRED PER CORE SOP 0200,R4 / 0300,R6) VERIFY COUNT AND INSPECT. |  |  |
| 30 | MOLD MOLD SOP 0400 REV 8 CALIBRATION PER MOLD SOP 0900 REV 5 PREPARATION PER MOLD SOP 1100R2/1200R2/1300R1 SAND TESTING PER MOLD SOP 1400R2/1500R3/1600R2 | MOLD PER WORK INSTRUCTIONS IN MAPICS ROUTING AND SOPS REFERENCED. ENGINEER OF RECORD – ROGER BROMAN, CONSULT ON MOLD-RELATED CONCERNS. MOLD MATERIALS REQUIRED PER MAPICS BOM. NOTIFY ENGINEER OF ANY SUBSTITUTIONS. |  |  |
| 40 | POUR MELT SOP 0100R5 MELT SOP 0700R2 MELT SOP 0600R2 | METAL MUST BE AOD REFINED OR AOD INGOT. VIRGIN METAL ADDITIONS ALLOWED. RECORD POURING TEMPERATURE: __________ CASTING POURED AT: ________________ DATE: _______________ HEAT #”s: _____________________________ ELAPSED POUR TIME_____________ KEEL BLOCKS POURED: __NA__________ Sample from ladle to be analyzed for final chemical analysis and reported on material certifications. Sample Taken by:_______________ Analyzed: _________________Date: ________________ |  |  |
| 50 | MELT SOP 0800R2 | SHAKEOUT |  |  |
| 60 | ARC RISE SOP 0100R1 | REMOVE RISERS AS DIRECTED BY SUPERVISOR. |  |  |
| 70 | HEAT TREAT HEAT SOP 0103R5 | SOLUTION ANNEAL. MAKE SURE TO BLOCK ALL FLANGES OF FORM AND RACETRACK TO MINIMIZE CREEP DISTORTION. Soak Temp: 2050F, Soak Time: At least 7 hours , Quench Type: Air Cool MAKE SURE TEST MATERIAL IS PLACED IN THE CORRECT ZONE. |  |  |
| 80 | PHYSICAL TESTING | OBTAIN TEST SPECIMENS AND SUBMIT FOR PHYSICAL TESTING. REPORT RESULTS AS PART OF STEP 510. |  |  |
| NOTE |  | THE ORDER OF CLEANING PROCESSES MAY BE ALTERED DUE TO CAPACITY CONSTRAINTS. HOLD POINTS AND COMPLIANCE WILL NOT BE COMPROMISED. EIO WILL BE ADVISED OF ALL CHANGES THAT MAY RESULT IN A REQUEST FOR DEVIATION FROM REQUIREMENTS. |  |  |
| 90 | GRIND GSWA SOP 0100R3 | SWING GRIND TO REMOVE RISER REMAINS AND FLASH IF REQUIRED. |  |  |
| 100 | GRIND GCHI SOP 0100R2 | CHIP AND HAD GRIND SURFACE OF PART AS REQUIRED FOR CONTOUR. |  |  |
| 110 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF X-RAY . EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 120 | X-RAY AT MQS MQS PROCEDURE 20.H.010 REV 0 | X-RAY PER TECHNIQUE # 12726 USE CALIBRATED DENSITOMETER FOR DENSITY VERIFICATION. WHEN MARKING USE BLACK MARKERS. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. | RT – LEVEL II |  |
| 130 | X-RAY CQP 401 REV 5 | X-RAY INTERPRETATION. ACCEPTANCE MSS SP 54. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. IF OK CHECK HERE ______ AND SEND TO STEP 160. REJECTED CHECK HERE ________ MARK UP DEFECTS AND SEND THE CASTING TO STEP XXX. | RT – LEVEL II |  |
| 140 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING 100% RT INSPECTION. |  |  |
| 150 | GRIND GCHI SOP 0100R2 | CHIP AND HAND GRIND EXCAVATION AS REQUIRED. |  |  |
| 160 | INTERIM VISUAL INSPECTION CQP-500 REV 4 | VISUALLY INSPECT 100% of COMPONENT ACCORDING TO ASTM A802 LEVEL 3 IN NON MACHINED AREAS AND LEVEL 2 IN MACHINED AREAS. IF OK CHECK HERE _______ . IF REJECTED CHECK HERE ____ . MARK AND REPAIR AT STEP 190. | VT - LEVEL II |  |
| 170 | INTERIM 100% L.P. CQP 0300 REV 10 | L.P. 100% OF COMPONENT. ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE ________GO TO 190. IF REJECTED CHECK HERE __________ | LP - LEVEL II |  |
| 180 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING 100% VISUAL AND LP INSPECTION. |  |  |
| 190 | GRIND GCHI SOP 0100R2 | CHIP AND HAND GRIND EXCAVATION OR VISUAL DEFECTS AS REQUIRED. |  |  |
| 200 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE ________ IF REJECTED SEND BACK TO STEP 190 | LP - LEVEL II |  |
| 210 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| 220 | WELD MAP | MAP ALL MAJOR WELDS WITH DIGITAL PHOTO/MAPS INDICATING LOCATION. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA. USE YELLOW MARKER. SUBMIT MAP WITHIN 24 HOURS OF START OF WELDING. MUST INDICATE ON MAP ALL MAJOR WELDS, DEFINED AS GREATER THAN 20% OF THE WALL OR 1 INCH WHICHEVER IS LESS OR 10 SQUARE INCHES APPROXIMATLY 3.3”X3.3”. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF WELD STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 230 | QA APPROVAL HOLD POINT | QA TO APPROVE ELECTRODE PRIOR TO USE. PROCEDURE USED: _______________, ________________, ___________________ LIST ALL MATERIAL/LOTS USED:___________________, _________________, __________________ QUALITY ENG. Name: ____________________ Date: ____________ |
| 240 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |
| 250 | GRIND GCHI SOP 0100R2 | HAND GRIND WELDS. |  |  |
| 260 | L.P. WELD CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE __________ WASH AND SEND TO STEP 280. IF REJECTED CHECK HERE __________ | LP - LEVEL II |  |
| 270 | Repeat | Repeat steps 180 to 260as required till clear through Visual Inspection & Penetrant Inspection. Document rework ON STEPS S180 TO S270. IF OK CHECK HERE ____________AND PROCEED TO STEP 280. |  |  |
| 280 | REPEAT STEPS | SUPPLEMENTAL REPAIR STEPS | 1ST | 2ND | 3RD | 4TH | 5TH |
| S180 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING RADIOGRAPHY. |  |  |  |  |  |
| S190 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. | LP - LEVEL II |  |  |  |  |
| S220 | WELD MAP | MAP ALL MAJOR WELDS WITH DIGITAL PHOTO/MAPS INDICATING LOCATION. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA. USE YELLOW MARKER. MUST INDICATE ON MAP ALL MAJOR WELDS, DEFINED AS GREATER THAN 20% OF THE WALL OR 1 INCH WHICHEVER IS LESS OR 10 SQUARE INCHES APPROXIMATLY 3.3”X3.3”. SUBMIT MAP WITHIN 24 HOURS OF START OF WELDING. |  |  |  |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF WELD STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |  |  |  |
| S240 | QA APPROVAL HOLD POINT | QA TO APPROVE ELECTRODE PRIOR TO USE. PROCEDURE USED: _____________, _____________ , ________________ MATERIAL /LOT USED :_________________, ________________, _________________ QUALITY ENG. Name: ____________________ Date: ____________ |  |  |  |  |  |
| S250 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |  |  |  |
| S260 | GRIND GCHI SOP 0100R2 | HAND GRIND WELDS. |  |  |  |  |  |
| S270 | L.P. WELD CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE __________ WASH AND SEND TO STEP 280. IF REJECTED CHECK HERE __________AND RETURN TO STEP S180. | LP - LEVEL II | OK REJ | OK REJ | OK REJ | OK REJ |
|  | Repeat | Repeat steps s180 to S270 as required till clear through Visual Inspection & Penetrant Inspection. | QA ENG. |  |  |  |  |
| 280 | TEST MAG PERM SOP MAG PERM 100, REV 1 | TEST MAG PERMEABILITY REPAIR AREAS TEST AT LEAST EVERY 2 INCH SQUARE OF WELD. ACCEPTANCE 1.02. IF OK CHECK HERE _______AND GO TO STEP 300. IF REJECTED CHECK HERE _______. |  |  |
| 290 | GRIND GCHI SOP 0100R2 | GRIND AREAS OF NON COMPLIANCE AND RETURN TO STEP 280. REPEAT UNTIL COMPLIANCE IS ACHIEVED. |  |  |
| 300 | X-RAY ( NOTE) | IF RADIO GRAPHED AREAS ARE GREATER THAN FOUR TO FIVE INCHES THE CASTING WILL BE SENT TO MQS. SEND TO MQS CHECK HERE_____________. RADIOGRAPH AT CAF CHECK HERE ___________. | QA ENGINEER |  |
| 310 A | MQS X-RAY DEFECTS REPAIRED BY WELDING | X-RAY PER TECHNIQUE # 12726 USE CALIBRATED DENSITOMETER FOR DENSITY VERIFICATION. ALL RT REJECTS, INCLUDING SURFACE DEFECTS WILL BE VERIFIED BY RT. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. | LEVEL II |  |
| 310 B | CAF X-RAY DEFECTS REPAIRED BY WELDING CQP 401 REV 5 | X-RAY PER TECHNIQUE # 12726 USE CALIBRATED DENSITOMETER FOR DENSITY VERIFICATION. ALL RT REJECTS, INCLUDING SURFACE DEFECTS WILL BE VERIFIED BY RT. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. | RT - LEVEL II |  |
| 320 | X-RAY CQP 401 REV 5 | X-RAY INTERPRETATION. ACCEPTANCE MSS SP 54. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. IF OK CHECK HERE ______ AND SEND TO STEP 340. REJECTED CHECK HERE ________ MARK UP DEFECTS AND SEND THE CASTING TO STEP S321. | RT - LEVEL II |  |
|  | REPEAT STEPS | SUPPLEMENTAL REPAIR STEPS | 1ST | 2ND | 3RD | 4TH | 5TH |
| S321 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING RADIOGRAPHY. |  |  |  |  |  |
| S322 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. | LP - LEVEL II |  |  |  |  |
| S323 | WELD MAP | MAP ALL MAJOR WELDS WITH DIGITAL PHOTO/MAPS INDICATING LOCATION. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA. USE YELLOW MARKER. MUST INDICATE ON MAP ALL MAJOR WELDS, DEFINED AS GREATER THAN 20% OF THE WALL OR 1 INCH WHICHEVER IS LESS OR 10 SQUARE INCHES APPROXIMATLY 3.3”X3.3”. SUBMIT MAP WITHIN 24 HOURS OF START OF WELDING. SUBMIT MAP WITHIN 24 HOURS OF START OF WELDING. |  |  |  |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF WELD STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |  |  |  |
| S324 | QA APPROVAL HOLD POINT | QA TO APPROVE ELECTRODE PRIOR TO USE. PROCEDURE USED: _______________, _______________, _____________ MATERIAL /LOT USED :________________, _______________, _____________________ QUALITY ENG. Name: ____________________ Date: ____________ |  |  |  |  |  |
| S325 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |  |  |  |
| S326 | GRIND GCHI SOP 0100R2 | HAND GRIND WELDS. |  |  |  |  |  |
| S327 | L.P. WELD CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE __________ WASH AND SEND TO STEP 300, RT. IF REJECTED CHECK HERE __________AND RETURN TO STEP S321. | LP - LEVEL II | OK REJ | OK REJ | OK REJ | OK REJ |
|  | Repeat | Repeat steps s321 to S327 as required till clear through Visual Inspection & Penetrant Inspection. | QA ENG. |  |  |  |  |
| 340 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF VISUAL AND LP STEPS. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 350 | FINAL VISUAL INSPECTION CQP-500 REV 4 | VISUALLY INSPECT 100% of COMPONENT ACCORDING TO ASTM A802 LEVEL 3 IN NON MACHINED AREAS AND LEVEL 2 IN MACHINED AREAS. IF OK CHECK HERE _______. SEND TO STEP 453. IF REJECTED CHECK HERE __________ . MARK AND REPAIR. INITIAL WHEN COMPLETE. MUST BE PERFORMED BY LEVEL II in VT. | VT - LEVEL II |  |
| 360 | FINAL L.P. CQP 0300 REV 10 | FINAL L.P. 100% OF COMPONENT. ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE __________ WASH AND SEND TO STEP 455. IF REJECTED CHECK HERE __________ | LP - LEVEL II |  |
| 380 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING FINAL PENETRANT INSPECTION. |  |  |
| 385 | GRIND GCHI SOP 0100R2 | CHIP AND HAD GRIND EXCAVATION AS REQUIRED. |  |  |
| 390 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. IF OK CHECK HERE ________ IF REJECTED SEND BACK TO STEP 385. | LP - LEVEL II |  |
| 400 | WELD MAP | MAP ALL MAJOR WELDS WITH DIGITAL PHOTO/MAPS INDICATING LOCATION. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA. USE YELLOW MARKER. SEND MAPS WITHIN 24 HOURS OF WELDING. MUST INDICATE ON MAP ALL MAJOR WELDS, DEFINED AS GREATER THAN 20% OF THE WALL OR 1 INCH WHICHEVER IS LESS OR 10 SQUARE INCHES APPROXIMATLY 3.3”X3.3”. |  |  |
| 420 | QA APPROVAL HOLD POINT | QA TO APPROVE ELECTRODE PRIOR TO USE. PROCEDURE USED: ____________________ MATERIAL/LOT USED:__________________________ QUALITY ENG. Name: ____________________ Date: ____________ |
| 430 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1(Flat) or 25 SMAW-CF8MNMN MOD REV 0 (Vertical) FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |
| 440 | GRIND GCHI SOP 0100 REV 2 | HAND GRIND WELDS. |  |  |
| 450 | L.P. WELDS CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. IF OK CHECK HERE __________ WASH AND SEND TO STEP 453. IF REJECTED CHECK HERE __________AND RETURN TO STEP 440. | LP - LEVEL II |  |
|  | Repeat | Repeat steps ___350 TO 450_____as required till welds clear Final Liquid Penetrant Inspection. Document rework on a supplemental MTS | qa eng. |  |
| 451 | TEST MAG PERM SOP MAG PERM 100, REV 1 | TEST MAG PERMEABILITY REPAIR AREAS. RECORD ON WELD MAP LIST. TEST AT LEAST EVERY 2” SQUARE OF WELD. ACCEPTANCE 1.02. IF OK CHECK HERE _______AND GO TO STEP 430. IF REJECTED CHECK HERE _______. |  |  |
| 452 | GRIND GCHI SOP 0100R2 | GRIND AREAS OF NON COMPLIANCE AND RETURN TO STEP 451. REPEAT UNTIL COMPLIANCE IS ACHIEVED. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF LAYOUT. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ APPROVAL RECEIVED ON ___________________ | Q ENG OR QA MGR |  |
| 100 | INTERIM LAYOUT SOP LAYOUT 0100 | INSPECT CASTING TO VERIFY DIMENSIONS. THIS STEP MAY BE MOVED. NOTE: THE FIRST PART PRODUCED OF EACH TYPE A, B AND C WILL BE DIMENSIONED BY LAWTON PATTERN. IF DIMENSIONED BY LAWTON IT WILL BE DOCUMENTED HERE. Subsequent casting done internally per Romer Arm. |  |  |
| 455 | HEAT TREAT | STRESS RELIEF. Load casting into cold furnace. Ramp up to 1100 F at rate of 200 F per hour. Hold at temp 4 hours. Furnace cool to 500 F at 50 F per hour. Air cool. Submit furnace charts to QA. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF VISUAL AND LP STEPS. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 460 | FINAL VISUAL INSPECTION CQP-500 REV 4 | VISUALLY INSPECT 100% of COMPONENT ACCORDING TO ASTM A802 LEVEL 3 ALL CONDITIONS. THIS STEP MAY BE UNNECESSARY IF OK AT STEP 350. IF OK CHECK HERE _______. IF REJECTED CHECK HERE __________ . MARK AND REPAIR AT STEP 390. MUST BE PERFORMED BY LEVEL II in VT. | VT - LEVEL II |  |
| 470 | FINAL L.P. CQP 0300 REV 10 | FINAL L.P. 100% OF COMPONENT. ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. THIS STEP MAY BE UNNECESSARY IF OK AT STEP 350. IF OK CHECK HERE __________ WASH AND SEND TO STEP 455. IF REJECTED CHECK HERE __________. DOCUMENT REPAIRS USING S321 THROUGH S327. | LP - LEVEL II |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIO AND DCMA AT LEAST FIVE DAYS IN ADVANCE OF MAG PERM STEPS. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 500 | FINAL MAG PERM INSPECTION SOP MAG PERM 100, REV 1 | PERFORM MAG PERM TESTING WITH SEVRIN GAUGE. ACCEPTANCE 1.02. CHECK THE ENTIRE SURFACE ON A 6”BY6” GRID. REPORT RESULTS. USE A 6” SQUARE BLOCK TO INDICATE TEST LOCATIONS AND RECORD RESULTS. COMPLIANT AREAS WILL NOT BE MARKED. MARK NONCOMPLIANT AREAS WITH AN “X” FOR REPAIR. OK CHECK HERE _____AND GO TO STEP 530. IF REJECTED CHECK HERE ______. |  |  |
| 510 | GRIND GCHI SOP 0100 REV 2 | HAND GRIND WITH SUITABLE CONE OR OTHER SIMILAR GRINDER AS REQUIRED TO ENSURE REMOVAL OF MATERIAL TO ACHIEVE MAG PERM REQUIREMENT. CIRCLE AREA REMEDIATE FOR RETEST. |  |  |
| 520 | RETEST MAG PERM SOP MAG PERM 100, REV 1 | RETEST MAG PERMEABILITY AT FAILED TEST POINTS. MARK NONCOMPLIANT AREAS WITH AN “X” FOR REPAIR. ACCEPTANCE 1.02. IF OK CHECK HERE _______. IF REJECTED CHECK HERE _______RETURN TO STEP 510. |  |  |
| 530 | DOC. REVIEW | REVIEW DOCUMENTS AS REQUIRED IN CAF CHECKLIST, ALL DOCUMENTS NOTED TO BE ACCESSIBLE FOR AUDITING. (SHIPPER, C OF C, M.T.R., M.T.S., INSPECTION REPORT, X-RAY READER SHEETS AND HEAT TREAT CHARTS) |  |  |
| NOTICE | RELEASE FROM EIO | PROVIDE DOCUMENTS TO EIO. SENT ON ____________ BY __________________. RECEIVED RELEASE FROM EIO ON _________________. | Q ENG OR QA MGR |  |
| 540 | PACK AND SHIP | PACKAGE AND SHIP TO MAJOR TOOL. |  |  |
| 1000 | REVISION HISTORY | ORIGINAL 12-14-04. Approved 12-14-04. Revision level 1- Revised 1-26-05 new page 8, correct High stress areas, Revision level 2 3-16-05, delete LO step 455. Revision 3 3-28-05 Added note regarding hold point at weld step 400. Revision level 4 written for C-2 casting 4-18-05. Rev 5 added Layout SOP# and note regarding first casting layout responsibility. 5-10-05. Rev 6 added word LOT to weld material steps. 5-29-05. Rev 7 6-14-05 added “LOT” to weld step on supplement page. Rev. 8 7-29-05 added stress relief , deleted weld hold points, added vertical weld procedure, and several editorial changes. REV 9 8-28-05 – MODIFIED RT STEPS AND ADDED REQUIREMENT TO RT ALL RT DEFECTS INCLUDING SURFACE. | CARUUD |  |

RED AREA INDICATES HIGH STRESSED AREA

# GENERAL ISOMETRIC

# VIEW FROM TOP SIDE

TOP SIDE ISOMETRIC    		     TOP SIDE VIEW 	          BOTTOM SIDE ISOMETRIC	       BOTTOM SIDE VIEW

# Text boxes

TABS DESIGNATE CRITICAL AREA