Listing of changes made to the working C-2 doc package

The C-2 document package posted here (in 3 zip files) is for review only. These files have had an initial review by Pete Djordjevich, necessary to release the casting for shipment to Major Tool – The files may be edited for format and/or content prior to the official release of the document package to PPPL.

10/4/05 – Roy Sheppard

Deleted weld chemistry reports & inserted chemistry reports from manufacturers

9/8/05 – Roy Sheppard

Inserted RT photos into C-2 Document package – Posted separate zip file of welding photos – These photos are NOT in Doc package

9/6/05 – Roy Sheppard

Created single document & new table of contents page – Renumbered shim documents so that they did not overlap with coil documents – Posted new file

8/30/05 – Roy Sheppard

Deleted duplicate files – Deleted obsolete Doc file & replaced with updated file

7/25/05 – Roy Sheppard

Deleted duplicate files saved in original ZIP – New Zip file posted

7/25/05 – Roy Sheppard

Corrected this file to correct note above by Pete Djordjevich. Note should read:

C2 shim spreadsheet has been updated to now show correct deviated chemistry. Section 4.2.1 now shows MN at 2.97 versus 2.8, and SI at .7 versus .5.  The correct dock specification, dock#1 has now been attached. The revised spreadsheet and dock #1-8 files are dated 6-29-05, the previous copies should be discarded.

6/29/05 - Roy Sheppard

Original QA release form for C-2 has also been updated – New version, dated 6/29 signed by Charles Ruud of Metal Tek

6/29/05 - Peter Djordjevich

C2 spreadsheet has been updated to now show correct deviated chemistry. Section 4.2.1 now shows MN at 2.97 versus 2.8, and SI at .7 versus .5.  The correct dock specification, dock#1 has now been attached. The revised spreadsheet and dock #1-8 files are dated 6-29-05, the previous copies should be discarded.