# Outstanding Materials Test Reports

|  | 77K Cryo |  |  |  | 293K Room Temp |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Property | Required | C-1 Casting Heat 27728 (averages) | LNM 4455 Electrode | Metrode B316NF Electrode | Required | C-1 Casting Heat 27728 (averages) | LNM 4455 Electrode | Metrode B316NF Electrode |
| Elastic Modulus | 21 Msi (144.8 Gpa) | Need New Test | Need 1 Test Bar | Need 1 Test Bar | 20 Msi (137.9 Gpa) | 21.0 | Need 1 Test Bar | Need 1 Test Bar |
| 0.2% Yield Strength | 72 ksi (496.4 Mpa) | _ | _ | _ | 34 ksi (234.4 Mpa) | 34,200 | _ | _ |
| Tensile Strength | 95 ksi (655 Mpa) | _ | _ | _ | 78 ksi (537.8 Mpa) | 83,800 | _ | _ |
| Elongation | 32% | _ | _ | _ | 36% | 51.5% | _ | _ |
| Charpy V – notch Energy | 35 ft. lbs. (47.4 J) | 78 | Need Charpy Coupon | Need Charpy Coupon | 60 ft-lbs (81.3 J) | 142 | 138 | 151 |