We are requesting a deviation for the chemistry for the 5 pieces C Coil and 6 pieces A Coil shim castings.

Two elements were slightly out of specification.  Both are within the original specification used for the proto type casting that passed the mechanical and cryogenic testing.

ENERGY INDUSTRIES OF OHIO

Purchase Order Number:  PPPL-FP-LTS-2

Material Specification:  CF8MNMN MOD

Pattern Number:  SE-141-033 COIL A SHIM - 6 Pieces

Pattern Number:  SE-141-073 COIL C SHIM - 5 Pieces

Element                  Min              Actual             Max

C                         0.040           0.070             0.070

CR                      18.000           18.100            18.500

MN                       2.300           2.970             2.800  Was 2.6-3.0

MO                      2.100           2.450             2.500

N                         0.240           0.255             0.280

NI                        13.000           13.120            13.500

P                         0.000           0.010             0.015

S                         0.000           0.010             0.015

SI                         0.000           0.700              0.500  Was 0.3 -0.7

Sincerely,

Peter Djordjevich

Peter Djordjevich

djord@earthlink.net

EarthLink Revolves Around You.