MANUFACTURING AND TEST SEQUENCE (MTS)

For Energy Industries of Ohio

# Coil C1

| OPER. # | STATION | DESCRIPTION OF PROCESS | INITIAL | DATE |
| --- | --- | --- | --- | --- |
| 10 | CAD Group | Verify the integrity of the Princeton models and assure it is the latest revision. Models need to be inspected for rips and tears. |  |  |
| 20 | CAD Group | Confirm critical dimensions with Princeton. Identify amounts of finish stock, tolerance of non-machined areas, and draft allowance. |  |  |
| 30 | CAD Group | Procure stock allowances from Major Machine, and shrink allowances from Metaltek. |  |  |
| 40 | CAD Group | Send out model for final approval to Dave Williamson, Major Machine, and Metaltek. |  |  |
| 50 | CAD Group | Post new model on-site for solidification modeling. |  |  |
| 60 | CAD Group | Create Pro-E pattern models for cope pattern and get approval from Metaltek. |  |  |
| 70 | Bench Group | Pull inventory, rough cut and glue up cope pattern for router machining. |  |  |
| 80 | CAM Group | Create Surfcam tool paths for cope pattern and verify tool paths using Surfcam verification program. |  |  |
| 90 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 100 | CAM Group | Setup pattern material blocks on router from datum points and run cope pattern complete. |  |  |
| 110 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 120 | CAD Group | Cope pattern, cores, and core boxes are checked as a final assembly upon completion. Failure of a core to fit or a closure problem will result in reworking of the core box to proper tolerance. Then the mold is reassembled for final dimensional verification. |  |  |
| 130 | CAD Group | Create Pro-E pattern models for drag pattern and get approval from Metaltek. |  |  |
| 140 | Bench Group | Pull inventory, rough cut and glue up drag pattern for router machining. |  |  |
| 150 | CAM Group | Create Surfcam tool paths for drag pattern and verify tool paths using Surfcam verification program. |  |  |
| 160 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 170 | CAM Group | Setup pattern material blocks on router from datum points and run drag pattern complete. |  |  |
| 180 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 190 | CAD Group | Drag pattern, cores, and core boxes are checked as a final assembly upon completion. Failure of a core to fit or a closure problem will result in reworking of the core box to proper tolerance. Then the mold is reassembled for final dimensional verification. |  |  |
| 200 | CAD Group | Create Pro-E pattern models for core box #1 and get approval from Metaltek. |  |  |
| 210 | Bench Group | Pull inventory, rough cut and glue up core box #1 for router machining. |  |  |
| 220 | CAM Group | Create Surfcam tool paths for core box #1 and verify tool paths using Surfcam verification program. |  |  |
| 230 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 240 | CAM Group | Setup pattern material blocks on router from datum points and run core box #1 complete. |  |  |
| 250 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 260 | CAD Group | Create Pro-E pattern models for core box #2 and get approval from Metaltek. |  |  |
| 270 | Bench Group | Pull inventory, rough cut and glue up core box #2 for router machining. |  |  |
| 280 | CAM Group | Create Surfcam tool paths for core box #2 and verify tool paths using Surfcam verification program. |  |  |
| 290 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 300 | CAM Group | Setup pattern material blocks on router from datum points and run core box #2 complete. |  |  |
| 310 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 320 | CAD Group | Create Pro-E pattern models for core box #3 and get approval from Metaltek. |  |  |
| 330 | Bench Group | Pull inventory, rough cut and glue up core box #3 for router machining. |  |  |
| 340 | CAM Group | Create Surfcam tool paths for core box #3 and verify tool paths using Surfcam verification program. |  |  |
| 350 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 360 | CAM Group | Setup pattern material blocks on router from datum points and run core box #3 complete. |  |  |
| 370 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 380 | CAD Group | Create Pro-E pattern models for core box #4 and get approval from Metaltek. |  |  |
| 390 | Bench Group | Pull inventory, rough cut and glue up core box #4 for router machining. |  |  |
| 400 | CAM Group | Create Surfcam tool paths for core box #4 and verify tool paths using Surfcam verification program. |  |  |
| 410 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 420 | CAM Group | Setup pattern material blocks on router from datum points and run core box #4 complete. |  |  |
| 430 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 440 | CAD Group | Create Pro-E pattern models for core box #5 and get approval from Metaltek. |  |  |
| 450 | Bench Group | Pull inventory, rough cut and glue up core box #5 for router machining. |  |  |
| 460 | CAM Group | Create Surfcam tool paths for core box #5 and verify tool paths using Surfcam verification program. |  |  |
| 470 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 480 | CAM Group | Setup pattern material blocks on router from datum points and run core box #5 complete. |  |  |
| 490 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 500 | CAD Group | Create Pro-E pattern models for core box #4 and get approval from Metaltek. |  |  |
| 510 | Bench Group | Pull inventory, rough cut and glue up core box #6 for router machining. |  |  |
| 520 | CAM Group | Create Surfcam tool paths for core box #6 and verify tool paths using Surfcam verification program. |  |  |
| 530 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 540 | CAM Group | Setup pattern material blocks on router from datum points and run core box #6 complete. |  |  |
| 550 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 560 | CAD Group | Create Pro-E pattern models for core box #7 and get approval from Metaltek. |  |  |
| 570 | Bench Group | Pull inventory, rough cut and glue up core box #7 for router machining. |  |  |
| 580 | CAM Group | Create Surfcam tool paths for core box #7 and verify tool paths using Surfcam verification program. |  |  |
| 590 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 600 | CAM Group | Setup pattern material blocks on router from datum points and run core box #7 complete. |  |  |
| 610 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 620 | CAD Group | Create Pro-E pattern models for core box #8 and get approval from Metaltek. |  |  |
| 630 | Bench Group | Pull inventory, rough cut and glue up core box #8 for router machining. |  |  |
| 640 | CAM Group | Create Surfcam tool paths for core box #8 and verify tool paths using Surfcam verification program. |  |  |
| 650 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 660 | CAM Group | Setup pattern material blocks on router from datum points and run core box #8 complete. |  |  |
| 670 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 680 | CAD Group | Create Pro-E pattern models for core box #9 and get approval from Metaltek. |  |  |
| 690 | Bench Group | Pull inventory, rough cut and glue up core box #9 for router machining. |  |  |
| 700 | CAM Group | Create Surfcam tool paths for core box #9 and verify tool paths using Surfcam verification program. |  |  |
| 710 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 720 | CAM Group | Setup pattern material blocks on router from datum points and run core box #9 complete. |  |  |
| 730 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 740 | CAD Group | Create Pro-E pattern models for core box #10 and get approval from Metaltek. |  |  |
| 750 | Bench Group | Pull inventory, rough cut and glue up core box #10 for router machining. |  |  |
| 760 | CAM Group | Create Surfcam tool paths for core box #10 and verify tool paths using Surfcam verification program. |  |  |
| 770 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 780 | CAM Group | Setup pattern material blocks on router from datum points and run core box #10 complete. |  |  |
| 790 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 800 | CAD Group | Create Pro-E pattern models for core box #5a and get approval from Metaltek. |  |  |
| 810 | Bench Group | Pull inventory, rough cut and glue up core box #5a for router machining. |  |  |
| 820 | CAM Group | Create Surfcam tool paths for core box #5a and verify tool paths using Surfcam verification program. |  |  |
| 830 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 840 | CAM Group | Setup pattern material blocks on router from datum points and run core box #5a complete. |  |  |
| 850 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 860 | CAD Group | Create Pro-E pattern models for core box #6a and get approval from Metaltek. |  |  |
| 870 | Bench Group | Pull inventory, rough cut and glue up core box #6a for router machining. |  |  |
| 880 | CAM Group | Create Surfcam tool paths for core box #6a and verify tool paths using Surfcam verification program. |  |  |
| 890 | CAM Group | Calibrate router per 5AX Calibration.doc. |  |  |
| 900 | CAM Group | Setup pattern material blocks on router from datum points and run core box #6a complete. |  |  |
| 910 | CAM Group | Calibrate router per 5AX Calibration.doc. If router has lost calibration during machining operation, all work after previous validation must be reviewed. If an out-of-tolerance condition exists, these items must be noted on a non-conforming material. After a non-conforming item is identified, EIO must be notified, and a review of Lawton quality and engineering must take place for disposition of item. |  |  |
| 920 | Bench Group | Final assembly of all components. This includes all sanding for cosmetics and painting to seal the wood. Pattern components are located and aligned using wooden dowel pins. Dowel pinholes were precisely located during the router operation per Pro-E model and Surfcam program. Inspection of various critical areas takes place in this operation using hand tools such as dial calipers and scales. |  |  |
| 930 | CAD Group | Laser scan finished patterns, cores, and core boxes. Then compare components to the Pro-E models. |  |  |
| 940 | Bench Group | Take digital photos on Thursday of each week to capture progress and solve problems. |  |  |
| 950 | Bench Group | Skid and crate all patterns components in a way that ensures complete protection from pattern damage. |  |  |
| 960 | Project Leader | Assist in molding and mold closing process at Metaltek. This ensures tooling will go together well through dimensional alignment. |  |  |
| 970 | Project Leader | Any non-conformance issues found are to be reported to EIO quality, at the time they are found regardless as to which step of the process is active. |  |  |