| OPER. # | STATION | DESCRIPTION OF PROCESS | Name | Date |
| --- | --- | --- | --- | --- |
| 10 | QUALITY RELEASE | REVIEW AND APPROVE MTS. RECEIVED APPROVAL FROM EIO ON ____________ FROM ____________ SIGNED QUALITY MANAGER |  |  |
| 20 | PATTERN NPAT SOP 0100REV2 | APPLY APPROPRIATE PART NUMBER, SERIAL NUMBER, FOUNDRY MARK, TO THE PATTERN. |  |  |
| 30 | MOLD MOLD SOP 0400 REV 8 CALIBRATION PER MOLD SOP 0900 REV 5 PREPARATION PER MOLD SOP 1100R2/1200R2/1300R1 SAND TESTING PER MOLD SOP 1400R2/1500R3/1600R2 | MOLD PER WORK INSTRUCTIONS IN MAPICS ROUTING AND SOPS REFERENCED. ENGINEER OF RECORD – ROGER BROMAN, CONSULT ON MOLD-RELATED CONCERNS. MOLD MATERIALS REQUIRED PER MAPICS BOM. NOTIFY ENGINEER OF ANY SUBSTITUTIONS. |  |  |
| 40 | POUR MELT SOP 0100R5 MELT SOP 0700R2 MELT SOP 0600R2 | METAL MUST BE AOD REFINED OR AOD INGOT. VIRGIN METAL ADDITIONS ALLOWED. RECORD POURING TEMPERATURE: __________ CASTING POURED AT: ________________ DATE: _______________ HEAT #”s: _____________________________ ELAPSED POUR TIME_____________ KEEL BLOCKS POURED: ____________ Sample from ladle to be analyzed for final chemical analysis and reported on material certifications. Sample Taken by:_______________ Analyzed: _________________Date: ________________ |  |  |
| 50 | MELT SOP 0800R2 | SHAKEOUT |  |  |
| 60 | ARC RISE SOP 0100R1 | REMOVE RISERS AS DIRECTED BY SUPERVISOR. |  |  |
| 70 | HEAT TREAT HEAT SOP 0103R5 | SOLUTION ANNEAL. With C-1 Coil. |  |  |
| 80 | PHYSICAL TESTING | OBTAIN TEST SPECIMENS AND SUBMIT FOR PHYSICAL TESTING. REPORT RESULTS AS PART OF STEP 480. |  |  |
| 90 | GRIND GSWA SOP 0100R3 GCHI SOP 0100R2 | SWING GRIND TO REMOVE RISER REMAINS AND FLASH IF REQUIRED. CHIP AND HAD GRIND SURFACE OF PART AS REQUIRED. |  |  |
| 100 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| 110 | VISUAL INSPECTION CQP-500 REV 4 | VISUALLY INSPECT 100% of COMPONENT ACCORDING TO ASTM A802 LEVEL 3 ALL CONDITIONS. IF OK CHECK HERE _______ . IF REJECTED CHECK HERE ____ . MARK AND REPAIR AT STEP 130. | VT - LEVEL II |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIOAND DCMA AT LEAST FIVE DAYS IN ADVANCE OF LP STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 120 | 100% L.P. CQP 0300 REV 10 | L.P. 100% OF COMPONENT. ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA- LEVEL 2. IF OK CHECK HERE ________ IF REJECTED CHECK HERE __________ MARK AND REPAIR AT STEP 120. | LP - LEVEL II |  |
| 130 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING 100% VISUAL AND LP INSPECTION. |  |  |
| 140 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA- LEVEL 2. | LP - LEVEL II |  |
| 150 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| 160 | WELD MAP | MAP ALL WELDS WITH DIGITAL PHOTO/MAPS. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA.. USE YELLOW MARKER. MUST SEND REPORT ON ALL WELDS OVER 10% OF NOMINAL WALL THICKNESS TO CUSTOMER. DEFECTS>10% YES ______, REPORT SENT BY _____________________ DATE______________ DEFECTS < 10 % __________________SIGN BY QA ENG. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIOAND DCMA AT LEAST FIVE DAYS IN ADVANCE OF XRAY AND LAYOUT STEPS. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 170 | CAF X-RAY CQP 401 REV 5 | X-RAY PER TECHNIQUE: To be determined. USE CALIBRATED DENSITOMETER FOR DENSITY VERIFICATION. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. | RT - LEVEL II |  |
| 180 | X-RAY CQP 401 REV 5 | X-RAY INTERPRETATION. ACCEPTANCE MSS SP 54. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. IF OK CHECK HERE ______ AND SEND TO STEP 310. REJECTED CHECK HERE ________ MARK UP DEFECTS AND SEND THE CASTING TO STEP 200. | RT – LEVEL II |  |
| 190 | LAYOUT | INSPECT CASTING TO VERIFY DIMENSIONS. THIS MAY BE PERFORMED BEFORE OR AFTER STEP 180. DIMENSIONED _________________ DATE _____________ RELEASED ____________(ENGINEER ONLY) |  |  |
| 200 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING RADIOGRAPHY. |  |  |
| 210 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. ACCEPTANCE CRITERIA- LEVEL 2. | LP - LEVEL II |  |
| 220 | WELD MAP | MAP ALL WELDS WITH DIGITAL PHOTO/MAPS. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE, FILE WITH QA.. MUST SEND REPORT ON ALL WELDS OVER 10% OF NOMINAL WALL THICKNESS TO CUSTOMER. DEFECTS>10% YES ______, REPORT SENT BY _____________________ DATE______________ DEFECTS < 10 % __________________SIGN BY QA ENG. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIOAND DCMA AT LEAST FIVE DAYS IN ADVANCE OF WELD STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 230 | QA APPROVAL HOLD POINT | QA TO APPROVE ELECTRODE PRIOR TO USE. PROCEDURE USED: ____________________ MATERIAL USED:__________________________ QUALITY ENG. Name: ____________________ Date: ____________ |
| 240 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1 FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |
| 250 | GRIND GCHI SOP 0100R2 | HAND GRIND WELDS. |  |  |
| 260 | L.P. WELD CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 2. IF OK CHECK HERE __________ WASH AND SEND TO STEP 300. IF REJECTED CHECK HERE __________AND RETURN TO STEP 220. | LP - LEVEL II |  |
|  | Repeat | Repeat steps __220 to 260___as required till clear through Visual Inspection & Penetrant Inspection. Document rework on a supplemental MTS | QA ENG. |  |
| 270 | TEST MAG PERM SOP MAG PERM 100, REV 1 | TEST MAG PERMEABILITY REPAIR AREAS RECORD ON WELD MAP LIST. TEST AT LEAST 5 POINTS PER WELD. ACCEPTANCE 1.02. IF OK CHECK HERE _______AND GO TO STEP 290. IF REJECTED CHECK HERE _______. |  |  |
| 280 | GRIND GCHI SOP 0100R2 | GRIND AREAS OF NON COMPLIANCE AND RETURN TO STEP 270. REPEAT UNTILL COMPLIANCE IS ACHIEVED. |  |  |
| 290 | CAF X-RAY DEFECTS REPAIRED BY WELDING CQP 401 REV 5 | X-RAY PER TECHNIQUE: To be determined. USE CALIBRATED DENSITOMETER FOR DENSITY VERIFICATION. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. | RT - LEVEL II |  |
| 300 | X-RAY CQP 401 REV 5 | X-RAY INTERPRETATION. ACCEPTANCE MSS SP 54. ATTACH TECHNIQUE, READER SHEET FOR ALL RADIOGRAPHS. MUST INDICATE RADIOGRAPHER AND ASNT CERTIFICATION LEVEL ON READER SHEET. IF OK CHECK HERE ______ AND SEND TO STEP 310. REJECTED CHECK HERE ________ MARK UP DEFECTS AND SEND THE CASTING TO STEP 200. | RT - LEVEL II |  |
|  | Repeat | Repeat steps __200 TO 300____as required till welds clear X-RAY. Document rework on a supplemental MTS | QA ENG. |  |
| 310 | SAND BLAST BLAS SOP 0100R6 | SANDBLAST (REMOVE ALL BLAST MATERIAL FROM CASTING) SANDBLASTING WILL BE DONE USING RECYCLED SHARP ANGULAR AGGREGATE. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIOAND DCMA AT LEAST FIVE DAYS IN ADVANCE OF VISUAL AND LP STEPS. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 320 | FINAL VISUAL INSPECTION CQP-500 REV 4 | VISUALLY INSPECT 100% of COMPONENT ACCORDING TO ASTM A802 LEVEL 2 ALL CONDITIONS. IF OK CHECK HERE _______. IF REJECTED CHECK HERE __________ . MARK AND REPAIR AT STEP 340. MUST BE PERFORMED BY LEVEL II in VT. | VT - LEVEL II |  |
| 330 | FINAL L.P. CQP 0300 REV 10 | FINAL L.P. 100% OF COMPONENT. ACCEPTANCE PER ASTM A903. ACCEPTANCE CRITERIA-LEVEL 1 FOR HIGH STRESSED AREAS, LEVEL 2 FOR ALL OTHER AREAS. SEE LP DRAWING. IF OK CHECK HERE __________ WASH AND SEND TO STEP 410. IF REJECTED CHECK HERE __________ | LP - LEVEL II |  |
| 340 | WELD SOP 0100 REV 7 | EXCAVATE ANY DEFECTS FOUND DURING FINAL PENETRANT INSPECTION. |  |  |
| 350 | L.P. EXCAVATION CQP-300 REV 10 | L.P. ALL EXCAVATIONS PRIOR TO WELDING TO ENSURE REMOVAL OF DEFECT. ACCEPTANCE PER A903. | LP - LEVEL II |  |
| 370 | WELD MAP | MAP ALL WELDS WITH DIGITAL PHOTO/MAPS. SERIALIZE DEFECTS ON CASTING, USE SCALE IN PHOTOS AND DOCUMENT SIZE. THIS IS TO BE PERFORMED BY SUPERVISOR, INSPECTION LEAD MAN OR THEIR DESIGNEE. FILE WITH QA. MUST SEND REPORT ON ALL WELDS OVER 10% OF NOMINAL WALL THICKNESS TO CUSTOMER. NOMINAL WALL THICKNESS TO CUSTOMER. DEFECTS.>10% YES ______, REPORT SENT BY ________________________ DATE____________ DEFECTS < 10 % __________________SIGN BY QA ENG. |  |  |
| 380 | WELD SOP 0100 REV 7 | WELD REPAIR DEFECTS AS MARKED. FOR WELDS <2” - WPS 10-SMAW-CF8MNMN MOD REV 1 FOR WELDS <8” - WPS 15-GMAW-CF8MNMN MOD REV 2 |  |  |
| 390 | GRIND GCHI SOP 0100 REV 2 | HAND GRIND WELDS. |  |  |
| 400 | L.P. WELDS CQP 0300 REV 10 | L.P. WELD REPAIRS ACCEPTANCE PER ASTM A903. IF OK CHECK HERE __________ WASH AND SEND TO STEP 460. IF REJECTED CHECK HERE __________AND RETURN TO STEP 390. | LP - LEVEL II |  |
|  | Repeat | Repeat steps ___390 TO 410_____as required till welds clear Final Liquid Penetrant Inspection. Document rework on a supplemental MTS | qa eng. |  |
| 410 | TEST MAG PERM SOP MAG PERM 100, REV 1 | TEST MAG PERMEABILITY REPAIR AREAS. RECORD ON WELD MAP LIST. TEST AT LEAST 5 POINTS PER WELD. ACCEPTANCE 1.02. IF OK CHECK HERE _______AND GO TO STEP 430. |  |  |
| 420 | GRIND GCHI SOP 0100R2 | GRIND AREAS OF NON COMPLIANCE AND RETURN TO STEP 420. REPEAT UNTILL COMPLIANCE IS ACHIEVED. |  |  |
| NOTICE | WITNESS NOTIFICATION | PROVIDE NOTICE TO EIOAND DCMA AT LEAST FIVE DAYS IN ADVANCE OF MAG PERM STEP. EIO NOTIFIED ON _____________ DCMA NOTIFIED ON _______________ | Q ENG OR QA MGR |  |
| 430 | FINAL MAG PERM INSPECTION SOP MAG PERM 100, REV 1 | PERFORM MAG PERM TESTING WITH SEVRIN GAUGE. ACCEPTANCE 1.02. CHECK THE ENTIRE SURFACE ON A 6”BY6” GRID. REPORT RESULTS. USE A 6” SQUARE BLOCK TO INDICATE TEST LOCATIONS AND RECORD RESULTS. COMPLIANT AREAS WILL NOT BE MARKED. MARK NONCOMPLIANT AREAS WITH AN “X” FOR REPAIR. OK CHECK HERE _____AND GO TO STEP 470. IF REJECTED CHECK HERE ______. |  |  |
| 440 | GRIND GCHI SOP 0100 REV 2 | HAND GRIND WITH SUITABLE CONE OR OTHER SIMILAR GRINDER AS REQUIRED TO ENSURE REMOVAL OF MATERIAL TO ACHIEVE MAG PERM REQUIREMENT. CIRCLE AREA REMEDIATE FOR RETEST. |  |  |
| 450 | RETEST MAG PERM SOP MAG PERM 100, REV 1 | RETEST MAG PERMEABILITY AT FAILED TEST POINTS. MARK NONCOMPLIANT AREAS WITH AN “X” FOR REPAIR. ACCEPTANCE 1.02. IF OK CHECK HERE _______. IF REJECTED CHECK HERE _______RETURN TO STEP 450 |  |  |
| 460 | PHOTOGRAPH | TAKE DIGITAL PICTURES. |  |  |
| 470 | AUDIT REVIEW | PROCESS DOCUMENT TO PROGRAM MANAGER FOR COMPLIANCE AUDIT. |  |  |
| 480 | DOC. REVIEW | REVIEW DOCUMENTS AS REQUIRED IN CAF CHECKLIST, ALL DOCUMENTS NOTED TO BE ACCESSIBLE FOR AUDITING. (SHIPPER, C OF C, M.T.R., M.T.S., INSPECTION REPORT, X-RAY READER SHEETS AND HEAT TREAT CHARTS) |  |  |
| NOTICE | RELEASE FROM EIO | PROVIDE DOCUMENTS TO EIO. SENT ON ____________ BY __________________. RECEIVED RELEASE FROM EIO ON _________________. | Q ENG OR QA MGR |  |
| 490 | PACK AND SHIP | PACKAGE AND SHIP TO MAJOR TOOL. |  |  |
| 1000 | REVISION HISTORY | ORIGINAL 12-14-04. | CARUUD |  |