Statement of Work:  Modular Coil Winding Form Materials 
Test Specimens

1.  To provide NCSX with cast material for testing,  access holes indicated in the drawing below shall be cut from the Type C Prototype to the maximum diameter possible while still allowing enough stock for clean up on the prototype casting.

2.  Piece B shall be cut into (4) quarters and shipped to MetalTek where it shall be welded back together using MetalTek's weld procedures for the "production" winding.  As soon as completed, it shall be shipped to the address in (4) below.

3. If MetalTek has a spare polidal break shim available from the C1 casting, it shall cut the break in half along its narrow dimension and weld it back together as in (2).  Ship to address below as soon as completed.

4.  Pieces A,C, and D shall be shipped immediately after cutting to PPPL, James Forrestal Campus, Rt. 1 N, Rec. 3, C-Site, Princeton, NJ 08543  Attn:  P. Heitzenroeder.

# Text boxes

A

B

C

D