Page: 1

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Drawing ID / Rev

Sub ID

Part ID

Qty

SE120 / --

1

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

0

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

700-BLUE TEAM, ENGINEERING

SE120 / --

Sub: 0 / Seq: 10

1.00

1.00

1.00

(U)

ENGINEERING / PROJECT MANAGEMENT

SOW 3.2.1 TASK 2

MIT/QA PLANS FOR PVVS FOR VVSA

SOW 3.1 TASK 1

3.1.1 METHODS FOR FABRICATING VVSA

3.1.2 DESIGN CHANGES

3.1.3 PRELIMINARY MIT/AQ FOR VVSA

3.1.4  BUDGETARY COST/SCHEDULE FOR VVSA

SOW 3.3.1 &  SOW 3.3.2 Task 8

3.3.1 FINAL MIT/QA FOR VVSA

3.3.2 FINAL COST/SCHEDULE FOR VVSA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

4434

200.0

SE120 / --

INCONEL625_062_GTAW-WELD WIRE/GTAW, .062 DIA

10

Vendor Part ID: INCONEL625_062_GTAW

Mfg Part ID: INCONEL 625

(U)

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

4434

300.0

SE120 / --

INCONEL625_093_GTAW-WELD WIRE/GTAW, .093 DIA

20

Vendor Part ID: INCONEL625_093_GTAW

Mfg Part ID: INCONEL 625

(U)

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

753-CAD/CAM - LARGE MILLING

SE120 / --

Sub: 0 / Seq: 20

1.00

1.00

1.00

(U)

N/C PROGRAMMING

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

825-FINAL INSPECTION - PLANTS 1 &

SE120 / --

Sub: 0 / Seq: 30

1.00

1.00

1.00

(U)

FINAL VISUAL INSPECTION

NOTE:  (3) 180 DEGREE PERIODS

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

425-SHIPPING - PLANTS 1 & 2

SE120 / --

Sub: 0 / Seq: 40

1.00

1.00

1.00

(U)

SHIP PER CUSTOMER RELEASE FORM

SHIPPING CONFIGURATION TBD (ENGINEERING / CUSTOMER INPUT REQUIRED)

(CONTAINER MANUFACTURED IN SUB I.D. 2)

AT A MINIMUM ENSURE THE PART IS COMPLETELY WRAPPED WITH PLASTIC FOAM AND SHRINK WRAPPED.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 2

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

SPECIAL CRATE REQUIREMENTS:

CONTAINER MUST BE CLEARLY MARKED WITH THE FOLLOWING INFORMATION:

SUPPLIER:

MAJOR TOOL & MACHINE, INC.

1458 E. 19TH ST.

INDIANAPOLIS, IN 46218

CONTENTS:

SE120-001 NCSX VVSA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 0 / Seq: 50

1.00

1.00

1.00

MISC/SUBLET

(U)

FREIGHTLINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

SE120 / --

1

VVSA 360 DEGREE ASSEMBLY

1

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 1 / Seq: 10

1.00

1.00

1.00

(U)

1.  FINAL COSMETICS

2.  TEST FIT ASSEMBLE THE THREE 120 DEGREE PERIODS TOGETHER.  (ENGINEERING, Q/A, AND CUSTOMER SOURCE WITNESS REQUIRED).

NOTE THAT THIS SEQUENCE IS CONTINGENT PARTS DO NOT SHIP INDIVIDUALLY AS COMPLETED.

3.  TOUCH UP CLEAN PART PER CLEANING PROCEDURE NCSX-CSPEC-120-01-00, 3.3.2.4

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 1 / Seq: 20

1.00

1.00

1.00

(U)

WITNESS / VERIFY ASSEMBLY.

VERIFY CLEANLINESS.

COORDINATE ENGINEERING / CUSTOMER WITNESS.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

SE120 / --

3

VVSA 120 DEGREE PERIOD

4

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 4 / Seq: 10

3.00

3.00

3.00

(U)

POSITION SETS OF (2) 60 DEGREE SEGMENTS ONTO THE FABRICATING AND MACHINING FIXTURE.

SMX LASER TRACKER TO ASSIST SETUP AND VERIFY PROFILE PRIOR TO FITTING AND WELDING.

TRIM, FIT, PREP, AND TACK WELD (ONLY) EACH SET OF (2) 60 DEGREE PERIODS INTO A 120 DEGREE PERIOD.

AFTER PARTS ARE COMPLETETELY TACKED TOGETHER NOTIFY Q/A FOR ALIGNMENT / PROFILE VERIFICATION (REQUIRED PRIOR TO PROCEDING).

NOTE SEQUENCE QUANTITY OF 3 PROVIDES 3 120 DEGREE  SUB-ASSEMBLIES

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 4 / Seq: 20

3.00

3.00

3.00

(U)

LASER TRACKER.  VERIFY PROFILE OF TACK WELDED 120 DEGREE PERIODS.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 3

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

VERIFY WELD JOINT ALIGNMENT.

RECORD IDC DATA

Part Number: 120 DEGREE PERIOD

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 4 / Seq: 30

3.00

3.00

3.00

(U)

WELD THE CENTER JOINT.

BACK PURGE THE OUTSIDE WELD JOINT SURFACES.  PURGE DAM MATERIAL MUST BE MADE FROM EITHER 625 INCONEL OR 300 SERIES STAINLESS STEEL.

WELD ROOT PASSES (INCREMENTALLY, USING BACK-STEPPING METHOD TO MINIMIZE SHRINKAGE) ON ALL WELD JOINTS.

CWI VISUAL INSPECTION / ACCEPTANCE REQUIRED FOR EACH PASS PRIOR TO COVERING.  100% UNDER 8X MAGNIFICATION PER ASME CODE ARTICLE 6, SECTION V.

ACCEPTANCE PER AWS D1.6, 6.29.1.

MAGNETIC PERMEABILITY INSPECTION OF EACH ROOT PASS AND IT'S HEAT AFFECTED ZONE IS ALSO REQUIRED.  NOTIFY Q/A AFTER EACH ROOT PASS IS COMPLETED

FOR VERIFICATION.

BLEND SMOOTH

TOUCH UP POLISH THE INTERIOR SURFACE

PREPARE FOR FLANGE MACHINING / PORT SPOT LOCATION

0

Program Count:

Drawing Count:

0

1

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 4 / Seq: 40

3.00

3.00

3.00

(U)

PROFILE VERIFICATION PRIOR TO MACHINING THE FLANGES

MAGNETIC PERMEABILITY VERIFICATION (AFTER EACH PASS OF WELD IS APPLIED)

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

162-DORRIES SCHARMANN GANTRY

SE120 / --

Sub: 4 / Seq: 50

3.00

3.00

3.00

(U)

LOAD THE CRADLE AND 120 DEGREE PERIOD ONTO THE MACHINE TABLE.  POSITION AND SETUP TO DATUM TARGET ALIGMENT POINTS, N/C THE FLANGE FACING UP

(ANGLED) COMPLETE PER DRAWING / PROGRAM (FACE, GROOVE, AND HOLES).  SPOT / QUALIFY THE FLANGE ANGLED DOWNWARD IN THIS SETUP FOR MACHINING

AFTER THE PART IS INVERTED.

NOTIFY Q/A FOR VERIFICATION

NOTIFY FABRICATING FOR PORT INSTALLATION

POSTION AND INDICATE THE TOOLING BALL OF EACH PORT SUB-ASSEMBLY TO ASSIST INSTALLATION AND TACK WELDING IN PLACE.

NOTE THAT THIS WILL BE PERFORMED ONE SIDE AT A TIME.  AFTER THE PERIPHERAL, AND TOP FACING PORT SUB-ASSEMBLIES ARE POSITIONED AND FIRMLY TACK

WELDED, REMOVE THE PART FROM THE MACHINE FOR WELDING THESE PORTS (PERFORMED IN FOLLOWING SEQUENCE), AND RE-POSITIONING.  THE PART WILL BE

RETURNED INVERTED FOR RE-ALIGNMENT, POSITIONING AND TACK WELDING THE LOWER PORT SUB-ASSEMBLIES.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 4 / Seq: 52

3.00

3.00

3.00

(U)

WHILE PART IS STILL ON MACHINE, POSITION AND FIT THE ACCESSIBLE PORT SUB-ASSEMBLIES (FACING UP AND OUT).  THE MACHINE TOOL WILL PROVIDE THE EXACT

LOCATION (PLUS CALCULATED WELD SHRINKAGE ALLOWANCE) FOR EACH PORT SUB-ASSEMBLY.

INSTALL ADEQUATE TEMPORARY BRACING TO ENSURE THE PORT SUB-ASSEMBLIES DO NOT MOVE PRIOR TO PERMANENT INSTALLATION.

AFTER ALL ACCESSIBLE PORT SUB-ASSEMBLIES ARE FIRMLY TACK WELDED (AND BRACED) IN PLACE, REMOVE THE CRADLE AND 120 DEGREE PERIOD FROM THE

MACHINE TOOL AND INSTALL IT ONTO A WELDING POSITIONER AND WELD PER THE FOLLOWING:

BACK PURGE THE OUTSIDE WELD JOINT SURFACES.  PURGE DAM MATERIAL MUST BE MADE FROM EITHER 625 INCONEL OR 300 SERIES STAINLESS STEEL.

WELD ROOT PASSES (INCREMENTALLY, USING BACK-STEPPING METHOD TO MINIMIZE SHRINKAGE) ON ALL WELD JOINTS.

CWI VISUAL INSPECTION / ACCEPTANCE REQUIRED FOR EACH PASS PRIOR TO COVERING.  100% UNDER 8X MAGNIFICATION PER ASME CODE ARTICLE 6, SECTION V.

ACCEPTANCE PER AWS D1.6, 6.29.1.

MAGNETIC PERMEABILITY INSPECTION OF EACH ROOT PASS AND IT'S HEAT AFFECTED ZONE IS ALSO REQUIRED.  NOTIFY Q/A AFTER EACH ROOT PASS IS COMPLETED

FOR VERIFICATION.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 4

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

BLEND SMOOTH

TOUCH UP POLISH THE INTERIOR SURFACE

INSTALL THE 120 DEGREE PERIOD ONTO THE ELEVATED CRADLE FOR MACHINING THE SECOND FIELD JOINT FLANGE, AND POSITIONING THE LOWER PORT

SUB-ASSEMBLIES.  ENSURE THE PART IS SECURED FIRMLY TO REDUCE EXCESS CHATTER CAUSED BY ELEVATION AND SUBSEQUENT LACK OF REGIDITY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 4 / Seq: 53

3.00

3.00

3.00

(U)

INSPECT FLANGE MACHINING AND PORT LOCATION ON MACHINE.  RE-INSPECT PORT LOCATION AFTER WELDING.  (LASER TRACKER)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

162-DORRIES SCHARMANN GANTRY

SE120 / --

Sub: 4 / Seq: 55

3.00

3.00

3.00

(U)

RE-POSITION 120 DEGREE PERIOD TO DATUM TARGET ALIGMENT POINTS, N/C REMAINING FIELD JOINT FLANGE FACE (NOW ANGLED UP) COMPLETE PER DRAWING /

PROGRAM.

NOTIFY Q/A FOR VERIFICATION

NOTIFY FABRICATING FOR PORT INSTALLATION.

POSTION AND INDICATE THE TOOLING BALL OF EACH PORT SUB-ASSEMBLY TO ASSIST INSTALLATION AND TACK WELDING IN PLACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 4 / Seq: 57

3.00

3.00

3.00

(U)

WHILE PART IS STILL ON MACHINE, POSITION AND FIT THE REMAINING PORT SUB-ASSEMBLIES (NOW FACING UP).  THE MACHINE TOOL WILL PROVIDE THE EXACT

LOCATION (PLUS CALCULATED WELD SHRINKAGE ALLOWANCE) FOR EACH PORT SUB-ASSEMBLY.

INSTALL ADEQUATE TEMPORARY BRACING TO ENSURE THE PORT SUB-ASSEMBLIES DO NOT MOVE PRIOR TO PERMANENT INSTALLATION.

AFTER ALL REMAINING PORT SUB-ASSEMBLIES ARE FIRMLY TACK WELDED (AND BRACED) IN PLACE, REMOVE THE CRADLE AND 120 DEGREE PERIOD FROM THE

MACHINE TOOL AND INSTALL IT ONTO A WELDING POSITIONER AND WELD PER THE FOLLOWING:

BACK PURGE THE OUTSIDE WELD JOINT SURFACES.  PURGE DAM MATERIAL MUST BE MADE FROM EITHER 625 INCONEL OR 300 SERIES STAINLESS STEEL.

WELD ROOT PASSES (INCREMENTALLY, USING BACK-STEPPING METHOD TO MINIMIZE SHRINKAGE) ON ALL WELD JOINTS.

CWI VISUAL INSPECTION / ACCEPTANCE REQUIRED FOR EACH PASS PRIOR TO COVERING.  100% UNDER 8X MAGNIFICATION PER ASME CODE ARTICLE 6, SECTION V.

ACCEPTANCE PER AWS D1.6, 6.29.1.

MAGNETIC PERMEABILITY INSPECTION OF EACH ROOT PASS AND IT'S HEAT AFFECTED ZONE IS ALSO REQUIRED.  NOTIFY Q/A AFTER EACH ROOT PASS IS COMPLETED

FOR VERIFICATION.

BLEND SMOOTH

TOUCH UP POLISH THE INTERIOR SURFACE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 4 / Seq: 58

3.00

3.00

3.00

(U)

INSPECT FLANGE MACHINING AND PORT LOCATION ON MACHINE.  RE-INSPECT PORT LOCATION AFTER WELDING.  (LASER TRACKER)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 4 / Seq: 60

3.00

3.00

3.00

(U)

INSPECT ON MACHINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 4 / Seq: 70

3.00

3.00

3.00

(U)

PREPARE 120 DEGREE UNITS FOR VACUUM TEST.

INSTALL SEALS AND COVER PLATES TO THE FIELD JOINTS.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 5

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

36.0

10

(U)

FIELD JOINT SEALS

Material Certification:

Part Number: FIELD JOINT SEALS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

900.0

20

(U)

.625-11UNC-2A X 3.0 SHCS

Material Certification:

Part Number: .625-11UNC-2A X 3.0 SHCS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

900.0

30

(U)

.625-11UNC-2B HEX NUT

Material Certification:

Part Number: .625-11UNC-2B HEX NUT

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

900.0

40

(U)

.625 FLAT WASHER

Material Certification:

Part Number: .625 FLAT WASHER

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

SE120 / --

Sub: 4 / Seq: 73

3.00

3.00

3.00

MISC/SUBLET

(U)

VACUUM TEST THE 120 DEGREE PERIOD, AND EACH PORT SUB-ASSEMBLY INDIVIDUALLY PER THE FOLLOWING:

THE VESSEL UNDER TEST SHALL BE EVACUATED USING A TURBO MOLECULAR PUMP TO AN INTERNAL PRESSURE OF LESS THAN OR EQUAL TO 1 X 10(-7) TORR.  THE

TOTAL HELIUM LEAK RATE FOR THE PORT EXTENSION SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S.

Part Number: SE120

Part Description: VVSA.

Customer: PPPL

Test Certification: VACUUM TEST CERTIFICATE  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

Sub: 4 / Seq: 80

3.00

3.00

3.00

(U)

CUT THE PORT OPENINGS IN THE VESSEL WALL.

GRIND / BLEND AT LEAST 1/16" OF MATERIAL FROM CUT EDGE TO COMPLETELY REMOVE THE RECAST LAYER AND HEAT AFFECTED ZONE.

TOUCH UP POLISH THE AFFECTED SURFACED TO RESTORE TO A 32 MICRO-INCH SURFACE FINISH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 4 / Seq: 93

3.00

3.00

3.00

(U)

FINAL DIMENSIONAL INSPECTION.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

SE120 / --

6

VVSA 60 DEGREE PERIOD

5

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 6

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 5 / Seq: 10

6.00

6.00

6.00

(U)

FABRICATION OPERATION # 1

1.  INSTALL 9 DIE FORMED PANELS AND 1 FIELD JOINT FLANGE ONTO FABRICATION FIXTURE.  TRIM, FIT, AND ALIGN EACH PANEL TO IT'S RESPECTIVE ADJACENT PANELS

AND FIXTURE REST STOPS.  NOTE THAT THE FIXTURE REST STOPS ARE POSITIONED AT NOMINAL (+.090") GEOMETRIC POSITION TO AVOID STARTING ANY LOWER THAN

MID-TOLERANCE.  GAPS BETWEEN THE PRODUCTION PANELS AND FIXTURE REST STOPS (UP TO .090") ARE PERMITTED.

ALIGN AND TACK WELD (ONLY) PANELS TOGETHER.

ENSURE EACH PANEL IS ALIGNED SMOOTH AND CONTINUOUS TO ITS ADJACENT MEMBER AND MIS-MATCH IS MINIMIZED.  CWI / ENGINEERING CONCURRENCE

REQUIRED.

ASSIST Q/A WITH PROFILE VERIFICATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

Part Number: VVSA 60 DEGREE PERIOD

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 5 / Seq: 20

6.00

6.00

6.00

(U)

INSPECTION OPERATION # 1

AFTER THE PART IS COMPLETELY TACK WELDED, INSPECT / VERIFY POSITIONING, FITUP, AND PROFILE OF TACK WELDED PERIOD PER THE FOLLOWING:

ENSURE THE PART PROFILE IS WITHIN THE UPPER HALF OF THE APPLIED BI-LATERAL TOLERANCE AS FOLLOWS:  VARIFY THAT NO INSPECTION POINT IS ABOVE THE

HIGH LIMIT OF TOLERANCE (OUTWARD) OR BELOW NOMINAL (INWARD).

RECORD ACTUAL (HIGH/LOW RANGE) ON MTM IDC

REPORT ANY OUT OF TOLERANCE READINGS VIA MTM NCR.

NOTIFY ENGINEERING (DOUG McCORKLE) FOR EVALUATION OF RESULTS PRIOR TO RELEASING PART.

ENSURE THE PART / FIXTURE DATUM TARGETS ARE ADEQUATELY POSITIONED FOR THE NEXT SEQUENTIAL INSPECTION

INSPECT AND RECORD THE MAGNETIC PERMEABILITY OF THE WELDS AND HEAT AFFECTED ZONES.

Part Number: VVSA 60 DEGREE PERIOD

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 5 / Seq: 30

6.00

6.00

6.00

(U)

FABRICATION OPERATION # 2

INSTALL EXTERIOR STIFFENING FEATURES (FIXTURING) TO THE VESSEL.  TACK WELD THE STIFFENERS TO THE PART.

NOTE THAT THE STIFFENER MATERIAL IS ALSO INCO 625, NO TABS REQUIRED.

BACK PURGE THE OUTSIDE WELD JOINT SURFACES.  PURGE DAM MATERIAL MUST BE MADE FROM EITHER 625 INCONEL OR 300 SERIES STAINLESS STEEL.

WELD ROOT PASSES (INCREMENTALLY, USING BACK-STEPPING METHOD TO MINIMIZE SHRINKAGE) ON ALL WELD JOINTS.

CWI VISUAL INSPECTION / ACCEPTANCE REQUIRED FOR EACH PASS PRIOR TO COVERING.  100% UNDER 8X MAGNIFICATION PER ASME CODE ARTICLE 6, SECTION V.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 7

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

ACCEPTANCE PER AWS D1.6, 6.29.1.

MAGNETIC PERMEABILITY INSPECTION OF EACH ROOT PASS AND IT'S HEAT AFFECTED ZONE IS ALSO REQUIRED.  NOTIFY Q/A AFTER EACH ROOT PASS IS COMPLETED

FOR VERIFICATION.

Test Certification: WELD INSPECTION CERTIFICATION  Rev:

Part Number: VVSA 60 DEGREE PERIOD

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 5 / Seq: 40

6.00

6.00

6.00

(U)

INSPECTION OPERATION # 2

AFTER THE ROOT WELDS ARE COMPLETE (FABRICATION DEPT. WILL COORDINATE); RE-INSPECT / VERIFY PART PROFILE IS WITHIN APPLIED TOLERANCE AND RECORD

WELDING SHRINKAGE / DISTORTION REALIZED TO THIS POINT.

RECORD ACTUAL (INDIVIDUAL) MEASUREMENTS ON INSPECTION FORM (SE120-2MTM).

INSPECT AND RECORD MAGNETIC PERMEABILITY.

REPORT ANY OUT OF TOLERANCE READINGS VIA MTM NCR.

NOTIFY ENGINEERING (DOUG McCORKLE) FOR EVALUATION OF RESULTS PRIOR TO RELEASING PART.

ENSURE THE FIXTURE DATUM TARGETS ARE ADEQUATELY POSITIONED FOR THE NEXT SEQUENTIAL INSPECTION.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 5 / Seq: 70

6.00

6.00

6.00

(U)

FABRICATION OPERATION # 4

AFTER OBTAINING ENGINEERING PROFILE ACCEPTANCE, WELD THE REMAINDER OF THE  STRUCTURAL WELD JOINTS (SEQUENCE WELDING TO MINIMIZE DISTORTION

AND NUMBER OF INTER-PASSES).

AFTER WELDING IS COMPLETE, REMOVE THE OUTSIDE STIFFENING PLUG.  BLEND / TOUCH UP ATTACHMENT WELDS AS REQUIRED.

LAYOUT THE PORT ASSEMBLY LOCATION.  (ANGULAR LOCATION / OVERALL LENGTH  AND OUTLINE ARE SCRIBED ON FIXTURE). **********(HEIGHT FROM FIXTURE

PLATE TO CENTER OF TUBE NEEDED (IN ROUTING))**********

POSITION AND WELD THE PORT SUB-ASSEMBLY IN PLACE PER DRAWING.

FINISH POLISHING AND CLEANING THE INTERIOR SURFACES OF THE PORT SUB-ASSEMBLY.  RESTORE TO A 32 MICRO-INCH SURFACE FINISH.  REFER TO CLEANING

PROCEDURE # ?????

INSTALL THE VACUUM TEST CAP TO THE CONFLAT FLANGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 5 / Seq: 100

6.00

6.00

6.00

(U)

INSPECTION OPERATION # 3

PROFILE VERIFICATION.

VERIFY MAGNETIC PERMEABILITY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE120 / --

Sub: 5 / Seq: 110

6.00

6.00

6.00

(U)

MASK THE INTERIOR SURFACES AND FLANGE FACE.  BLAST THE OUTSIDE SURFACE 100% USING 220 GRIT VIRGIN ALUMINUM OXIDE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE120 / --

Sub: 5 / Seq: 115

6.00

6.00

6.00

(U)

REMOVE MASKING AND PROTECTIVE PLASTIC

FINISH POLISHING 60 DEGREE SEGMENT (TOUCH UP)

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 8

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

CLEAN PART PER CLEANING SPECIFICATION (TBD)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE120 / --

Sub: 5 / Seq: 120

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE STRUCTURAL WELDS AND VESSEL WALL

RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 1

7

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 7 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5880

1810

35,280.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 1

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 7 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAGNETIC PERMEABILITY CERT.  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 1

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 7 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 9

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 7 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 1

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 7 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 7 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 7 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 1

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 7 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 7 / Seq: 40

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

RE-STRIKE PANEL TO RESTORE PROFILE

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 7 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 10

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 7 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 7 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 1

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 2

9

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 9 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

2035

1810

12,210.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 2

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 9 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 11

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 2

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 9 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 9 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 2

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 9 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 9 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 9 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 2

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 9 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 12

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 9 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 9 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 9 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 9 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 2

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 3

10

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 10 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5829

1810

34,974.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 13

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 3

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 10 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 3

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 10 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 10 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 3

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 10 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 10 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 10 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 14

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Part Number: VVSA PANEL # 3

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 10 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 10 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 10 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 10 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 10 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 3

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 4

11

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 11 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 15

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

2117

1810

12,702.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 4

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 11 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 4

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 11 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 11 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 4

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 11 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 16

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 11 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 11 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 4

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 11 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 11 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 11 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 11 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 11 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 4

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 17

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 5

12

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 12 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

4004

1810

24,024.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 5

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 12 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 5

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 12 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 12 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 18

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 5

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 12 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 12 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 12 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 5

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 12 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 12 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 12 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 12 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 19

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 12 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 5

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 6

21

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 21 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

2800

1810

16,800.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 6

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 21 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 6

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 21 / Seq: 20

6.00

6.00

6.00

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 20

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 21 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 6

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 21 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 21 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 21 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 6

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 21 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 21 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 21

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 21 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 21 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 21 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 6

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 7

22

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 22 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1500

1810

9,000.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 7

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 22

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 22 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 7

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 22 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 22 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 7

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 22 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 22 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 22 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 7

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 22 / Seq: 35

6.00

6.00

6.00

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 23

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 22 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 22 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 22 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 22 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 7

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 8

23

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 23 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

3500

1810

21,000.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 24

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 8

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 23 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 8

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 23 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 23 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 8

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 23 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 23 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 25

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 23 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 8

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 23 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 23 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 23 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 23 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 23 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 8

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VVSA PANEL # 9

24

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 26

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

SE121 / A

Sub: 24 / Seq: 10

6.00

6.00

6.00

(U)

PRIOR TO HANDLING AND CUTTING PLATE MATERIAL, NOTIFY Q/A FOR SURFACE FINISH, PLATE THICKNESS, AND MAGNETIC PERMEABILITY VERIFICATION.

1.  NEST AND PROGRAM PER PROVIDED GEOMETRY.

2.  BURNOUT AND CLEANUP PANEL PER NESTING / PROGRAM.

3.  CLEANUP EDGES.  ENSURE ALL DROSS AND RE-CAST LAYER IS REMOVED, BLENDED SMOOTH, AND CORNERS ARE SLIGHTLY RADIUSED.

4.  NOTIFY Q/A TO VISUAL INSPECT SURFACE FINISH, AND RE-INSPECT MAGNTIC PERMEABILITY PRIOR TO MOVING PARTS TO THE NEXT OPERATION.

5.  METAL STAMP PART I.D. AND SERIAL NUMBER ON EACH PANEL WITHIN THE BOUNDARY OF THE EXCESS TRIM STOCK.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

3200

1810

19,200.0

INCONEL 625_5-PLATE,NICKEL ALLOY .375" THK

10

Vendor Part ID: INCONEL 625_5

(U)

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: VVSA PANEL # 9

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 24 / Seq: 15

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FINISH / VERIFY MAGNETIC PERMEABILITY OF THE RAW MATERIAL PRIOR TO CUTTING (MATERIALS DEPT. WILL COORDINATE) AND EACH

PANEL AFTER CUTTING / CLEANING PER THE FOLLOWING:

Test Certification: MAG. PERMEABILITY CERT  Rev:

Specification: ASTM A800  Rev:

Part Number: VVSA PANEL # 9

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 24 / Seq: 20

6.00

6.00

6.00

(U)

LOAD AND ALIGN DIE SET # ___________ INTO THE 750 TON HYDRAULIC PRESS.

INSTALL PANEL BLANK INTO THE DIE SET.

HYDRAULICALLY FORM EACH PANEL TO CONFORM TO INSPECTION GAGE #__________.

PANEL TO GAGE GAP TOLERANCE:  .08" MAX.

ENSURE THE PANEL MATERIAL EXTENDS BEYOND THE PERIMETER OF THE TRIM-LINES OF THE GAGE BY AT LEAST 1" (FOR ACCURATE TRIMMING).

NOTIFY Q/A FOR INTERIM PROFILE VERIFICATION OF EACH PANEL AS THEY ARE FORMED.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 24 / Seq: 21

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .188" MAX.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 9

Test Certification: INTERIM DIM. INSP. MAP  Rev:

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 27

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

Sub: 24 / Seq: 25

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 24 / Seq: 27

6.00

6.00

6.00

(U)

INSTALL AND WELD ANNEAL BRACING IN PLACE PER WPS....

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

520-SUBLET, EXOTIC HEAT TREAT

SE121 / A

Sub: 24 / Seq: 30

6.00

6.00

6.00

THRML TR/NA SA

(U)

SOLUTION ANNEAL FORMED PANEL PER THE FOLLOWING:

HOLD AT 1900 DEGREES F.  (+/- 15 DEGREES) HOLD FOR 45 MINUTES (+/ 5 MINUTES)

Certification: H/T CERTIFICATE

Part Number: VVSA PANEL # 9

Furnace charts: FURNACE CHART

Specification: AMS2774  Rev: JUL95

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 24 / Seq: 35

6.00

6.00

6.00

(U)

VISUAL INSPECT SURFACE FOR DAMAGE, PITTING, GOUGES, SCRAPES ETC.....

VERIFY MAGNETIC PERMEABILITY AND RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

341-PACIFIC 750

SE121 / A

Sub: 24 / Seq: 40

6.00

6.00

6.00

(U)

RE-STRIKE PANEL

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.

LAYOUT TRIM-LINES ON THE PANEL ESTABLISHED FROM THE MACHINED PERIMETER OF THE INSPECTION GAGE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

260-SANDBLAST

SE121 / A

Sub: 24 / Seq: 50

6.00

6.00

6.00

(U)

SHOT BLAST WITH 180-220 GRIT VIRGIN ALUMINUM OXIDE MEDIA.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 24 / Seq: 60

6.00

6.00

6.00

(U)

TRIM PERIMETER TO PROVIDED TRIM-LINES.  NOTE THAT INSTALLING THE WELD PREP IS NOT REQUIRED AT THIS STAGE (ADDITIONAL FITTING / TRIMMING MAY BE

REQUIRED AT INSTALLATION)

SAND AND POLISH THE INSIDE SURFACE 100% TO ACHIEVE A 32 MICRO SURFACE FINISH.

INSTALL PROTECTIVE COVERING OVER THE MAJORITY OF THE POLISHED SURFACE (STAYING CLEAR OF THE WELD JOINTS)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 24 / Seq: 70

6.00

6.00

6.00

(U)

VERIFY PROFILE TO INSPECTION GAGE #__________.  GAP TOLERANCE:  .08" MAX.  PERIMETER SHOULD FALL WITHIN .03" OF GAGE PERIMETER.

RECORD ON INSPECTION MAP.

INSPECT AND RECORD INTERIOR SIDE SURFACE FINISH.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 28

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

INSPECT AND RECORD MAGNETIC PERMEABILY.

Part Number: VVSA PANEL # 9

Test Certification: FINAL DIM. INSP. MAP  Rev:

Test Certification: MAGNETIC PERMEABILITY CERT.

Specification: ASTM A800

0

Program Count:

Drawing Count:

0

2

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VESSEL FLANGES

81

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 81 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT FLANGES PER DRAWING / NESTING / PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

2000

4434

12,000.0

10

Vendor Part ID: INCONEL 625_1

Mfg Part ID: INCONEL 625

(U)

PLATE, INCONEL 625, 2.0" THK

INCONEL 625 (UNS N06625) PER ASTM B 443-00

ANNEALED

MAGNETIC PERMEABILITY SHALL NOT EXCEED 1.00 (REF. ASTM A800).

SURFACE MUST BE PROTECTED FROM CONTACT WITH IRON AND IRON ALLOY MATERIALS

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 81 / Seq: 20

6.00

6.00

6.00

(U)

N/C PER PROGRAM (SEMI-FINISH)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

106-DEBURR/ASSEMBLY PLT 1 HIGH

Sub: 81 / Seq: 30

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 81 / Seq: 40

6.00

6.00

6.00

(U)

INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

NEUTRAL BEAM PORT

26

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

Sub: 26 / Seq: 10

3.00

3.00

3.00

(U)

ASSEMBLE AND WELD FLANGE TO SIDEWALL

BLEND WELDS FLUSH ON INSIDE SURFACES

POLISH INSIDE SURFACES TO 32 MICRO.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 29

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

CWI VISUAL INSPECT WELDS PER.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

150.0

50

(U)

.500-13UNC-2A X 2.0 SHCS

Material Certification:

Part Number: .500-13UNC-2A X 2.0 SHCS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

150.0

60

(U)

.500-13UNC-2B HEX NUT

Material Certification:

Part Number: .500-13UNC-2B HEX NUT

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

150.0

70

(U)

.500 FLAT WASHER

Material Certification:

Part Number: .500 FLAT WASHER

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 26 / Seq: 20

3.00

3.00

3.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

818-MQS CONTRACTOR X-RAY

Sub: 26 / Seq: 30

3.00

3.00

3.00

(U)

100% RADIOGRAPHIC INSPECT STRUCTURAL WELDS (IDENTIFIED ON PART) PER THE FOLLOWING:.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 26 / Seq: 40

3.00

3.00

3.00

(U)

N/C FLANGE FACE AND HOLES PER DRAWING AND PROGRAM.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 26 / Seq: 50

3.00

3.00

3.00

(U)

DEBURR AND CLEANUP

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 30

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 26 / Seq: 60

3.00

3.00

3.00

(U)

INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

#12 SIDEWALLS

36

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 36 / Seq: 10

3.00

3.00

3.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1300

3,900.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P2 PORT SIDEWALL

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 36 / Seq: 15

3.00

3.00

3.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 36 / Seq: 20

3.00

3.00

3.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 36 / Seq: 30

3.00

3.00

3.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 36 / Seq: 40

3.00

3.00

3.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

#12 FLANGE

37

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 31

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

410-BURNOUT TABLE

Sub: 37 / Seq: 10

3.00

3.00

3.00

(U)

BUNOUT FLANGE SEGMENTS PER NESTING.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1800

1810

5,400.0

INCONEL 625_2-PLATE,NICKEL ALLOY .75" THK

10

Vendor Part ID: INCONEL 625_2

Mfg Part ID: INCONEL 625

(U)

INCONEL 625

PLATE,NICKEL ALLOY .75" THK

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 37 / Seq: 20

3.00

3.00

3.00

(U)

SEMI-FINISH MACHINE FLANGE PER DRAWING AND PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 37 / Seq: 30

3.00

3.00

3.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 37 / Seq: 40

3.00

3.00

3.00

(U)

DIMENSIONAL INSPECTION ON MACHINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

#12 WELD BACKING

69

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 69 / Seq: 10

3.00

3.00

3.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

555.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 69 / Seq: 15

3.00

3.00

3.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 32

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 69 / Seq: 20

3.00

3.00

3.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 69 / Seq: 30

3.00

3.00

3.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 69 / Seq: 40

3.00

3.00

3.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

VACUUM TEST CAP

80

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 80 / Seq: 10

3.00

3.00

3.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1000

1810

3,000.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 80 / Seq: 20

3.00

3.00

3.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 80 / Seq: 30

3.00

3.00

3.00

(U)

DIMENSIONAL INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 33

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

/

6

#2 (4"DIA) PORT

27

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 27 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 27 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#2 TUBE

38

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 38 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 34

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

Vendor Part ID: SE121-001P-5

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P2 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 38 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 38 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 35

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 38 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#2 FLANGE

39

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 39 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

6", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number:

Material Certification:

Part Number: 6" CONFLAT FLANGE

Part Description: P2 PORT FLANGE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 36

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#2 WELD BACKING

68

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 68 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 68 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 37

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 68 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 68 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 68 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

70

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 70 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 70 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 70 / Seq: 30

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 38

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#4 HT PORT  HORIZONTAL TEARDRO

28

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

Sub: 28 / Seq: 10

6.00

6.00

6.00

(U)

ASSEMBLE AND WELD FLANGE TO SIDEWALL

BLEND WELDS FLUSH ON INSIDE SURFACES

POLISH INSIDE SURFACES TO 32 MICRO.

CWI VISUAL INSPECT WELDS PER.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

50

(U)

.500-13UNC-2A X 2.0 SHCS

Material Certification:

Part Number: .500-13UNC-2A X 2.0 SHCS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

60

(U)

.500-13UNC-2B HEX NUT

Material Certification:

Part Number: .500-13UNC-2B HEX NUT

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

70

(U)

.500 FLAT WASHER

Material Certification:

Part Number: .500 FLAT WASHER

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 28 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

818-MQS CONTRACTOR X-RAY

Sub: 28 / Seq: 25

6.00

6.00

6.00

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 39

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

100% RADIOGRAPHIC INSPECT STRUCTURAL WELDS (IDENTIFIED ON PART) PER THE FOLLOWING:.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 28 / Seq: 30

6.00

6.00

6.00

(U)

FINISH N/C FLANGE FACE PER DRAWING AND PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 28 / Seq: 40

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 28 / Seq: 50

6.00

6.00

6.00

(U)

DIMESIONAL INSPECTION (ON MACHINE)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 SIDEWALLS

40

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 40 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1500

9,000.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 40 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 40 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING

BLEND WELD FLUSH TO BASE METAL

POLISH INTERIOR TO ACHIEVE A 32 MICRO-INCH SURFACE FINISH

CWI INSPECTION......

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 40

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 40 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 40 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 FLANGE

41

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 41 / Seq: 10

6.00

6.00

6.00

(U)

BUNOUT FLANGE SEGMENTS PER NESTING.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1800

1810

10,800.0

INCONEL 625_2-PLATE,NICKEL ALLOY .75" THK

10

Vendor Part ID: INCONEL 625_2

Mfg Part ID: INCONEL 625

(U)

INCONEL 625

PLATE,NICKEL ALLOY .75" THK

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 41 / Seq: 20

6.00

6.00

6.00

(U)

SEMI-FINISH MACHINE FLANGE PER DRAWING AND PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 41 / Seq: 30

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 41 / Seq: 40

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION ON MACHINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 WELD BACKING

63

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 63 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 41

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 63 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 63 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 63 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 63 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

71

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 71 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1000

1810

6,000.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 71 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 42

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 71 / Seq: 30

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#5 (8"DIA) PORT

29

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 29 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 29 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 43

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#5 TUBE

42

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 42 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

Vendor Part ID: SE121-001P-5

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P5 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 42 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 44

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 42 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 42 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#5 FLANGE

43

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 43 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 45

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

8", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number: 8" CONFLAT FLANGE

Part Description: P5 PORT FLANGE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#5 WELD BACKING

62

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 62 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 46

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 62 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 62 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 62 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 62 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

72

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 72 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 72 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 47

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#6 (12"DIA) PORT

30

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 30 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 30 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#6 TUBE

44

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 48

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 44 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P6 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 44 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 44 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 49

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 44 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#6 FLANGE

45

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 45 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

12", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number: 12" CONFLAT FLANGE

Part Description: P6 PORT FLANGE

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 50

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#6 WELD BACKING

61

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 61 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 51

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 61 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 61 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 61 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 61 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

73

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 73 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 73 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 52

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#7 (8"DIA) PORT

31

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 31 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 31 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#7 TUBE

46

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 46 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 53

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P7 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 46 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 46 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 54

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 46 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#7 FLANGE

47

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 47 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

8", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number: 8" CONFLAT FLANGE

Part Description: P7 PORT FLANGE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 55

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#7 WELD BACKING

60

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 60 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 60 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 56

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 60 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 60 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 60 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

74

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 74 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 74 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#8 (6"DIA) PORT

32

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 57

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 32 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 32 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#8 TUBE

48

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 48 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 58

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P8 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 48 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 48 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 59

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

230-FABRICATION - WEIDNER

SE121 / A

Sub: 48 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#8 FLANGE

49

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 49 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

6", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number: 6" CONFLAT FLANGE

Part Description: P8 PORT FLANGE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 60

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#8 WELD BACKING

59

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 59 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 59 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 59 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 61

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 59 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 59 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

75

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 75 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 75 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#10 OVAL PORT

33

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

Sub: 33 / Seq: 10

6.00

6.00

6.00

(U)

ASSEMBLE AND WELD FLANGE TO SIDEWALL

BLEND WELDS FLUSH ON INSIDE SURFACES

POLISH INSIDE SURFACES TO 32 MICRO.

CWI VISUAL INSPECT WELDS PER.......

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 62

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

50

(U)

.500-13UNC-2A X 2.0 SHCS

Material Certification:

Part Number: .500-13UNC-2A X 2.0 SHCS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

60

(U)

.500-13UNC-2B HEX NUT

Material Certification:

Part Number: .500-13UNC-2B HEX NUT

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

70

(U)

.500 FLAT WASHER

Material Certification:

Part Number: .500 FLAT WASHER

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 33 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

818-MQS CONTRACTOR X-RAY

Sub: 33 / Seq: 30

6.00

6.00

6.00

(U)

100% RADIOGRAPHIC INSPECT STRUCTURAL WELDS (IDENTIFIED ON PART) PER THE FOLLOWING:.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 33 / Seq: 40

6.00

6.00

6.00

(U)

N/C FLANGE FACE AND HOLES PER DRAWING AND PROGRAM.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 33 / Seq: 50

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 63

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 33 / Seq: 60

6.00

6.00

6.00

(U)

INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 SIDEWALLS

50

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 50 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1500

9,000.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 50 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 50 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING

BLEND WELD FLUSH TO BASE METAL

POLISH INTERIOR TO ACHIEVE A 32 MICRO-INCH SURFACE FINISH

CWI INSPECTION......

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 50 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 50 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 FLANGE

51

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 64

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 51 / Seq: 10

6.00

6.00

6.00

(U)

BUNOUT FLANGE SEGMENTS PER NESTING.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1800

1810

10,800.0

INCONEL 625_2-PLATE,NICKEL ALLOY .75" THK

10

Vendor Part ID: INCONEL 625_2

Mfg Part ID: INCONEL 625

(U)

INCONEL 625

PLATE,NICKEL ALLOY .75" THK

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 51 / Seq: 20

6.00

6.00

6.00

(U)

SEMI-FINISH MACHINE FLANGE PER DRAWING AND PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 51 / Seq: 30

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 51 / Seq: 40

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION ON MACHINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 WELD BACKING

58

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 58 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 58 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 65

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 58 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 58 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 58 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

76

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 76 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1000

1810

6,000.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 76 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 76 / Seq: 30

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 66

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#11 (6"DIA) PORT

34

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 34 / Seq: 10

6.00

6.00

6.00

(U)

INSTALL AND WELD CONFLAT FLANGE TO TUBE PER DRAWING AND WPS.....

FIT AND TRIM THE LENGTH FOR INSTALLATION (USE REFERENCE SCRIBE LINES ON BUILD FIXTURE).  PREP FOR WELDING IN PLACE.

GRIND / BLEND THE INTERIOR WELD SMOOTH.

POLISH THE ENTIRE INSIDE SURFACE SMOOTH TO ACHIEVE A 32 MICRO SURFACE FINISH.  CLEAN THE INTERIOR SURFACES PER............

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 34 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#11 TUBE

52

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 52 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVE AND INSPECT TUBE PER MTM P.O.

NOTIFY ENGINEERING (DOUG McCORKLE) WHEN PART ARRIVES.

VISUAL INSPECT SURFACE FINISH FOR PITS, NICKS, GOUGES, SCRAPES, SCRATCHES, ETC....

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 67

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

5647

6.0

10

(U)

TUBE, ROUND, INCONEL 625, SEAMLESS OR WELDED.  ASTM B444 OR ASTM B705

P11 PORT TUBE

4" O.D. X .125" WA X 48"

NOTE THAT THE FOLLOWING REQUIREMENTS WILL BE PERFORMED / TESTED BY MAJOR TOOL & MACHINE AFTER DELIVERY.  ALL EFFORTS TO ACCOMODATE / ENSURE

SUCESS MUST BE MAINTAINED:

MAGNETIC PERMEABILITY REQUIREMENT:  1.01 MAX.

VACUUM INTEGRITY REQUIREMENT:  TOTAL HELIUM LEAK RATE FOR THE TUBE SHALL BE LESS THAN OR EQUAL TO 1.7 X 10(-9) TORR-L/S

INTERIOR SURFACE FINISH REQUIREMENT:  INTERIOR WELD BEADS WILL BE GROUND FLUSH.  THE ENTIRE INTERIOR SURFACE WILL BE POLISHED TO A 32 MICRO

SURFACE FINISH AND VERIFIED PER ASME B46.1.

EXTERIOR SURFACE FINISH:  MILL SURFACE ACCEPTABLE.  NO PITS, SCRAPES OR GOUGES.

MATERIAL CERTIFICATION AND TEST REPORTS REQ'D WITH SHIPMENT.

Material Certification:

Part Number: P11 PORT TUBE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 52 / Seq: 20

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY OF THE PORT EXTENTION TUBE (AS RECEIVED).  RECORD ACTUAL I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

405-SAWS- PLANT 2

SE121 / A

Sub: 52 / Seq: 30

6.00

6.00

6.00

(U)

SAW ONE END SQUARE REMOVING NO MORE THAN 1/2" OF MATERIAL.

DEBURR SAWED EDGE

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 68

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121 / A

Sub: 52 / Seq: 40

6.00

6.00

6.00

(U)

BLEND THE INSIDE WELD FLUSH.

POLISH THE ENTIRE INTERIOR SURFACE TO A 32 MICRO-INCH SURFACE FINISH.

PREP FOR FLANGE INSTALLATION.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#11 FLANGE

53

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

SE121 / A

Sub: 53 / Seq: 10

6.00

6.00

6.00

(U)

RECEIVING INSPECTION

RECEIVE AND INSPECT THE FOLLOWING PARTS:

(THEY SHOULD ALL ARRIVE TOGETHER)

F10000000NC4

FG1000CI

FG1000VU

FB1000C12S

GC0275S

CONTACT ENGINEERING (DOUG McCORKLE) WHEN PARTS ARRIVE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

10

(U)

FLANGE, CONFLAT, NON-ROTATABLE

8", CLEAR BOLT HOLES, 304L

Material Certification:

Part Number: 8" CONFLAT FLANGE

Part Description: P11 PORT FLANGE

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000CI-GASKET KIT (10/PK), COPPER, FOR 10" CFF

20

(U)

GASKET KIT (10/PACK), COPPER, INDIVIDUAL SEAL, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 69

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Material Certification:

Part Number: FG1000CI

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FG1000VU-GASKET, VITON, FOR 10" CFF

30

(U)

GASKET, VITON, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FG1000VU

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

FB1000C12S-BOLT AND NUT KIT, 12 PT, SILVER PLATED

40

(U)

BOLT AND NUT KIT (25/PACK), 12 POINT, ASTM A193 GR. B8 SILVER PLATED, FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: FB1000C12S

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

6.0

GC0275S-GASKET CLIP KIT (10/PK), FOR 10" CFF

50

(U)

GASKET CLIP KIT (10/PACK)

FOR 10" CONFLAT FLANGE

VARIAN VACUUM TECHNOLOGIES

Material Certification:

Part Number: GC0275S

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#11 WELD BACKING

57

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 57 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 57 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 70

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 57 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 57 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 57 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

77

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 77 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

100

1810

600.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 77 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 VT PORT  VERTICAL TEARDROP

35

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 71

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

Sub: 35 / Seq: 10

6.00

6.00

6.00

(U)

ASSEMBLE AND WELD FLANGE TO SIDEWALL

BLEND WELDS FLUSH ON INSIDE SURFACES

POLISH INSIDE SURFACES TO 32 MICRO.

CWI VISUAL INSPECT WELDS PER.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

50

(U)

.500-13UNC-2A X 2.0 SHCS

Material Certification:

Part Number: .500-13UNC-2A X 2.0 SHCS

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

60

(U)

.500-13UNC-2B HEX NUT

Material Certification:

Part Number: .500-13UNC-2B HEX NUT

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

300.0

70

(U)

.500 FLAT WASHER

Material Certification:

Part Number: .500 FLAT WASHER

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 35 / Seq: 20

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECT

INSPECT INTERIOR SURFACE FINISH OF THE PORT SUB-ASSEMBLY.  RECORD ACTUAL ON MTM IDC.

INSPECT THE MAGNETIC PERMEABILITY OF THE FLANGE TO TUBE WELD AND SURROUNDING AREA.  RECORD ACTUAL RANGE ON I.D.C.

ATTENTION:  PRIOR TO HANDLING THE PARTS OR COMENSING ANY WORK, READ AND UNDERSTAND THE FOLLOWING:

THE MAGNETIC PERMEABILITY, VACUUM INTEGRITY, AND SURFACE FINISH REQUIREMENTS FOR THIS VESSEL ARE VERY STRINGENT.  ALL EFFORTS MUST BE MADE TO

AVOID SURFACE CONTAMINATION AND DAMAGE WHILE PROCESSING / HANDLING THIS MATERIAL.  IT MUST NOT COME IN DIRECT CONTACT WITH IRON OR IRON BASED

MATERIALS (EG CHAINS, CLAMPS, LIFT TRUCK FORKS, STEEL RACKS, TABLES, HAND TOOLS, ETC...)  IT MUST NOT BE STORED, STACKED, OR STAGED DIRECTLY ONTO

IRON OR STEEL FIXTURING.  DO NOT USE ANY TOOLS (EG BRUSHES / GRINDING WHEELS) THAT ARE EITHER FERROUS, OR MAY HAVE BEEN PREVIOUSLY USED ON

FERROUS ALLOYS.  WELDING OF TOOLING AND/OR FIXTURING (EG HALF CLAMPS, BRACING, ETC…) TO THE COMPONENT PART MUST BE MINIMIZED (ENGINEERING

CONCURRENCE REQUIRED FOR ALL CERCUMSTANCES).  IN ALL SUCH CASES INCONEL 625 TABS MUST BE ATTACHED TO THE TOOL / FIXTURE TO AVOID

CONTAMINATION TO THE PRODUCTION MATERIAL.  EXTREME CARE MUST BE TAKEN TO ENSURE THE SURFACES ARE PROTECTED FROM GOUGING, SCRATCHING, AND

ANY CONTACT WITH FORIGN MATERIAL.  CONTACT ENGINEERING (DOUG McCORKLE) IF UNCLEAR.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

818-MQS CONTRACTOR X-RAY

Sub: 35 / Seq: 30

6.00

6.00

6.00

(U)

100% RADIOGRAPHIC INSPECT STRUCTURAL WELDS (IDENTIFIED ON PART) PER THE FOLLOWING:.......

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 35 / Seq: 40

6.00

6.00

6.00

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 72

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

(U)

N/C FLANGE FACE AND HOLES PER DRAWING AND PROGRAM.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 35 / Seq: 50

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 35 / Seq: 60

6.00

6.00

6.00

(U)

INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 SIDEWALLS

54

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 54 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1500

9,000.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 54 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 54 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING

BLEND WELD FLUSH TO BASE METAL

POLISH INTERIOR TO ACHIEVE A 32 MICRO-INCH SURFACE FINISH

CWI INSPECTION......

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 54 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 73

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 54 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 FLANGE

55

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 55 / Seq: 10

6.00

6.00

6.00

(U)

BUNOUT FLANGE SEGMENTS PER NESTING.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1800

1810

10,800.0

INCONEL 625_2-PLATE,NICKEL ALLOY .75" THK

10

Vendor Part ID: INCONEL 625_2

Mfg Part ID: INCONEL 625

(U)

INCONEL 625

PLATE,NICKEL ALLOY .75" THK

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 55 / Seq: 20

6.00

6.00

6.00

(U)

SEMI-FINISH MACHINE FLANGE PER DRAWING AND PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 55 / Seq: 30

6.00

6.00

6.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 55 / Seq: 40

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION ON MACHINE

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

#12 WELD BACKING

56

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121-003P / 0

Sub: 56 / Seq: 10

6.00

6.00

6.00

(U)

PREPARE SHEET FOR SUBCONTRACT LASER CUTTING

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

185

1,110.0

INCONEL 625_660-SHEET,NICKEL ALLOY .125" THK

10

(U)

INCONEL 625 SHEET, .125" THICK PER

AMS 5599 / ASTM B443 (UNS N06625).

CERT AND MILL TEST REPORT REQ'D WITH SHIPMENT.

Material Certification:

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 74

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Part Number: SE121-003P-4

Part Description: WELD BACKING RING

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 56 / Seq: 15

6.00

6.00

6.00

LASER/CUTTING

(U)

LASER CUT PER PROVIDED GEOMETRY.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

230-FABRICATION - WEIDNER

SE121-003P / 0

Sub: 56 / Seq: 20

6.00

6.00

6.00

(U)

PREP AND WELD PER DRAWING (SIZE TO EXISTING PORT)

BLEND WELD FLUSH TO BASE METAL

0

Program Count:

Drawing Count:

1

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

415-ROLLING/SHEAR/BRAKE PRESS

SE121 / A

Sub: 56 / Seq: 30

6.00

6.00

6.00

(U)

IF NECESSARY RE-ROLL / ROUND/ RE-FORM WELD BACKING BAND

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

SE121 / A

Sub: 56 / Seq: 40

6.00

6.00

6.00

(U)

VERIFY MAGNETIC PERMEABILITY.  RECORD I.D.C. DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

6

VACUUM TEST CAP

78

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 78 / Seq: 10

6.00

6.00

6.00

(U)

BURNOUT A 10.0" DIAMETER DISK AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1000

1810

6,000.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

108-TOOL ROOM - PLANT 1

Sub: 78 / Seq: 20

6.00

6.00

6.00

(U)

MACHINE PER DRAWING (DRAWING NEEDED!!!!)

(GRIND ONE FACE AND DRILL BOLT CIRCLE, DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

REF CONFLAT FLANGE DRAWING FOR BOLT CIRCLE

GRIND 32 SURFACE FINISH ON ONE SIDE

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 75

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

APPLY A WOOD OR CARDBOARD PROTECTOR ONTO THE GROUND FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 78 / Seq: 30

6.00

6.00

6.00

(U)

DIMENSIONAL INSPECTION

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

FIELD JOINT BLANKS  USED FOR V

82

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 82 / Seq: 10

3.00

3.00

3.00

(U)

BURNOUT AND CLEANUP.

SAND THE BURNED EDGES SMOOTH.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

1500

1810

4,500.0

304L_8-PLATE,SST .75" THK

10

Vendor Part ID: 304L_8

Mfg Part ID: 304L MATERIAL

(U)

PLATE, 304L STAINLESS STEEL

.75" THK

CERTS & MILL TEST REPORT REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 82 / Seq: 20

3.00

3.00

3.00

(U)

MACHINE PER DRAWING AND PROGRAM

DRILL TAP VACUUM PORT (1/2" NPT))

DRILL AND REAM A CENTER HOLE FOR TOOLING BALL (.2500", TOLERANCE TBD).  THIS WILL BE USED AS A TARGET FOR SMX INSPECTION AFTER INSTALLATION TO

VERIFY POSITION OF THE PORT.

APPLY A WOOD OR CARDBOARD PROTECTOR TO THE FLANGE SIDE FACE.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 82 / Seq: 30

3.00

3.00

3.00

(U)

DIMENSIONAL INSPECTION (ON MACHINE)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

3

FIELD JOINT SPACERS

25

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

410-BURNOUT TABLE

Sub: 25 / Seq: 10

3.00

3.00

3.00

(U)

BURNOUT FLANGES PER DRAWING / NESTING / PROGRAM

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Dimensions

Vendor

Qty

Drawing ID / Rev

Part ID

Piece #

2000

4434

6,000.0

INCONEL 625_1-PLATE,NICKEL ALLOY 3.0" THK

10

Vendor Part ID: INCONEL 625_1

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp

Page: 76

Date:06/23/03

User ID: MANUEL

Drawing ID / Rev

Engineer

Qty

Part ID

Workorder

SE120 / --

SE120-001/0

SE120-001-NCSX VACUUM VESSEL SUB ASSEMBLY

1

BLUE/DOUG MCCORKLE

Mfg Part ID: INCONEL 625

(U)

INCONEL 625

PLATE,NICKEL ALLOY 3.0" THK

CERTS & MILL TEST REPORTS REQ'D WITH SHIPMENT.

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

Service ID

450-SUBLET

Sub: 25 / Seq: 20

3.00

3.00

3.00

MISC/SUBLET

(U)

BLANCHARD GRIND BOTH SIDES TO 3.0" +/-.010

SURFACE FINISH REQUIREMENT:  32 MICRO.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

820-RECEIVING INSPECTION

Sub: 25 / Seq: 30

3.00

3.00

3.00

(U)

RECEIVE AND INSPECT

VERIFY THICKNESS DIMESION

VERIFY SURFACE FINISH

RECORD IDC DATA

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

154-TC-3500

Sub: 25 / Seq: 40

3.00

3.00

3.00

(U)

N/C INTERIOR AND EXTERIOR PERIMETER AND HOLES PER DRAWING AND PROGRAM.

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

105-DEBURR/ASSEMBLY PLT 1 LOW

Sub: 25 / Seq: 50

3.00

3.00

3.00

(U)

DEBURR AND CLEANUP

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

805-INPROCESS INSPECTION - PLANT

Sub: 25 / Seq: 60

3.00

3.00

3.00

(U)

INSPECT (ON MACHINE)

0

Program Count:

Drawing Count:

0

0

Inspection Count :

Drawing ID / Rev

Sub ID

Part ID

Qty

/

1

SHIPPING CONTAINERS

2

Resource

Drawing ID / Rev

Operation

QtyPer

StartQty

EndQty

425-SHIPPING - PLANTS 1 & 2

SE120 / --

Sub: 2 / Seq: 10

1.00

1.00

1.00

(U)

BUILD THREE SHIPPING CRADLES PER ENGINEERING SKETCH

APPROXIMATE SIZE:

7' X 12'

0

Program Count:

Drawing Count:

0

0

Inspection Count :

M:SE120-001/0-0 /Inc Matl /Inc Legs

MTTRAVLR.qrp