How about:

- Bring the 120º segments together

- Lay in reasonably sized cut section of the spool plates that Major Tool produces from the formed spool

- Mark and Grind edges as necessary to custom fit

- Tack in backing strips on each side OR install precurved removable thin channel sections to deliver backing gas. (Major tool uses rectangular cups that a guy holds over the area being welded when joining plates together

- Position and install leak check Helium delivery tubes

- Weld spool sections in place using the backing gas or backing ring as a consumable

- After each section, reach up or down through the gap at the uninstalled plate to install the insulation

This will:

- eliminate 4 welds at each joint;

- provide for a standard code weld configuration on a simple 3/8” thick section;

- provide for a uniform transition of the vacuum vessel shell;

- allow for radiography of the welds;

- allow for careful positioning of leak check tubing;

- allow for visual examination of the weld using a boroscope;

- eliminate the need to dangle and fixture the spool in place; etc.

Mike Viola January 7, 2005