VVSA-2 Supplier-Generated NCR’s

| NUMBER | DATE | STATUS | ITEM | ISSUE |
| --- | --- | --- | --- | --- |
| 17157 | 5/12/2005 | Closed | All VVSA's | Magnetic Permeability to be 1.02 max |
| 17167 | 5/12/05 | Closed | All VVSA's | 1.02 Max magnetic permeability |
| 17233 | 5/12/2005 | Closed | All VVSA's | 1.02 max magnetic permeability |
| 17237 | 5/12/2005 | Closed | All VVSA's | 1.02 max magnetic permeability |
| 17240 | 5/12/2005 | Closed | All VVSA's | 1.02 Max magnetic permeability |
| 17286 | 5/12/2005 | Closed | All VVSA's | 1.02 max on magnetic permeability. |
| 17287 | 5/12/2005 | Closed | All VVSA's | 1.02 max on magnetic permeability. |
| 17288 | 5/12/2005 | Closed | All VVSA's | 1.02 max magnetic permeability parts check. |
| 17314 | 5/12/05 | Closed | All VVSA's | 1.02 Max magnetic permeability. |
| 17342 | 5/12/05 | Closed | All VVSA's | 1.02 Max magnetic permeability. |
| 18097 | 10/13/2005 | Closed | VVSA 2 | Rejected magnetic permeability of 1.02 max. |
| 18097 | 10/13/2005 | Closed | VVSA 2 | Rejected magnetic permeability of 1.02 max. |
| 18154 | 10/13/2005 | Closed | VVSA 2 | Problem 1.02 max permeability. |
| 18155 | 10/13/2005 | Closed | VVSA 2 | 1.02 Max permeability checks greater than 1.02 and less than 1.4 |
| 18762 | 12/2/2005 | Closed | VVSA 2 | Requirement-Magnetic permeability |
| 19254 | 2/14/2006 | Closed | VVSA 2 | Both lot 8 & 9 outer Helicoflex metal seals are too small to allow for proper fit of retaining strip |
| 19392 | 3/10/2006 | Closed | VVSA 2 | SE121-013 zone B5 469 +/- .005 dimension varies around part over and undersized, .240 - .432. |
| 19393 | 3/10/2006 | Closed | VVSA 1 & 2 | The 1.25 +/-0.10 dimension is undersize after re-work to achieve flatness. |
| 19464 | 3/21/2006 | Closed | VVSA 1 & 2 | Weld configurations on all ports |
| 19562 | 4/13/2006 | Closed | VVSA 2 | Profile deviation on the vessel ends causes a misalignment to the vessel flange |
| 19697 | 4/25/2006 | Closed | VVSA 2 | The profile of the flange of half A checks -0.194/+0.190 under low limit and 0.002 over high limit. |
| 19832 | 5/12/2006 | Closed | VVSA 2 | Testing operation the high vacuum gauge display wouldn't illuminate. |
| 19868 | 6/8/2006 | Closed | VVSA 2 | Port NB has deformation to hole pattern after welding. |
| 20069 | 7/27/06 |  | VVSA 2 | Port Lengths and Dome Misalignment |
| 20120 | 7/27/06 |  | VVSA 2 | Port NB Flange Thickness and 2 Dwg SE120-013 dimensions (0.469 & 0.637) |
| 20175 | 7/27/06 |  | VVSA 2 | Various Dimensional OOT shown in final Veri-Surf Data |