Week of 5/5/06

VVSA Quality Items

- Closed:

  - NC 19391 concerning rework of end flanges.

  - NC 19108 concerning the spacer flange chamfers

- Pending from MTM:

  - NC18888 for the misaligned VVSA-1 bosses.
Status: Open - Awaiting update showing CA completed

  - NC 19081 concerning the spacer flange weld configuration.
Status: Open - Acknowledge corrective action

  - NC 19289 concerning rework of Neutral Beam ports (all 3 segments).
Status: Open - Awaiting update showing CA completed.  Note this NC was written to cover all 3 VVSA segments with the presumption that similar distortion would occur on each.  Unfortunately that approach means that the NC will not be closed until CA for all 3 VVSA segments is complete.  F. Malinowski & D. McCorkle discussed a solution where Doug would split this into 3 NC’s and attach the disposition from 19289 to each.  Both Brad Nelson & Mike Viola, the other signers, agree with this solution.

  - NC 19392 concerning VVSA-1 SE121-013 ZONE B5 . .469 +/-.005 dimension varies around part over and undersized, .240-.432.
Status: Open - Awaiting update showing CA completed

  - NC 19697 concerning profile of VVSA-1 end flanges.
Status: Open - Awaiting update showing CA completed

  - NC 19562 VVSA-2 end flange misalignment.
Status: Open - Awaiting update showing CA completed

  - NC’s for Weld Repairs.

  - New NC for final VVSA scan.

- Pending from PPPL

  - NC 19116 concerning flange disposition due to manufacturer change.
Status: Sign off to Close when MDC flanges are delivered (with VVSA-1)

  - NC 19704 VVSA-3 Profile after hole cutting.
Status: Open - Awaiting Disposition