# PPPL-NCSX Memorandum

To:	Project Engineer (PPPL)

From:	Leonard Myatt (Myatt Consulting, Inc.)

Date:	June 30, 2004

Subject: Material Property Data Base to be used for NCSX Analyses

This document is a compilation of salient material property data to be used in all project calculations. Values are listed in a summary table with supporting documentation included as attachments. At this time, the table is incomplete, but recommendations are made for judiciously filling the significant cells.

- MCWF Casting: A series of tensile tests with strain gages would provide the elastic modulus (E) and Poisson’s ratio (ν) while a cooldown to 77K test would provide the coefficient of thermal expansion (α or CTE). Q: Is any of this data already available from casting vendor tests?

- VPI’d MC Conductor: A transverse compression test of the 2x5 array should fill the missing E data. A torsion test of a single conductor should provide two of three shear moduli where the applied torque and angle of twist are sufficient outputs. A representative FE model is included to demo this result. The third shear modulus value could be determined from ultrasonic testing (refer to R.P. Reed for details). And a cooldown to 77K test would provide the CTE data.

- The VPI S-Glass + Kapton properties are provided by R. P. Reed. He says, OK for analysis but not worthy of Design Criteria accountability (no traceable source).

Allowable stress levels are a natural extension of this document, and will be added as required.

Table 1.0 is a proposed structural material property data base to be used in all NCSX project stress calculations. Data is taken from NBS, ITER and NCSX test data. Minor changes are made to the referenced values, such as retaining two significant figures and achieving some consistency between similar insulating materials.

Table 1.0 Material Property Data Base for use in (80K) Structural Analyses

| Material | Ex [GPa] | Ey [GPa] | Ez [GPa] | x /K] | y /K] | z /K] | Gxy [GPa] | Gxz [GPa] | Gyz [GPa] | xy [-] | yz [-] | xz [-] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 316LN SS Annealed | 209 | 13 | 81 | 0.283 |
| MCWF Casting | Tensile w/SG | CD w/SG |  | Tensile w/SG |
| OFHC Cu | 136 | 14 | 51 | 0.34 |
| VPI S-Glass | 21 | 28 | 22 | 7.9 | 6.9 | 9.6 | 0.2 |
| VPI S-Glass + Kapton (courtesy R.P.Reed) | 19 | 26 | 21 | 7.9 | 4.2 | 6.0 | 0.2 |
| Prepreg S-Glass | 22 | 30 | 28 | 7.4 | 5.3 (6.2) | 10 | 0.2 |
| Prepreg S-Glass + Kapton | 21 | 22 | 27 | 7.5 | 3.8 | 6.2 | 0.2 |
| VPI’d MC Conductor | 37 (TBD:2x5Test) | 78 | CD w/SG | CD | Ultrasonic | Twist Test |  |

Notes:

1. Orthotropic material coordinate system:

- x is the through-thickness direction

- y is in the direction of the wrap (i.e., around the conductor perimeter)

- z is parallel to the conductor axis

2. Cells filled in yellow signify FE-based values.

3. Cells filled in blue signify low-risk assumed values of comparable materials.

4. SG = Strain Gages, CD = Cool Down

Supporting Documentation

1. 316LN SS Annealed

1. 316LN SS Annealed, continued

2. MCWF Casting (assume isotropic)

Tensile test with strain gages yields:

- Elastic Modulus

- Poisson’s Ratio

- Yield Stress

- Ultimate Strength

Cooldown to 77K with strain gages yields:

- Coefficient of Thermal Expansion

Q: Do either of the casting vendors already have any of this data?

Len,

In looking over elastic modulus data for 316-like cast alloys for Phil's specifications, I came across data from ITER (EU/KfK) that is very discouraging. I list the values that were reported for the elastic modulus at 7 K (tested in helium gas) and 4 K (liquid helium):

25 ton casting

Orientation = "Y"    124-179 GPa

Orientation = "X"    162-176 GPa

Orientation = "Z"    168-214 GPa

1 ton casting, one orientation

4 mm diameter specimen 148-176 GPa

6 mm diameter specimen 126-190 GPa

12 mm diameter specimen 170 GPa

20 mm diameter specimen 113-158 GPa

Wrought 316LN alloy

All orientations 192-211 GPa

Source: A. Nyilas, et al, European Cryogenic Material Testing Program for ITER Coils and Intercoil Structures, Advances Cryogenic Engineering- Materials, vol. 48 (2002), AIP Press, pp 123-130.

I do not know if this very large variability is caused by measurement inconsistencies, grain size and orientation variability, flaws, or ferrite variability. Also, the chemistry is different from ours; their alloy contains more Mn, N, and Mo. However, the chemical variations should not account for the variations in the elastic modulus. The relative tightness of the wrought data suggest that the variations are due to metallurgical factors

These data do suggest that the values that I provided you for the wrought ITER 316LN are too high. Maybe, until we obtain data on our casting, a modest "sensitivity study" is in order to assess the effects of possible variations of the elastic modulus of up to 50%.

Dick Reed

3. OFHC Cu

Simon, Drexler & Reed, NIST Monograph 177

4. Epoxy-Glass Insulation Systems

3. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

4. Epoxy-Glass Insulation Systems, continued

Included here for the purpose of estimating Poisson’s Ratio for VPI’d and Prepreg insulation systems.

5. VPI’d MC Conductor

5. VPI’d MC Conductor, continued

The plot below shows shear stresses in a 0.31” W x 0.351” H x 2” L  conductor section (middle 0.4” shown) which is subjected to an axial torsional displacement at its ends. The material is assumed to be isotropic with an elastic modulus of 78 GPa (11.3 Msi) and a Poisson’s ratio of 0.3. The plot title lists the shear modulus determined from model results (29 GPa) and analytical shear stress (T/(0.214HW2) or 873 MPa which nearly match the analytical value of E/(2(1+ν)) or 30 GPa and finite element stress of 862 MPa.

The polar moment of inertia is a trivial calculation for a circular cross-section and more complicated for a non-circular cross-section. So, using finite element results such as the maximum shear stress (taumx), angle of twist (dth) and torque (t_applied) to determine the effective shear modulus (gfe) requires taking some liberties, like the definition of the effective section radius (r_sec) as shown in the following calculations:

r_sec=sqrt(h**2+w**2)/2

jfe=t_applied*r_sec/taumx

gfe=t_applied*l_tot/(jfe*dth)

In spite of the lack of formalism, the agreement with more traditional methods is excellent and will be carried into future analyses when ever it is necessary. Notice that the maximum shear stress produced by this torsional load is SYZ (or SθZ in a cylindrical coordinate system). This is consistent with a GXZ or GYZ in a Cartesian CS.

# Text boxes

Room Temp Test Results

3-pt Flexure Test Results