26 Jan 2006

Additional Drawing Notes

NCSX

External Saddle Loops

Templates Fabrication

2.	THE MATERIAL USED SHALL BE COPPER ALLOY UNS C 11000, ANNEALED OR 1/8 HARD (H00-TEMPER) PER ASTM B370 OR ASTM B152

3.	MACHINED EDGES ARE TO BE DEBURRED AND SMOOTH TO PRECLUDE INJURY FROM HANDLING.

4.	PART NUMBERS AND ALIGNMENT ARROWS ARE TO BE PERMANENTLY MECHANICALLY ETCHED INTO THE TEMPLATE SURFACE EXACTLY AS SHOWN IN THE DRAWING. SOME TEMPLATES HAVE TWO TAG NUMBERS AND ALIGNMENT ARROWS. TAG NUMBERS AND ARROWS ARE USED TO ORIENT THE TEMPLATE DURING INSTALLATION.

- HANDLING AND PROCESSING SHALL BE CONTROLLED TO MINIMIZE WORK HARDENING.  MACHINED TEMPLATES ARE TO BE DELIVERED TO PPPL WITH THE SAME TEMPER AS THE STOCK SHEETS ( RAW MATERIAL). IT IS RECOGNIZED THAT THE CUT EDGES MAY BE SLIGHTLY HARDENED FROM THE CUTTING PROCESS.

- THE EDGES ARE TO BE PERPENDICULAR TO THE TEMPLATE SURFACE TO + OR – 5 DEGREES  (+ OR – 0.004 INCH)

7.	COATING THE SURFACE TO FACILITATE MACHINING IS PERMITTED. THE TEMPLATES ARE USED TO LOCATE AND WIND MAGNETIC COILS AND ARE REMOVED AFTERWARD.

8.	THE LOCATOR SEMICIRCULAR HOLES AND THEIR RESPECTIVE LOCATIONS ARE TO BE POSITIONED TO + OR – 0.005 INCH AND VERIFIED BY INSPECTION. THE GENERAL TEMPLATE DIMENSIONS ARE TO BE WITHIN + OR – 0.020 INCH OF THE IDEAL GEOMETRY (DXF MODEL). THE PPPL PROVIDED E SIZE DRAWINGS WITH FULL SCALE TEMPLATES ARE TO BE USED BY THE VENDOR AS A "GO- NO GO" GAUGE.