Major Tool & Machine, Inc.
Page: 1
 1458 East 19th Street
MTM N/C: 19942
Date: 06/01/06
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

ENERGY INDUSTRIES OF OHIO
Customer:
Telephone:
216-496-2314
Contact:
NANCY HORTON
NKHFlowen@aol.com
E-Mail:
216-328-2001
Fax:

S005242-F/Ln:1
Customer P.O.:
SE141-114 / MODULAR COIL WINDING FORM TYPE
Part:
A1
Serial No./Qty:
6
Revision:
SE141-114
Drawing ID:

317-636-6433
Telephone:
MIKE GRIFFITH
Reported By:
Fax:
317-634-9420
E-Mail:
mGriffith@MajorTool.com

Problem:
Workorder: 65709/1.0 Sub:1 Op:132
      Inspection Test #: 70  rejected: : {h|,02|A}: .046
      Inspection Test #: 80  rejected: 48.50 ± .03: : 48.454
      Inspection Test #: 130  rejected: OUTER AS CAST SURFACES: {g|,5|A|B|C}: -0.165 TO 0.288
      Inspection Test #: 140  rejected: 2 X .40: : .350 TO .420
      Inspection Test #: 150  rejected: 4 X .03 X 45: : .010 TO .040
      Inspection Test #: 170  rejected: P TO M: {g|,2|R|T|S}: POINTS NOT COLLECTED
      Inspection Test #: 180  rejected: DATUM D SIDE
      VERIFY SHELL INTERSECT CLEARANCE USING GAGE    MTMFX-3473: : AREAS BY T HOLES 5-10,
15 - 42, 84 - 94 WILL NOT ACCEPT GAGE
      Inspection Test #: 190  rejected: M TO M1: {g|,02|R|T|S}: -.0287 TO .268
      Inspection Test #: 210  rejected: Q TO N: {g|,2|R|T|S}: POINTS NOT COLLECTED
      Inspection Test #: 230  rejected: N TO N1: {g|,02|R|T|S}: -.0297 TO .0321
      Inspection Test #: 240  rejected: 2 X .06/.09 X 45: : .030 TO .060
      Inspection Test #: 270  rejected: .375-16 HOLES: {#|,06|R|T|S}: .002 TO .066
      Inspection Test #: 280  rejected: DATUM E FLANGE: {f|,01}: .029
      Inspection Test#: 285 rejected: surface 250
      Inspection Test #: 290  rejected: DATUM D FLANGE: {f|,01}: .028
      Inspection Test #: 410  rejected: Ø1.375-6: {#|d,06|M|A|D}: .062
      Inspection Test #: 480  rejected: Ø1.885: {#|d,06|N|A|E}: .007 TO .076
      Inspection Test #: 640  rejected: 2X .88 - 1.13: : 1.13 TO 1.14
      Inspection Test #: 780  rejected: INNER AS CAST SURFACES: {g|,5|A|B|C}: -.321 TO .149
      Inspection Test #: 790  rejected: WING SURFACES: {g|-,12;;;\,25|A|B|C}: .009 TO -.150

Workorder: 65709/1.0 Sub:1 Op:130
      Inspection Test #: 10  rejected: CHECK CLEARANCE OF ITEM 5 TO
ITEM 6.
: d.001 -  d.002: .004 TO.005 

Proposed Disposition:
PROPOSE TO USE AS IS.

 9 Page IDC Attachment
Number of additional pages: 

Customer Disposition:       [   ] Use As Is          [  ] Rework          [  ] Repair          [  ] Scrap          [  ] Replace

n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420

 Major Tool & Machine, Inc.
Page: 2
 1458 East 19th Street
MTM N/C: 19942
Date: 06/01/06
 Indianapolis, IN 46218-4289
User ID: GRIFFITH

Title:
Date:

Major Tool Implemented By:

n:\mtmapps\Mtnonc14.qrp

Major Tool and Machine, Inc.  1458 East 19th Street, Indianapolis, IN 46218-4289  Tel: 317-636-6433  Fax: 317-634-9420