NCSX

Finite Element Analysis on Vacuum Vessel

9th June, 2008

Prepared by:_____________________________________________  S Avasarala

Modeling:

The 360 degree model is assembled from the basic part and the spool piece. The model is defeatured and merged as one solid; this has eliminated all contact regions and expedited the solution time in Workbench.  Due to the complex geometry and the problems in meshing, a very fine mesh with an element size of two inches had to be used. The FE model has 1492181 nodes and 738785 elements. The solver takes approximately 25 minutes.

Figure 1 shows the FE Model of the Vacuum Vessel

Figure 3 shows the port numbers

Material Properties:

Inconel 625 is used for modeling the Vacuum Vessel. In an effort to create a single solid model, the port extensions, too are modeled using Inconel 625 instead of 316 grade Stainless Steel. The material properties of Inconel and stainless steel compare as follows.

|  | Inconel 625 | Stainless Steel 316 |
| --- | --- | --- |
| Density | .305 lbm/in3 | .28021 lbm/in3 |
| Coefficient of Thermal Expansion | 7.3 e-6 /F | 9.44e-6 /F |
| Poisson’s Ratio | .312 | .31 |
| Young’s Modulus | 2.8 e7 psi | 2.97 e7 psi |

Analysis:

Two kinds of Analysis are done on the Vacuum Vessel;

- Static Analysis:  Deflection Under Gravity Load

- Thermal Analysis: Deflection at the 350 F temperature.

a) Static Analysis:  The bottom surfaces of port 12 are fixed and standard earth gravity of 386.09 in/s2 is applied.

Figure 2 shows the fixed supports

Results:

The maximum deflection is found to be .064063 on port #2.

Figure 4 shows the deformation under gravity

- Thermal analysis: The temperature is increased to 350 F from a free state of 71.6. The maximum deformation of 0.29387”   is found to be on port # 10.The following is the deformation plot.

Figure 5 shows the deformation under the thermal loads

The following table shows the deflections on each port.

| Port # | Deflection in inches |
| --- | --- |
| 2 | .26368 |
| 4 | .22646 |
| 5 | .25046 |
| 6 | .2549 |
| 7 | .138 |
| 8 | .22813 |
| 9 | .2251 |
| 10 | .27961 |
| 11 | .2105 |
| 12 | .20897 |
| 15 | .25768 |
| 17 | .23323 |
| 18 | .205 |