Resin Impregnated Modular Coil Conductor for FDR

1)  Modulus of elasticity

| Load Test | Specimen | Temperature (K) | Elastic Modulus (Mpsi) | Reference |
| --- | --- | --- | --- | --- |
| Tension, 150,000 cycles | Short race-track coil | LN2 | 11.6 | [5] |
| Longitudinal Tension | Long race-track coil | RT | 8.30 | [11] |
| Longitudinal Compression | Bare conductor, 1.34” long | RT | 9.114 | [6] |
| Transverse Compression | Bare conductor | RT | 6.42 and 6.28 | [10] Incorrect modulus |
| Transverse Compression | Bare conductor | LN2 | 4.32 and 12.65 | [10] Incorrect modulus |
| Longitudinal Shear | Bare conductor | RT | 0.139 (Shear modulus) | [7] |
| Flexural Test | Bare conductor | RT | 9.80 | [7] |
| Flexural Test | Bare conductor | LN2 | 11.59 | [7] |
| Flexural Test | Bare conductor | RT | 9.63 | [8] |
| Flexural Test | Bare conductor | LN2 | 11.08 | [8] |
| Flexural Test | Glass wrapped bare conductor | RT | 6.28 | [8] |
| Flexural Test | Glass wrapped bare conductor | LN2 | 7.37 | [8] |

2)  Fatigue Life

| Load Test | Specimen | Temperature (K) | Tensile Stress (ksi) | Reference |
| --- | --- | --- | --- | --- |
| 2.6E6 cycles @ 15,000 lb | Short race-track coil | LN2 | 14.4 | [9] Strain increase with test cycles |
| 1.5E5 cycles @ 15,000 lb, and | Short race-track coil | LN2 | 1.5E5 cycles @ 14.4 ksi | [5] No change in coil resistance from fatigue cycling |

3)  Coefficient of Thermal Expansion

| Load Test | Specimen | Temperature (K) | CTE (10x-6 m/m/K) | Reference |
| --- | --- | --- | --- | --- |
| Longitudinal |  | 80 |  |  |
| Longitudinal |  | 100 |  |  |
| Longitudinal |  | 150 |  |  |
| Longitudinal |  | 295 |  |  |
| Transverse |  | 80 |  |  |
| Transverse |  | 100 |  |  |
| Transverse |  | 150 |  |  |
| Transverse |  | 295 |  |  |

4)  Yield Strength and ultimate Strength

| Load Test | Yield/Ultimate Strength | Temperature (C) | Strength (ksi) | Reference |
| --- | --- | --- | --- | --- |
| Three-point bend | Yield strength | 25.5 | 36.2 | [11] |
| Three-point bend | Yield strength | -196 | 45.2 | [11] |
| Longitudinal Shear | Yield strength | RT | 3.67 | [11] |
| Longitudinal Shear | Ultimate strength | RT | 4.65 | [11] |

Turn Insulation: CTD-101K with S-2 Glass Insulation

1)  Strength and Modulus  [12] & [13]

| Load Test | Temperature (K) | Strength (ksi) | Modulus (Mpsi) | Resin Process |
| --- | --- | --- | --- | --- |
| Compression (Thru. thickness) | 295 | 114.6 | 1.87 | VPI |
| Compression (Thru. thickness) | 77 | 188.6 | 2.42 | VPI |
| Compression (Thru. thickness) | 4.2 | 197.3 | 2.86 | VPI |
| Interlaminate Shear | 77 | 15.67 | 4.05 (flexural modulus) | VPI |
| Interlaminate Shear | 4.2 | 17.41 | 4.95 (flexural modulus) | VPI |

Note:	Interlaminate shear strength and flexural modulus are obtained by short beam 	shear tests.

2)   Combined Shear and Compressive Properties [13]

| Temperature (K) | Fixture (deg.) | Shear Strength (ksi) | Compressive Strength (Mpsi) |
| --- | --- | --- | --- |
| 76 | 15 | 14.7 | 4.3 |
| 76 | 45 | 25.5 | 25.5 |
| 76 | 75 | 35.9 | 135.4 |
| 76 | 84 | 18.4 | 175.2 |

3)  Shear Modulus [12]

| Temperature (K) | In-plane (Mpsi) | Interlaminar (Mpsi) |
| --- | --- | --- |
| 300 | 0.6 | 0.59 |
| 77 | 1.4 | 1.00 |
| 4 | 1.6 | 1.10 |

- Coefficient of Thermal Expansion [13]

CTE and Thermal Expansion (TE) in the Warp and Fill Direction [12]

| Temperature (K) | CTE - Warp (10E-6 m/m/K) | CTE - Fill (10E-6 m/m/K) | TE –Warp (%) | TE – Fill (%) |
| --- | --- | --- | --- | --- |
| 80 | 5.20 | 5.42 | -0.16 | -0.17 |
| 100 | 5.77 | 6.04 | -0.15 | -0.15 |
| 150 | 6.84 | 7.19 | -0.11 | -0.12 |
| 295 | 6.97 | 7.46 | 0.00 | 0.00 |

Ground Insulation

1)  Modulus of elasticity

| Load Test | Specimen | Temperature (K) | Elastic Modulus (Mpsi) | Reference |
| --- | --- | --- | --- | --- |
| Normal to glass |  | 80 |  |  |
| Normal to glass |  | 100 |  |  |
| Normal to glass |  | 295 |  |  |
| Parallel to glass |  | 80 |  |  |
| Parallel to glass |  | 100 |  |  |
| Parallel to glass |  | 295 |  |  |

2)  Coefficient of Thermal Expansion

| Load Test | Specimen | Temperature (K) | CTE (10x-6 m/m/K) | Reference |
| --- | --- | --- | --- | --- |
| Normal to glass |  | 80 |  |  |
| Normal to glass |  | 100 |  |  |
| Normal to glass |  | 295 |  |  |
| Parallel to glass |  | 80 |  |  |
| Parallel to glass |  | 100 |  |  |
| Parallel to glass |  | 295 |  |  |

VPI Epoxy Resin – CTD-101K

1)  Thermal Expansion of CTD-101K  Through Thickness [1]

2)  Linear Cure Shrinkage of Epoxy Resin Ctd-101k [3]

For CTD-101K epoxy resin, the cure shrinkage is 1.48% with standard deviation of 0.16% for the following cure cycle:

2.5 hours ramp to 110 degrees C from ambient

5 hours hold at 110 degrees C

1 hour ramp to 125 degrees C

16 hours hold at 125 degrees C

10 hours cooldown to 25 degrees C

48 hours at ambient conditions

Casting Stainless Steel

1)  Thermal Expansion [4]

| Specimen | Temperature (Deg. K) | Length L (in) | dL/L (%) | Reference |
| --- | --- | --- | --- | --- |
| JPP-1 | 301 77 | 5.834 5.816 | -0.309 | [4] |
| JPP-2 | 301 77 | 5.832 5.815 | -0.291 | [4] |

Average = -0.300%

Resin Impregnated Modular Coil Conductor for PDR

- A singular conductor is comprised of four 0.3125” by 0.250” braided copper and is wound with glass/kapton turn insulation to form a  0.690” by 0.564” conductor.

1) Axial Compression Properties of An Single Modular Coil (ASTM D-695)

- 1.0-inch long [2]

| Temperature (K) | Compression Modulus (Msi) | Compression Strength (ksi) |
| --- | --- | --- |
| 76 | 5.3 | 48.2 |
| 100 | 6.8 | 45.8 |
| 150 | 7.9 | 40.9 |
| 295 | - | 26.6 (tentative) |

2) Axial Tension Properties of An Single Modular Coil (ASTM D-3039)

- 15.0-inch long [2]

| Temperature (K) | Tension Modulus (Msi) | Tension Strength (ksi) | Poisson's Ratio |
| --- | --- | --- | --- |
| 76 | 14.4 | 33.6 | 0.38 |
| 100 | 12.4 | 32.0 | 0.38 |
| 150 | 14.1 | 27.4 | 0.30 |
| 295 | 13.2 (tentative) | 25.0 | - |

- Flexural Properties of An Single Modular Coil (ASTM D-790)

- 10.0-inch long [2]

|  | Flatwise | Flatwise | Edgewise | Edgewise |
| --- | --- | --- | --- | --- |
| Temperature (K) | Flex. Modulus (Msi) | Flex. Strength (ksi) | Flex. Modulus (Msi) | Flex. Strength (ksi) |
| 76 | 4.3 | 43.0 | 4.0 | 44.8 |
| 100 | 4.3 | 39.8 | 4.5 | 43.4 |
| 150 | 4.3 | 39.4 | 4.1 | 38.9 |
| 295 | 3.9 | 27.7 | 3.7 | 29.5 |

Note: Flatwise means bending the specimen about its weaker axis while edgewise means 	bending the specimen about its stiffer axis

- Flexural Properties of A 2x2 Modular Coil Bundle (ASTM D-790) [2]

| Temperature (K) | Flexural. Modulus (Msi) | Flexural Strength (ksi) |
| --- | --- | --- |
| 76 | 4.1 | 40.9 |
| 100 | 3.2 | 35.1 |
| 150 | 2.9 | 30.1 |
| 295 | 2.6 | 25.6 |

Note: The test results for flexural strength and modulus of a bundle is lower than the values for a single modular coil conductor

- Shear Properties of A 2x2 Modular Coil Bundle (ASTM D-2344)  [2]

| Temperature (K) | Shear Modulus (Mpsi) | Shear Strength (ksi) |
| --- | --- | --- |
| 76 | 2.3 | 3.9 |
| 100 | 2.0 | 3.6 |
| 150 | 1.2 | 2.9 |
| 295 | 1.1 | 2.2 |

- CTE of An Single Insulated MC Conductor in the Longitudinal Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (9.53 + 8.87)/2 = 9.20 |
| 100 | (11.74+10.37)/2 = 11.06 |
| 150 | (15.42+15.97)/2 = 15.70 |
| 293 | (22.35+20.50)/2 = 21.43 |

- CTE of An Single Insulated MC Conductor in the Transverse Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (9.41 +11.14)/2 = 10.28 |
| 100 | (12.00+11.92)/2 = 11.96 |
| 150 | (15.94+16.24)/2 = 16.09 |
| 293 | (22.00+19.13)/2 = 20.57 |

- CTE of MC Turn Insulation in the Longitudinal Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (7.33 + 7.81)/2 = 7.57 |
| 100 | (11.00+11.29)/2 = 11.15 |
| 150 | (15.43+15.99)/2 = 15.71 |
| 293 | (19.36+19.47)/2 = 19.42 |

- CTE of MC Turn Insulation in the Transverse Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (11.28+10.58)/2 = 10.93 |
| 100 | (12.78+12.80)/2 = 12.79 |
| 150 | (14.60+15.64)/2 = 15.12 |
| 293 | (16.71+17.89)/2 = 17.30 |

- CTE of MC Ground Insulation in the Longitudinal Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (7.12 + 11.15)/2 = 9.14 |
| 100 | (12.02+12.11)/2 = 12.07 |
| 150 | (14.36+14.50)/2 = 14.43 |
| 293 | (20.32+21.05)/2 = 20.69 |

- CTE of MC Ground Insulation in the Transverse Direction [3]

Average of two specimens

| Temperature (K) | Coef. of Thermal Expansion (10x-6 m/m/K) |
| --- | --- |
| 76 | (7.75 +10.30)/2 = 9.03 |
| 100 | (10.66+11.17)/2 = 10.92 |
| 150 | (12.42+13.28)/2 = 12.85 |
| 293 | (20.16+21.16)/2 = 20.66 |

References

[1] CTD, CTD 101K CTE properties (neat resin), 1/23/2004

[2] Zatz I., Interim Materal Properties, 12/12/2003

[3] Fabian, Paul E., Test Program to Determine the Mechanical and Thermal Properties of the Epoxy/Insulation System for the NCSX Modular Ciols, Subcontract S-04353-G Report, 11/21/2003

[4] Kozub, T., Casting alloy CTE, 3/4/2004

[5] Kozub, T., NCSX Short Race-Track Coil Test at LN2 Temperature, 5/13/2004

[6]  Kozub, T., NCSX Composite Coil Testing, 4/5/2004

[7]  Kozub, T., NCSX Composite Coil Testing, 3/22/2004

[8]  Kozub, T., NCSX Composite Coil Testing, 3/15/2004

[9]  Kozub, T., SRT3 20X Life Cycle Test, 6/21/2004

[10] Kozub, T., NCSX Composite Coil Testing, 4/12/2004

[11] Kozub, T., NCSX Peer Review - Cable Conductor Material properties, Part II, Material Testing, 5/6/2004

[12] ITER, Structural Material Database, Article 3, Non-Metallic Material Database & Specifications, N11 FDR 2601-07-04 R0.1

[13] CTD, Inc., Engineered Material Solution – CTD-101K Epoxy Resin System