# Text boxes

※ Not Required for Stainless Steel Case

Shell Plate

Large Port

Opening

Cut Out

Water Jet

Fixing

Visual

Inspec.

Marking

Dimension

Check

(3D-Gauge)

Cold

Press

Attach PL.

Shell.PL.

※

Press

Hot Bend

Marking, Cutting

※

Attach Plate

required for

hot sizing

(heat mass)

Marking

Cutting

Water Jet

※

Heat up

※

Weld

※

Assy.

※

Hot Sizing

※

Removal

Attach PL.

Cutting

3D-Water

Jet

Cold

Press

for modifica-tion

Dimension

Check

(3D-Gauge)

Edge

Preparation

3D-Machining

Assy.

Shell Plate

Fixture Jig

Weld

Out Side

Removal

Fixture

Dimension

Inspec. 3D

Dimensional

Stabilizing

Heat Treatment

415℃

Marking

Port Opening

Edge Prep.

Machining

Port

Reinforcement

Assembly

Weld

Weld

Check

Closure

Plate for

Opening

Assy.

Closure

Plate

Weld

Stabilizing

Heat Treat

415℃

He

Leak

Test

under thermal

cycles

Removal

Closure Plate

Port Reinforcement and

Sector Flange

Marking

Cutting

Bending

Cold

Press

Cutting

3D. Water

Jet

Machine

3D

Dimension

Inspec.

Clean

Small Port

Opening

Cut Out

Water Jet

Large & small

Port Opening

Machine &

Edge Prep.

Cleaning

Removal

Fixture

Dimension

Inspection

Cleaning

Packing

Shipping

Weld

Inside

Back

Chip

Grinding

# ※Vessel shells set on Press machine

# after heated up to 900 C for JT-60U VV

(Hot-sizing press forming)

Dotted line : Special process required for Inconel 625

## NCSX Vacuum Vessel Fabrication Procedures  (Draft #1)

Attachment-4