Conclusions:  7/17 conference call on welds

Attendees:  PJ Fogarty; D. Williamson; P. Heitzenroeder; H. Neilson; W. Reirson;  R. Parsells; L. Dudek; B. Nelson; K. Freudenberg

Notes about the FEA models:

All shear goes through the welds.
	The flanges can separate.

- A/B flange weld tests:

  - ½” welds are fine from the point of view of stress – peak stress is 19 ksi. (ignoring singularity)

  - Will proceed with 2 U shims set back ¾” , but only weld ½”.

  - All welds will be ½”.

  - Kevin – re-check shear stresses to verify acceptability.

- A-B Casting weld tests:

  - Use the ¾” setback shims, but position shims for ½” setback.

- A-A flange weld stresses are very low – (model of continuous weld ~9ksi – allowing for segmentation peak stress might be ~14 ksi, which is fine!)

- B-C flange welds:

  - Peak stress presently is ~25 ksi, but in  2 elements, peak otherwise is 20 ksi. in that region of concern.  The remainder is about 16 ksi.

  - PJ will reconfigure shims in this area, using the wooden flange models to guide the design (ie, similar to the A/B transition shims that Fred devised).

  - Kevin will re-analyze stresses, first with ½” welds and then with ¾” welds for shims 1,2, and 3.

  - Kevin will also look at extending 1-2 bolts as a way of reducing these high stresses.  Bolt re-tightening may be an issue.

- Longer term:  Kevin is also to look at other load cases to verify that the worst case conditions have, in fact,  been identified.

Guiding philosophy for Lehman and Interface FDR:

We will keep peak stresses to <20 ksi (vs. 31.5 ksi allowable) by local weld sizing (ie, going to ½ x ¾ butt welds or fillet welds with 1/4” cover pass over them locally or use notched fillet welds similar to that which Fred devised for the a-b flange test. )