# Ground wrap insulation

1.588 + 4.123 x 2 = 11.422 inches perimeter of bundle

Twisted racetrack coil= approximately 200 inches in length

Layer 1 (Outer):

2 in. wide x 0.007 in. thick S-2 glass tape (butt lapped) = 100 wraps x 11.422 in.  = 1142 inches  = 32 yards

Layer 2 (Mid):

2 in. wide x 0.007 in. thick S-2 glass (half-lapped) = 200 wraps x 11.422 in.  = 2284 inches = 64 yards

1.5 in. wide x 0.00625 in thick Kapton (1/2-in. overlap) = 200 wraps x 11.422 in.  = 2284 inches = 64 yards

Layer 3 (Inner):

2 in. wide x 0.007 in. thick S-2 glass tape (butt lapped) = 100 wraps x 11.422 in.  = 1142 inches  = 32 yards

1.5 in. wide x 0.00325 in thick Kapton (1/2 inch space between wrap) = 100 wraps x 11.422 in.  = 1142 inches = 32 yards

## Groundwrap Insulation Plan

# Text boxes

1.588-in

REF

4.123-in

REF