(I) Analysis of the Modular Coil Conductor Flexure Test Data

1. Raw Data shows some inconsistent results (duplications, jumpy values)

| SC4A-4 | CC9A-4 |
| --- | --- |
| Deflection [mils] | Load [lbf] | Deflection [mils] | Load [lbf] |
| 237.71 | 1.31 | 238.59 | 0.58 |
| 240.07 | 3.78 | 240.69 | 0.58 |
| 240.07 | 6.24 | 243.18 | 3.78 |
| 240.07 | 6.24 | 243.30 | 6.24 |
| 240.07 | 6.58 | 243.30 | 6.24 |
| 240.19 | 7.99 | 243.55 | 6.92 |
| 241.20 | 13.94 | 244.29 | 10.12 |
| 241.20 | 13.94 | 245.04 | 13.60 |
| 241.20 | 17.47 | 245.04 | 13.60 |
| 243.55 | 23.47 | 247.02 | 18.54 |
| 243.55 | 23.47 | 249.38 | 22.07 |
| 245.77 | 24.88 | 249.38 | 22.07 |
| 247.40 | 29.09 | 252.11 | 29.43 |
| 249.99 | 33.64 | 253.85 | 34.37 |
| 249.99 | 33.64 | 255.95 | 38.24 |
| 251.50 | 39.30 | 255.95 | 38.24 |
| 253.22 | 41.38 | 258.07 | 45.59 |
| 253.22 | 41.38 | 260.67 | 50.19 |
| 255.34 | 48.79 | 260.67 | 50.19 |
| 258.57 | 48.79 | 263.28 | 61.08 |
| 260.17 | 54.07 | 264.64 | 61.08 |
| 260.17 | 54.07 | 266.01 | 64.28 |
| 261.04 | 58.61 |  |  |
| 264.53 | 66.02 |  |  |
| 264.53 | 66.02 |  |  |
| 266.51 | 71.30 |  |  |
| 268.37 | 71.30 |  |  |
| 270.60 | 75.85 |  |  |
| 270.60 | 75.85 |  |  |
| 270.72 | 79.38 |  |  |

2. Typical Force-Deflection Curves (Cleaned-Up)

Stiffness (m) of Specimen SC4A (Insulated): 	2160 lbf/in (Tom: 2128)

Stiffness (m) of Specimen CC9A (Bare):		2340 lbf/in (Tom: 2332)

>> The linear curve-fit appears to provide sufficient data conditioning.

3. Maximum Specimen Loads

The insulated conductor specimens are on-average loaded 50% higher than the bare specimens.

(II) Analysis of the Modular Coil Conductor Flexure Model Results

1. 3D Quarter-Symmetry ANSYS Model of Bare Conductor

- 10” long, L=6”, b=0.314”, d=0.349”, E=9.63 Mpsi (average of RT specimens)

- Stiffness by formula: m = 4Eb(d/L)3 = 2380 lb/in

- Stiffness by 3D model: m = Force/Disp = 2358 lb/in

- Stiffness by Test Data: mave = 2373 lb/in

2. 3D Quarter-Symmetry ANSYS Model of Insulated Conductor

- 10” long, L=6”, b=0.314”, d=0.349”, tIns=0.012”, E(Cond/Insul)=9.63/3.19 Mpsi

- Stiffness by formula: m = 48EI/L3 = 2628 lb/in

- Stiffness by 3D model: m = Force/Disp = 2599 lb/in

- Stiffness by Test Data: mave = 2211 lb/in (Why lower?)