NCSX Modular Coil Analysis Meeting Notes – Feb. 24, 2004.

Axial compression specimens:

- Aspect ratio of 1.6 causes barreling

- Should use an aspect ratio of 5-10.

- Remove the insulation.

- Use extensometers

Transverse compression specimens:

- Make a 2 x 5 VPI bundle.  This increases the length.

- PPPL's tester ram has a 4" dia.

- Use bare conductor.

- Non-destructive test. (hopefully!)

- Use extensometers across the whole sample.

- Do RT & LN2 temperatures.

- 3 samples / temp.

Tension specimens: for E in tension

- Use bare cable.

- Length:  2-4" for the test length.  + grip lengths.

- Use extensometers.

- Test at RT & LN2 temp.

- 3 samples / temp.

Notes:

- Measured strain from ep-gl surface.  This "shell" does not strain at the same rate as the Cu.

- LVDT measured actuator displacement.  Need to compensate for machine compliance.  CTD thinks this data is as good as you can get with displ. "off the specimen".

- Oak Ridge did similar measurement – got fairly similar results.  It's soft!

Cable Notes:

- Cable should be expected to behave much differently in tension and compression.

- Can probably only determine this from tests.

- May behave inelastically due to bending of individual strands.

- Cyclic flexure testing may be useful.

- Key is to put the strain gauge or extensiometer on the copper, NOT on the ep-gl shell.

- Pete suggests making a long bar and stretching it.  Jim can make up to 5' – currently has 4' specimens.

Thermal:

- Currently used potted samples to derive thermal conductivity.  Believed to be conservative.

- Len's model was monolithic but with no axial heat path.  Explicit model with traditional values of K for epoxy and cu.

- Brad notes we can let T go up slightly – this will force the winding onto the winding form and cool better.

- We need cured cable specimens and measure shrinkage from after it's cured all the way down to 80 K.  No current plan!

- Also need to measure cure shrinkage of the gl-ep composite.

-DR suggests doing it with the total cable-gl-ep-Kapton.

-PF suggests measuring mold cavity and comparing final cured cable 	dimensions to it. Need to use same pressures as used in "real" coil.

-JC suggests using straight T mold and measuring the change in 	length.

Flexure Test:

- Single conductor.

- Strain gauges top & bottom

- Dial indicators  along the length to measure bending profile.

- 20" overall length;  12" span.  Don't cut them all until results are obtained from this.

- Need the specimens to extend 4"  beyond the end supports.

- Need to decide what the failure mode is likely to occur in the specimen.

- PT suspects the bonded cable  has poor shear capacity.

- Need shear modulus, transverse compression.

- Get direct tension in legs of racetrack.

- Need to instrument it well enough to get a deformation profile.

- Use beam in a model with 3-point bend – use E-tension from racetrack and adjust shear modulus until the deformation profile matches.

- CTD suggests micromechanical modeling to guide the testing.

Fatigue:

- What is the criteria for failure?  Change in resistance?  Change in stiffness?  Displacements that affect field properties?

- Prefer that the coil strain be kept below some limit that does not change any of these properties.

- A wimpy winding is best – lets the winding form define the shape and dimensions.

- Fatigue criteria "strawman":  The winding shall not change in resistance by more than 5%, change in stiffness as measured by the "spring constant" of a racetrack shaped test coil of more than 5% when fatigue tested within the expected strain limits for a lifetime of 20?? x life or for life at 2?? x the expected strain limits.

- Initially, use strain rate predicted with soft cable properties.

- Dave to provide guidance.

- Mechanical test with resistance monitoring.

- The racetrack should use insulated cable.

- Test at LN2 temperature and RT.

- Test at 1 Hz.  It will take 36 hrs. to get 130,000 cycles.

Insulation Fatigue Life- modular coils only:

- Need to qualify the EXACT insulation system also (gl/kapton/ep).

- Use Inclined Shear/Compression test specimens.

- Use "standard" design criteria.

- The ITER data might suffice, (this is also for  CTD-101K)  but this would not reflect the Kapton.  Paul will provide data to Wayne.

Clean vs. Unclean Cable Strand:

- Beam test "up front" of a cleaned and uncleaned specimens to determine difference, if any.

Friday's Agenda:

- Review the above with Dick and fine tune.

- Dave, HM, and Len develop a plan for kick-off of mod. Coil checking/analyses.

- Fred, Pete set up a time for Pete to visit. During this visit, we will also discuss seismic calculations with him.