###### NCSX

Copper Cable Keystone Tests

By:  Jim Chrzanowski

November 5, 2001

SCOPE:  Perform tests on the proposed rectangular compacted copper cable to determine the amount of Keystoning which would result during winding of the Modular coils for NCSX.  Two Keystone trials were performed winding the copper braid conductor in both directions. Trial #1 was performed winding the conductor with the narrow side against the mandrel.  Trial #2 was performed winding the conductor with the wide side against the mandrel.

- Measurements were taken with the copper cable conductor bare.  (See Table 1)

- One half-lapped layer of dry glass insulation was applied over the bare conductor.  (1 inch wide x 0.007 inches thick)

- Measurements were taken with insulation on conductor. (See Table 1)

- The insulated conductor was hand wound onto a mandrel with a measured diameter of 3.181 inches.

- Once wound, conductor measurements were taken.  These steps were repeated for both trial sets.

# Table 1- Initial Conductor Measurements

| Location | Bare | Insulated | Bare | Insulated |
| --- | --- | --- | --- | --- |
|  | Side A | Side A | Side B | Side B |
| 1 | 0.631 | 0.653 | 0.519 | 0.541 |
| 2 | 0.637 | 0.655 | 0.520 | 0.542 |
| 3 | 0.640 | 0.660 | 0.525 | 0.553 |
| 4 | 0.640 | 0.660 | 0.529 | 0.548 |
| 5 | 0.640 | 0.664 | 0.525 | 0.547 |
| 6 | 0.640 | 0.660 | 0.534 | 0.554 |
| 7 | 0.640 | 0.665 | 0.539 | 0.558 |
| 8 | 0.642 | 0.668 | 0.538 | 0.556 |
| 9 | 0.633 | 0.660 | 0.537 | 0.557 |
| 10 | 0.635 | 0.660 | 0.535 | 0.557 |
| 11 | 0.635 | 0.650 | 0.535 | 0.556 |
| 12 | 0.635 | 0.665 | 0.530 | 0.548 |
| Average | 0.637 | 0.660 | 0.531 | 0.551 |

Trial #1- Conductor                                           Trial #2- Conductor

Winding Direction                                                Winding Direction

Side A         Bare

Side B                  Bare

Side B                                                                  Side A

Center Line- Winding Axis

# Results of Keystone Tests

## Trial #1                                                        Trial #2

Side C

Side C

Side A                             Side B              Side A                                       Side B

Side D                                                            Side D

Center Line- Winding Axis

# Table –2  Keystone Results- Trial #1

| Location | Insulated | Insulated | Insulated | Insulated |
| --- | --- | --- | --- | --- |
|  | Side A | Side B | Side C | Side D |
| 1 | 0.663 | 0.650 | 0.505 | 0.631 |
| 2 | 0.652 | 0.647 | 0.510 | 0.645 |
| 3 | 0.668 | 0.655 | 0.504 | 0.638 |
| 4 | 0.658 | 0.662 | 0.510 | 0.649 |
| 5 | 0.680 | 0.670 | 0.520 | 0.661 |
| 6 | 0.667 | 0.660 | 0.512 | 0.646 |
| 7 | 0.658 | 0.650 | 0.515 | 0.650 |
| 8 | 0.665 | 0.640 | 0.514 | 0.662 |
| 9 | 0.670 | 0.645 | 0.510 | 0.640 |
| Average | 0.665 | 0.653 | 0.511 | 0.647 |

# Table-3  Keystone Results- Trial #2

| Location | Insulated | Insulated | Insulated | Insulated |
| --- | --- | --- | --- | --- |
|  | Side A | Side B | Side C | Side D |
| 1 | N/A | N/A | 0.716 | 0.635 |
| 2 | 0.545 | 0.543 | 0.719 | 0.624 |
| 3 | 0.542 | 0.541 | 0.721 | 0.641 |
| 4 | 0.577 | 0.572 | 0.723 | 0.640 |
| 5 | 0.552 | 0.591 | 0.735 | 0.640 |
| 6 | 0.570 | 0.593 | 0.733 | 0.650 |
| 7 | 0.561 | 0.575 | 0.735 | 0.641 |
| 8 | 0.521 | 0.554 | 0.748 | 0.628 |
| 9 | 0.539 | 0.550 | 0.722 | 0.628 |
| Average | 0.551 | 0.565 | 0.728 | 0.636 |

#### Summary of Results

##### Trial #1…..Conductor Measurements

0.511 in.

Conductor                                                                     Conductor

Before                                                                             After

0.660 in.        Winding                                               0.665 in.          Winding         0.653 in.

0.551 in.                                                                            0.647 in.

Center Line- Winding Axis

Figure 1-  Trial #1 “Conductor Removed from Mandrel”

##### Trial #2….. Conductor Measurements

0.660 in.                                                                           0.636 in.

Conductor                                                                         Conductor

0.551 in.               Before				0.551 in.                    After                       0.565 in.

Winding                                                                             Winding

0.728 in.

CL Winding Axis

Figure 2- Trial #2  “Conductor Removed from Mandrel”

Note:  Any discrepancies in measurements are a result of conductor not being entirely rectangular prior to start of Trial #1 and reuse of same copper cable conductor for Trial #2.