# NCSX

## Coil Development Program

## Test Series #2

Vacuum Impregnation (VPI)

Of Tensile Specimen

Written By:  James H. Chrzanowski

December 5, 2002

TEST SERIES #2- VPI of Tensile Test Specimens

- Purpose: To prepare and to vacuum impregnate (2) insulated compacted copper rope specimens for material property testing.  The process will also be used to develop the VPI process for future coil impregnations.

- Materials and equipment:

  - Compacted copper rope (0. 5 inch x 0.63 inch)

  - Dry glass insulation (0.007 inch thick x ¾ inch wide)

  - Kapton insulation (0.00325 inch thick x ¾ inch wide)

  - 3-part epoxy system. …Product no. CTD-101K (Composite Technology Development Inc.)

  - 2-part stainless steel mold

  - Vacuum oven

  - Epoxy delivery system

- Test Procedure:

The following steps are to be used as a guide.  The Test Director has the authority to modify the tests.  All information from these tests is to be documented in the Logbook, including preparation activities, collected data, and changes to the SOW.

- Preparations:

  - Note:  Cotton gloves shall be worn during the handling of the copper insulation and during the insulating process.

## A.	Conductor Preparation

  - Cut (2) compacted copper rope specimens approximately 45 inches in length.

  - Apply (1) ½ lapped layer of dry glass (0.007 in. thick) and (1) ½ lapped layer of composite insulation dry-glass & Kapton tape over each copper conductor.  (See figure No. 1)

  - Once completed, cover conductors to ensure cleanliness prior to installing into the mold.

## B.	Mold Preparation

- Thoroughly clean and degrease the mold.  (See Figure 2)

- Apply spray mold release over all faces of the mold, which will be in contact with the epoxy resin.

Figure No. 2

- Apply spray mold release over all faces of the mold, which will be in contact with the epoxy resin.

- Install the (2) insulated copper conductors into the pockets provided in the mold.

- Secure the (2) halves of the mold together with a “Gortek” O-ring in position to provide the vacuum seal.

- Secure tygon tubing to the (4) inlet and outlets.

- Install the mold into the vacuum oven.

- Hookup the mold and epoxy delivery system per the diagram in Figure No. 3.

- Apply a vacuum to the mold as soon as possible by opening valves V3, V4 and V6.

# Figure No. 3 Epoxy Delivery System

V1….	To lower fill port #1			 Pressure gauge

V2….	To lower fill port #2			 Vacuum gauge

V3….	To upper fill port #1

V4….	To upper fill port #2

V5….	Vacuum pump to epoxy fill tank

V6….	Vacuum pump to epoxy overfill tank

## C.	Epoxy Preparation

Epoxy components by weight: CTD-101K  (3-part epoxy system)

  - Resin: (Part A)		100.0 parts-by-weight

  - Hardener: (Part B)		  90.0 parts-by-weight

  - Accelerator: (Part C) 		    1.5 parts-by-weight

- Approximately 1-gallon mixture will be prepared for the injection.

- Components should be pre-heated to 40-45 degrees C for at least 4 hours prior to mixing.

- Weigh out the components per the ratio’s identified above.

- Combined the combine the components into a container and thoroughly mix the components for approximately 10 minutes.

- Pour off approximately 1.5 pints to be used for viscosity measurements during impregnation.

Note:  The viscosity of the resin is to be monitored throughout the process.

## D.	VPI Procedure

- Pour the mixed components into the epoxy fill tank and seal the lid.

- Open valve V5 and apply a vacuum to the mixed epoxy components.  Maintain the vacuum on the epoxy for approximately 30 minutes. (Test Directors discretion)

- Close valve V5 and vent the epoxy tank to atmosphere.

- Slowly open valves V1 and V2 to allow the epoxy to enter the lower end of the mold.

- Continue until epoxy resin is exiting V3 and V4.  (Test Directors discretion)

- Close valves V3 and V4.

- The Test Director may elect to apply slight pressure (10 psig max) to the mold to milk the epoxy.

- Once the Test Director feels that the epoxy filling of the mold specimens is complete, begin to slowly ramp up the oven temperature by 20 degrees per hour until 135 degrees C has been reached. (accelerated cure cycle)

- Maintain the oven temperature for 1.5 hours at 135 degrees C.

- During this process the viscosity samples should periodically checked.

- After 1.5 hours at 135 degrees C, shut off the oven, and allow the mold to return to room temperature.

- Remove the mold from the oven.

- CAREFULLY open up the mold and remove the impregnated specimens.

#### VPI DATA SHEET

________________________________________________________________________

## Date of Test:				Test Director:

Team Members: ________________________________________________________________________

EPOXY MIX DATA

Weight of components-	Part A

Part B

Part C

Mixing time:

VACUUM READINGS:

Mold prior to impregnation:

Degassing of epoxy:

During VPI process:

PROCESS TIMES:

Start of Degassing operation:	_________	End of Degassing operation: __________

Start of Epoxy Fill: _________________	End of Epoxy Fill: ______________

Start of Ramp Up: __________________	Cure Temp. Reached: ______________

End of Cure Cycle: __________________

NOTES and OBSERVATIONS:

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

NOTES AND OBSERVATIONS

# Text boxes

Figure No. 1

Vac. pump

Epoxy Fill Tank

Epoxy overfill Tank

Mold

OVEN

Cold trap

### Vent

V1

V2

V3

V4

V6

V5

N2

V

P

P

V

V

P