# NCSX

## Coil Development Program

## Test Series #6

Vacuum Impregnation (VPI)

Of Tensile Specimen- 4 conductor

Written By:  James H. Chrzanowski

April 1, 2003

TEST SERIES #4- VPI of Tensile Test Specimens

- Purpose: To prepare and to vacuum impregnate (2) insulated compacted copper rope specimens for material property testing.  The process will also be used to develop the VPI process for future coil impregnations.  Note: Two additional sprues were added mid way to improve fill cycle.

- Materials and equipment:

  - Compacted copper rope (0.250 inch x 0.3125 inch) 2x2 bundle

  - Dry glass insulation (0.007 inch thick x ¾ inch wide)

  - Kapton insulation (0.00325 inch thick x ¾ inch wide)

  - 3-part epoxy system. …Product no. CTD-101K (Composite Technology Development Inc.)

  - 2-part stainless steel mold

  - Vacuum oven

  - Epoxy delivery system

- Test Procedure:

The following steps are to be used as a guide.  The Test Director has the authority to modify the tests.  All information from these tests is to be documented in the Logbook, including preparation activities, collected data, and changes to the SOW.

- Preparations:

  - Note:  Cotton gloves shall be worn during the handling of the copper insulation and during the insulating process.

## A.	Conductor Preparation

  - Cut (2) compacted copper rope specimens approximately 45 inches in length.

  - Apply (1) ½ lapped layer of dry glass (0.007 in. thick) and (2) ½ lapped layer of composite insulation dry-glass & Kapton tape over each copper conductor.  (See figure No. 1)

  - Once completed, cover conductors to ensure cleanliness prior to installing into the mold.

## B.	Mold Preparation

- Thoroughly clean and degrease the mold.  (See Figure 2)

- Apply spray mold release over all faces of the mold, which will be in contact with the epoxy resin.

Figure No. 2

- Apply spray mold release over all faces of the mold, which will be in contact with the epoxy resin.

- Install the (2) insulated copper conductors into the pockets provided in the mold.

- Secure the (2) halves of the mold together with a “Gortek” O-ring in position to provide the vacuum seal.

- Secure tygon tubing to the (6) inlet and outlets.

- Install the mold into the vacuum oven.

- Hookup the mold and epoxy delivery system per the diagram in Figure No. 3.

- Apply a vacuum to the mold as soon as possible by opening valves V3, V4 and V6.

- Pre-heat oven and mold to 55 degrees C prior to VPI.

# Figure No. 3 Epoxy Delivery System

V1….	To upper fill port #2

V2….	To lower fill port #1			 Pressure gauge

V3….	To lower fill port #2			 Vacuum gauge

V4….	To upper exit port #1

V5….	To upper exit port #2			V6….	To upper exit port #3

V7….	To upper exit port #4                         	V8….	Vacuum pump to epoxy fill tank

V9….	Vac. pump to epoxy overfill tank	V10...	Main fill valve

## C.	Epoxy Preparation

Epoxy components by weight: CTD-101K  (3-part epoxy system)

  - Resin: (Part A)		100.0 parts-by-weight

  - Hardener: (Part B)		  90.0 parts-by-weight

  - Accelerator: (Part C) 		    1.5 parts-by-weight

- Approximately 1-gallon mixture will be prepared for the injection.

- Components should be pre-heated to 55 +/- 5 degrees C for at least 4 hours prior to mixing.

- Weigh out the components per the ratio’s identified above.

- Combined the combine the components into a container and thoroughly mix the components for approximately 10 minutes.

- Pour off approximately 1.5 pints to be used for viscosity measurements during impregnation.

Note:  The viscosity of the resin is to be monitored throughout the process.

## D.	VPI Procedure

- Pour the mixed components into the epoxy fill tank and seal the lid.

- Open valve V9 and apply a vacuum to the mixed epoxy components.  Maintain the vacuum on the epoxy for approximately 30 minutes. (Test Directors discretion)

- Close valve V9 and vent the epoxy tank to atmosphere.

- Open valves V2 and V3. Slowly open valve V1 to allow the epoxy to enter the lower end of the mold.

- Continue until epoxy resin is exiting V4 and V5.  (Test Directors discretion)

- Close valves V4 and V5.

- Continue until epoxy resin is exiting V6 and V7.  (Test Directors discretion)

- Close valves V6 and V7.

- The Test Director may elect to apply slight pressure (10 psig max) to the mold to milk the epoxy.

- Once the Test Director feels that the epoxy filling of the mold specimens is complete, begin to slowly ramp up the oven temperature by 20 degrees per hour until 110 degrees C has been reached. (Cure temperature)

- Maintain the oven temperature for 5 hours at 110 degrees C.

- During this process the viscosity samples should periodically checked until the samples GEL.

- After 5 hours at 110 degrees C, ramp-up the oven to 125 degrees C.

- Maintain the oven temperature for 15 hours at 125 degrees C.

- At the end of the cure cycle, shut off the oven, and allow the mold to return to room temperature. DO NOT open the oven until the mold has returned to a temperature of at least 40 degrees C.

- Remove the mold from the oven.

- CAREFULLY open up the mold and remove the impregnated specimens.

#### VPI DATA SHEET

________________________________________________________________________

## Date of Test:				Test Director:

Team Members: ________________________________________________________________________

EPOXY MIX DATA

Weight of components-	Part A

Part B

Part C

Mixing time:

VACUUM READINGS:

Mold prior to impregnation:

Degassing of epoxy:

During VPI process:

PROCESS TIMES:

Start of Degassing operation:	_________	End of Degassing operation: __________

Start of Epoxy Fill: _________________	End of Epoxy Fill: ______________

Start of Ramp Up: __________________	Cure Temp. Reached: ______________

End of Cure Cycle: __________________

NOTES and OBSERVATIONS:

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

NOTES AND OBSERVATIONS

# Text boxes

Figure No. 1

Vac. pump

Epoxy Fill Tank

Epoxy overfill Tank

Mold

OVEN

Cold trap

### Vent

V1

V3 [right side]

V7

V6

V9

V8

N2

V

P

P

V

V

P

V2

V5

V4

Drain

Drain

V10