# NCSX

## Coil Development Program

## Test Series #16

Vacuum Impregnation (VPI)

Straight Tee Section

Written By:  Thomas Meighan

February 20, 2004

TEST SERIES #5- VPI of Straight Tee Specimens

- Purpose: To prepare and to vacuum impregnate a straight length tee section similar to the Modular coil cross-section with (40) insulated compacted copper rope specimens for material property testing.  This test series will also be used to develop the VPI process and to evaluate the integrity of the proposed bag mold for future coil impregnations.

- Materials and equipment:

  - Compacted copper rope (0. 350 inch x 0..391 inch)

  - Dry glass insulation (0.004 inch thick x 1 inch wide)

  - 3-part epoxy system. …Product no. CTD-101K (Composite Technology Development Inc.)

  - Stainless tee-section

  - Vacuum oven

  - Epoxy delivery system

  - ½ ID inch Chemflour tubing

- Test Procedure:

The following steps are to be used as a guide.  The Test Director has the authority to modify the tests.  All information from these tests is to be documented in the Logbook, including preparation activities, collected data, and changes to the SOW.

- Preparations:

  - Note:  Cotton or Nitril gloves shall be worn during the handling of the copper insulation and during the insulating process.

## A.	Conductor Preparation

  - Cut (80) compacted copper rope specimens approximately 48 inches in length.

  - Apply (1) ½ lapped layer of dry glass (0.004 in. thick) over each copper conductor.  (See figure No. 1)

  - Once completed, cover conductors to ensure cleanliness prior to installing into the mold.

##### End View- Cross Section [enlarged] showing half lapped winding concept

## B.	Tee Section Preparation

- Thoroughly clean and degrease the Tee section.  (See Figure 2)

- Apply spray mold release over all faces of the Tee section, which will be in contact with the epoxy resin.

- Install the inner copper Chill Plate and secure in place with a little RTV on the both ends.

4	Lay (3) layers of 0.010-inch thick dry glass and (2) layers of 0.003-inch Kapton film onto the open faces of the tee section.  Leave sufficient glass to over wrap the entire bundle once the (40) turns are in position.

Straight Tee Section- Figure No. 2

Install (4) layers of 10 turns each of the insulated copper conductors onto each side of the tee section. [80 total turns] See figure No. 4.  Ensure that the turns are held securely in place during the assembly process.

- Overlay the dry glass/Kapton ground wrap over the outside surface of the turns and secure in place with Kapton tape.

- Install the outer Copper Chill Plate and hold in place with clamps.

- Repeat this process for the opposite side of the tee section. [1]

- Install the epoxy feed sprus into the bundle at 11 locations.  Four locations on each side of the top edge of the bundle, four locations between the coil clamps (2 per clamp) and 2 locations on the end plate of the top side as shown in figure no. 3.  Seal them in place with silicone RTV. [3]

.

Install (2) layers of silicone rubber tape over the copper chill plate, forming a bag over the specimen. The ends shall be pressed into the groove with copper tubing and held in place with a strong back between the clamps.  [4]

- Paint RTV-11 over the bag surface to seal any small leaks in the bag and allow the RTV to cure before proceeding].  Once the RTV cures, pump down and look for leaks. Apply RTV sealer 108 to back of the 1/32” G-10 washer and place washers over the sprues and press firmly into place making contact with the self-fusing tape. Install the final coil clamps.

- Install epoxy impregnated felt between the clamps. [6]

- Install strong backs between the clamps to secure the ends of the silicone bag and impregnated felt. [7]

Epoxy Spru Configuration- Figure No. 3

Bag Mold Assembly Figure No. 4

- Secure ½ inch ID “Chemflour” tubing to the (11) Spru inlet and outlets.

- Install the mold into the vacuum oven and secure into position.

- Rotate the oven with the Tee specimen from the horizontal to vertical position using the overhead jib crane.  Secure in position.

# Test Director verify: ______________________ Date: __________

- Connect the bag mold Sprues to the epoxy delivery system per the diagram in shown in Figure No. 5.  Close all valves.

- Apply a vacuum to the mold as soon as possible by opening valves V8, V9, V10, V11, V12, V13, V14, V16 and V18

- Open valve V17 and place the vacuum oven under an equal vacuum as is being applied to the bag mold.

VALVE IDENTIFICATION KEY

V1….	To epoxy fill tank 			V9….	To mid fill/ return port

V2….	To upper fill port on bottom 		V10…. To epoxy return tank from mid port

V3….	To upper fill port on bottom		V11….  Return from 3/4  pt on Mold

V4….	To 1/4 fill port on side		V12….	To epoxy return from top of mold

V5…	To 1/4 fill port on side		 V13…	To epoxy return from top of mold

V6….	To mid fill/return port 		V14…	 Return from 3/4 pt on Mold

V7….	To mid fill/ return port		V15…	Epoxy fill tank Vacuum valve

V8….	To mid fill/ return port		V16…	Epoxy overfill Vacuum valve

V17…	Oven Vacuum valve

V18…	To epoxy return from Lead Box

Pressure gauge      	Vacuum gauge

## C.	Epoxy Preparation

Epoxy components by weight: CTD-101K  (3-part epoxy system)

  - Resin: (Part A)		100.0 parts-by-weight

  - Hardener: (Part B)		  90.0 parts-by-weight

  - Accelerator: (Part C) 		    1.5 parts-by-weight

- Approximately 3.5-gallon mixture will be prepared for the injection.

- Components should be pre-heated to 40-45 degrees C for at least 4 hours prior to mixing.

- Weigh out the components per the ratio’s identified above.

- Combine the components into a container and thoroughly mix for approximately 15 minutes.

- Pour off approximately 1.5 pints to be used for viscosity measurements during impregnation.

Note:  The viscosity of the resin is to be monitored throughout the process.

## D.	VPI Procedure

- Pour the mixed components into the epoxy fill tank and seal the lid.

- Open valve V15 and apply a vacuum to the mixed epoxy components.  Maintain a 2-3 Torr vacuum on the epoxy until the boiling (degassing) of the mixture has subsided (Test Directors discretion).

- Close valve V15 and vent the epoxy tank to atmosphere.

- Open valves V2, V3, V4 and 5.

- Slowly open valve V1 to allow the epoxy to enter the lower end of the mold via sprues A, B,F and G.

- Continue until epoxy resin is exiting sprue C, H and K.  (Test Directors discretion)

- Close valve V8 if exiting H and open valve V6.

- Close valve V9 if exiting C and open Valve V7.

- Close Valve 18 if exiting K

- Continue filling the bag mold until epoxy is observed exiting sprues D, E, H and I.  Allow 24 to 36 inches of epoxy to fill each line.  Close valves V10, V11, V12, V13 and V14.  Vent the overfill tank.

- Close valve V17 and SLOWLY vent the vacuum oven.

- The Test Director may elect to milk the epoxy through the mold following filling.  The pressures in the mold and vacuum should closely match. The following steps should be followed for the “Milking Process”.

  - Open valves V1, V2, V3, V4, V8, V9, V10, V11, V12, V13 and V14, and open the vent on the fill tank.  Close valve V6 & V7.

  - Slowly apply pressure to the overfill tank and vacuum oven to a maximum of 3 psig, keeping the pressure equal.

  - This will allow epoxy to flow from the overfill lines back through the coil.   DO NOT allow any of the air (nitrogen) in the overfill lines to re-enter the mold.

  - Reverse this process by slowly venting the overfill tank and applying the pressure to the fill tank.

  - Repeat this step as required.  (Test Directors discretion)

  - Once finished, slowly vent the tanks and oven.

  - Close valves V1, V2, V3, V4 and V5.

- Once the Test Director feels that the impregnation of the Tee specimen is complete, begin to slowly ramp up the oven temperature to 110 degrees C cure temperature at a ramp-up rate of 20 degrees per hour.

- During the entire cure process, maintain a 3 psig pressure inside of the vacuum oven.

- Maintain the oven temperature for 5 hours at 110 degrees C.

- During this process the viscosity samples should periodically checked until the samples GEL.

- After 5 hours at 110 degrees C, ramp-up the oven to 125 degrees C.

- Maintain the oven temperature for 15 hours at 125 degrees C.

- At the end of the cure cycle, shut off the oven, and allow the mold to return to room temperature. DO NOT open the oven until the mold has returned to a temperature of at least 40 degrees C.

- Remove the mold from the oven.

- CAREFULLY open up the mold and examine the impregnated Tee specimen.

#### VPI DATA SHEET

________________________________________________________________________

## Date of Test:				Test Director:

Team Members: ________________________________________________________________________

EPOXY MIX DATA

Weight of components-	Part A

Part B

Part C

Mixing time:

VACUUM READINGS:

Mold prior to impregnation:

Degassing of epoxy:

During VPI process:

Oven:					Mold:

During the Cure Cycle (Oven):

PROCESS TIMES:

Start of Degassing operation:	_________	End of Degassing operation: __________

Start of Epoxy Fill: _____________	End of Epoxy Fill: ______________

Start of Ramp Up: ______________	Cure Temp. Reached: ________ (110 deg. C)

Start of Ramp Up: ______________	Post Cure Temp. Reached: ________ (125 deg. C)

End of Cure Cycle: __________________

NOTES and OBSERVATIONS:

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

OVEN DATA SHEET:            	Date: _______________  	Sheet No. ________

| Time | Temperature Degrees C | Notes | Time | Temperature Degrees C | Notes |
| --- | --- | --- | --- | --- | --- |

NOTES AND OBSERVATIONS

# Text boxes

Figure No. 1

V

P

[1]

[2]

[6]

[7]

[3]

[5]

[4]

Epoxy enters the mold cavity through the Feed Sprues

0.014 in.

0.040 in.

0.054 in.