#### Phelps Dodge Copper Products Company

Quality Assurance/Customer Technical Assistance Group

41 Wawecus Street, Norwich, Connecticut 06360

Office: (860) 859-5926 . Fax: (860) 859-5930 . Cell: (860) 334-4164 . pcaselli@phelpsdodge.com

Certificate of Chemical Analysis

Date:	October 28, 2004

To:	Mike Adams – New England Wire

From:	Phil Caselli – Phelps Dodge

Order Number: 28302

Material: C10100 Oxygen Free Rod

Analyses on the coils given below were performed on a Thermo Jarrell Ash Atom Comp 2000 DC Arc CID Spectrograph, LECO RO300 Oxygen Analyzer, and a LECO S-400 Sulfur Analyzer.  The rod meets or exceeds the requirements of the latest revision of ASTM B 49.

Chemical Analysis

Date of Analysis 10/28/04

| Coil# | As | Bi | Cd | Fe | Ni | Pb | Sb | Se | Sn | Te | Ag | S | O |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23000260 | nd | 0.1 | nd | nd | nd | nd | nd | nd | nd | nd | 6.7 | 5.0 | 1 |
| 23000261 | nd | 0.1 | nd | nd | nd | nd | nd | nd | nd | nd | 6.7 | 5.0 | 1 |
| 23000289 | nd | 0.2 | nd | nd | nd | nd | nd | nd | nd | nd | 6.2 | 6.0 | 1 |
| 23000293 | nd | 0.1 | nd | nd | nd | nd | nd | nd | nd | nd | 4.9 | 6.0 | 1 |
| 23000298 | nd | 0.2 | nd | nd | nd | nd | nd | nd | nd | nd | 6.6 | 6.0 | 2 |

All values expressed as PPM.

nd = Not Detected

Philip F. Caselli

Manager, QA/CTAG