CTD-101 and CTD-101K

Epoxy Resin System

High Performance Resins for Cryogenic and Radiation Applications

¥	An anhydride cured epoxy system that was developed and tested for cryogenic applications down to liquid helium temperatures (-269oC/-452oF) as well as for its resistance to high energy radiation.

¥	Sets the performance standards in cryogenic and high radiation applications and is backed by performance data that meet all applicable test specifications.

¥	Good room temperature performance and handling characteristics: low viscosity and long pot-life.

¥	Non-carcinogenic resin system with very low toxicity. It is a non-solvent based system, and will not give off volatiles on cure.

¥	Wide range of properties and applications:

101 	is the basic system;

101K 	improved wetting and excellent impregnation of large coils

with highly tortuous paths.

Chemical Description	Diglycidyl Ether of Bisphenol-A (DGEBA) with anhydride curing agent.

Cure: 				1 1/2 hrs at 135¡ C; No Post Cure or

5 hrs at 110¡ C with a post cure of 16 hrs at 126¡ C

Other cure schedules available upon request

Process Compatabilities		Filament winding (FW)

Resin Transfer Molding (RTM)

Vacuum Pressure Impregnation (VPI)

Casting with or without filler

Advantages				* Non-Carcinogenic

* Low Toxicity

* Long Pot-Life, 60 hours at 40¡ C

* Low Viscosity, 400 cP at 40¡  C

* Excellent adhesion to fibers and fillers

* Specific Gravity  1.1 g/cc

* Mixing Temperature 40 - 60¡  C

MATERIAL PROPERTIES AT LIQUID NITROGEN TEMPERATURE (76 K)

PROPERTY

Compression Strength

Compression Modulus

Short Beam Shear Strength

Shear Modulus

Torsion Shear Strength

(3.2 mm rods)

Coefficient of Thermal Expansion

Viscosity @ 65oC

CTD-101A

60% S-2 Glass

[0,90] laminate

1400 MPa

(through thickness)

18 GPa

127 MPa

23 GPa

208 MPa

N/A

100 Cp

CTD-101K

50% S-2 Glass

[0,90] laminate

1300 MPa

(through thickness)

16.7 GPa

108 MPa

27.9 GPa

N/A

8.44 10-6 m/m-K

(300 K to 4 K)

<100 Cp

CTD-101K, with 50% vf [0.90] weave S-2ª Glass, Through Thickness: Unirradiated

Temperature

[K]

Compression Stress

| [MPa] | Compression Modulus [GPa] |
| --- | --- |

Strain to Failure

| [%] |
| --- |
| 295 | 790 | 12.9 | 6.15 |

Disclaimer:  The information and recommendations contained herein are based upon data believed to be accurate. However, no guarantee or warranty of any kind expressed or implied is made with respect to the information contained herein.

Room Temperature Performance of CTD-101 Resin

CTD-101A - Neat Resin: Unirradiated (Torsional Shear)

| Temperature [K] | Shear Strength [MPa] | Shear Modulus [GPa] | Shear Strain [radians] |
| --- | --- | --- | --- |
| 295 | 85 | 1.35 | 0.083 |
| 77 | 155 | 2.4 | 0.06 |

CTD-101A, with 50% vf unidirectional S-2ª Glass Fibers: Unirradiated

(Torsional Shear)

Temperature [K]

Shear Strength

[MPa]

Shear Modulus

[GPa]

Shear Strain

[radians]

Fracture Resistance

| G1C [KN/m] |
| --- |
| 295 | 103 | 5.2 | 0.096 | 0.43 |
| 77 | 201 | 9.1 | 0.039 | 0.36 |

CTD-101K, with 50% vf [0.90] weave S-2ª Glass, Through Thickness: Unirradiated

Temperature

[K]

Compression Strength

[MPa]

Compression Modulus

[GPa]

Strain to Failure

| [%] |
| --- |
| 295 | 790 | 12.9 | 6.15 |

Effect of Radiation at 330K on Torsion Properties (Tested at 77K)

Radiation

| [Rads] | Torsional Shear Strength [MPa] | Torsional Shear Modulus [GPa] |
| --- | --- | --- |

Torsional Shear

Strain [MPa]

Fracture Resistance

| G1C [KN/m] |
| --- |
| 0.00 | 201 | 9.1 | 0.039 | 0.36 |
| 4.7 x 108 | 161 | 7.7 | 0.029 | 0.28 |
| 4.7 x 109 | 93 | 8.4 | 0.015 | 0.15 |
| 2.3 x 1010 | 92 | 8.7 | 0.013 | 0.16 |